DIODE, SILICON, POWER SCHOTTKY RECTIFIER, BASED ON TYPE 1N5819

ESCC Detail Specification No. 5106/021

2.8 POWER BURN-IN CONDITIONS

For Variants 01, 04 01 to 04

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | Note1 | °C |
| Junction Temperature | Tj | +100 minimum | °C |
| Forward Current | IF | 1 minimum (Note 1) | A |

For Variants 02, 03

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +22 (+/-3) | °C |
| Junction Temperature | Tj | +150 (+0 -5) | °C |
| Average Output Rectified Current | IO | Note 2 | A |

NOTES:

1. IF and/or Tamb may be adjusted, within the given limit range, to attain the specified junction

temperature.

2. IO may be adjusted, within the given limit range, to attain the specified junction temperature.

Justification:

STMicroelectronics wishes apply the same condition that variant 01 and 04

2.9 OPERATING LIFE CONDITIONS

For Variants 01, 04 01 to 04

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | Note1 | °C |
| Junction Temperature | Tj | +125 minimum | °C |
| Forward Current | IF | 1 minimum (Note 1) | A |

For Variants 02, 03

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +22 (+/-3) | °C |
| Junction Temperature | Tj | +150 (+0 -5) | °C |
| Average Output Rectified Current | IO | Note 2 | A |

NOTES:

1. IF and/or Tamb may be adjusted, within the given limit range, to attain the specified junction

temperature.

2. IO may be adjusted, within the given limit range, to attain the specified junction temperature.

Justification:

STMicroelectronics wishes apply the same condition that variant 01 and 04

1.6 HANDLING PRECAUTIONS

These devices are susceptible to damage by electrostatic discharge. Therefore, suitable precautions shall be employed for protection during all phases of manufacture, testing, packaging, shipment and any handling.

Variants 01 and 04 are categorised as Class 2 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 2000 Volts.

Variants 02 and 03 are categorised as Class 3 2 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 8000 2000 Volts.

Justification:

Typing error during the first release.