Page 1 of 13

CAPACITORS, FIXED, CHIPS, CERAMIC DIELECTRIC, TYPE I

BASED ON TYPE 0805

ESCC Detail Specification No. 3009/003

| Issue 6 Draft C | April 2015 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# LEGAL DISCLAIMER AND COPYRIGHT

European Space Agency, Copyright © 2015. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| 732 | Specification updated to incorporate changes per DCR. Specification produced in MSWORD. Changes in presentation are possible. |

TABLE OF CONTENTS

1	GENERAL	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants and Range of Components	6

1.5	MAXIMUM RATINGS	8

1.6	PHYSICAL DIMENSIONS	8

1.7	FUNCTIONAL DIAGRAM	8

2	REQUIREMENTS	9

2.1	GENERAL	9

2.1.1	Deviations from the Generic Specification	9

2.2	MARKING	9

2.3	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	10

2.3.1	Room Temperature Electrical Measurements	10

2.3.2	High and Low Temperatures Electrical Measurements	10

2.4	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	11

2.5	BURN-IN	12

APPENDIX A	13

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3009.

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 30090030110C0JE

Detail Specification Reference: 3009003

Component Type Variant Number: 01 (as required)

Characteristic code: Capacitance Value (10pF): 10C0 (as required)

Characteristic code: Capacitance Tolerance (±5%): J (as required)

Rating code: Rated Voltage (100V): E (as required)

#### Characteristics and Ratings Codes

Characteristics and ratings to be codified as part of the ESCC Component Number shall be as follows:

Rated Capacitance Value Cn expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be picofarad (pF).

| Capacitance Value Cn (pF) | Code |
| --- | --- |
| X.XX | XCXX |
| XX.X | XXCX |
| XXX | XXX0 |
| XXX 101 | XXX1 |

Capacitance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (±) | Code Letter |
| --- | --- |
| 0.25pF | C |
| 0.5pF | D |
| 1% | F |
| 2% | G |
| 5% | J |
| 10% | K |

Rated Voltage expressed by the following codes:

| Rated Voltage (V) | Code Letter |
| --- | --- |
| 16 | X |
| 25 | A |
| 50 | C |
| 100 | E |
| 200 | G |

### Component Type Variants and Range of Components

The component type variants and range of components applicable to this specification are as follows:

| Variant Number | Style | Capacitance Range, Tolerance, Rated Voltage | Terminal Material and Finish |  | Weight Max (g) |
| --- | --- | --- | --- | --- | --- |
|  |  |  | End Terminations | Termination Finish |  |
| 01 | 0805 | See Note 1 | Ag/Pd | No finish (Note 2) | 0.1 |
| 03 | 0805 | See Note 1 | Ag/Pd/Pt | No finish (Note 2) | 0.1 |
| 05 | 0805 | See Note 1 | Ag + Ni barrier | Sn60, Sn62 or Sn63 solder dip | 0.1 |
| 06 | 0805 | See Note 1 | Ag + Ni barrier | Sn/Pb plating (Note 3) | 0.1 |
| 08 | 0805 | See Note 1 | Ag + Ni barrier | Au plating (Note 2) | 0.1 |

NOTES:

Available rated voltages, capacitance values and tolerances are as follows:

| Rated Voltage UR (V) | Capacitance Range Cn (pF) |  | Tolerance (±) | Value Series |
| --- | --- | --- | --- | --- |
|  | Min | Max |  |  |
| 200 | 1 | 9.1 | 0.25pF | E24 |
|  |  | 8.2 | 0.5pF | E12 |
|  | 10 | 681 | 1% | E96 |
|  |  |  | 2% | E48 |
|  |  | 680 | 5% | E24 |
|  |  |  | 10% | E12 |
| 100 | 1 | 9.1 | 0.25pF | E24 |
|  |  | 8.2 | 0.5pF | E12 |
|  | 10 | 1500 | 1% | E96 |
|  |  | 1540 | 2% | E48 |
|  |  | 1500 | 5% | E24 |
|  |  |  | 10% | E12 |
| 50 | 1 | 9.1 | 0.25pF | E24 |
|  |  | 8.2 | 0.5pF | E12 |
|  | 10 | 1780 | 1% | E96 |
|  |  |  | 2% | E48 |
|  |  | 1800 | 5% | E24 |
|  |  |  | 10% | E12 |
| 25 | 1 | 9.1 | 0.25pF | E24 |
|  |  | 8.2 | 0.5pF | E12 |
|  | 10 | 2210 | 1% | E96 |
|  |  | 2260 | 2% | E48 |
|  |  | 2200 | 5% | E24 |
|  |  |  | 10% | E12 |
| 16 | 1 | 9.1 | 0.25pF | E24 |
|  |  | 8.2 | 0.5pF | E12 |
|  | 10 | 2670 | 1% | E96 |
|  |  | 2740 | 2% | E48 |
|  |  | 2700 | 5% | E24 |
|  |  |  | 10% | E12 |

- Any capacitance value in the capacitance range may be available on request.

Variants 01, 03 and 08 are not suitable for solder assembly methods. They shall be assembled using glue or wire bond techniques.

Sn/Pb plating with minimum 10% Pb.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Rated Voltage | UR | 16, 25, 50, 100, 200 | V | Note 1 |
| Operating Temperature Range | Top | -55 to +125 | °C | Without derating. Tamb |
| Storage Temperature Range | Tstg | -55 to +125 | °C |  |
| Soldering Temperature | Tsol | +260 | °C | Note 2 |

NOTES:

As required; See Component Type Variants and Range of Components.

Duration 10 seconds maximum.

## PHYSICAL DIMENSIONS

| Symbols | Dimensions (mm) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Variants 01, 03, 06, 08 |  | Variant 05 |  |
|  | Min | Max | Min | Max |
| L | 1.7 | 2.3 | 1.7 | 2.8 |
| l | 1.05 | 1.45 | 1.05 | 1.95 |
| e | - | 1.8 | - | 2.3 |
| M | 0.1 | 0.75 | 0.1 | 0.75 |

## FUNCTIONAL DIAGRAM

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Qualification and Periodic Tests (Chart F4)

Solderability: not applicable to Variants 01, 03 and 08.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and as follows.

The information to be marked on the component or its primary package shall be:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

Electrical measurements shall be performed at room, high and low temperatures.

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | Test Method and Conditions | Tolerance (±) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Capacitance | CA | ESCC No. 3009 |  |  |  | pF |
|  |  |  | 0.25pF | Cn -0.25 | Cn +0.25 |  |
|  |  |  | 0.5pF | Cn -0.5 | Cn +0.5 |  |
|  |  |  | 1% | 0.99Cn | 1.01Cn |  |
|  |  |  | 2% | 0.98Cn | 1.02Cn |  |
|  |  |  | 5% | 0.95Cn | 1.05Cn |  |
|  |  |  | 10% | 0.9Cn | 1.1Cn |  |
| Tangent of Loss Angle | tgδ | ESCC No. 3009 | All |  |  |  |
|  |  | For Cn < 50pF |  | - | Note 1 |  |
|  |  | For Cn ≥ 50pF |  | - | 15 x10-4 | - |
| Insulation Resistance | RI | ESCC No. 3009 | All | 100 | - | GΩ |
| Voltage Proof | VP | ESCC No. 3009 | All | 2.5UR | - | V |

NOTES:

For Cn < 50pF, tgδ < 1.5 x (150/Cn + 7) x10-41.5150Cn+7×10-4, where the unit quantity for Cn is in pF.

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | Test Method and Conditions (Note 1) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Temperature Coefficient | TC | ESCC No. 3009 Tamb = -55 ±2°C, +20 ±2°C, +125 ±2°C Note 2 |  |  | 10-6/°C |
|  |  | For Cn > 20pF | -30 | +30 |  |
|  |  | For Cn ≤ 20pF | Note 3 |  |  |

NOTES:

The measurements shall be performed on a sample of 5 components from each manufacturing lot with 0 failures allowed. In the event of any failure a 100% inspection may be performed.

In the case of a 100% inspection, a 1% total percent defective is allowed.

Temperature Coefficient is not specified for Cn ≤ 20pF due to test equipment limitations.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

Unless otherwise specified the test methods and test conditions shall be as per the corresponding test defined in Room Temperature Electrical Measurements.

| Test Reference per ESCC No. 3009 | Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |  |
| Mounting |  |  |  |  |  |  |
| Final Measurements | Capacitance | CA | Record Values |  |  |  |
|  | Tangent of Loss Angle | tgδ | Note 1 |  |  |  |
|  | Insulation Resistance | RI | 100 |  | - | GΩ |
| Rapid Change of Temperature |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Notes 1, 2 |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -1 |  | +1 | pF or |
|  |  |  | -1 |  | +1 | % |
|  |  |  |  |  |  | (Note 3) |
|  | Tangent of Loss Angle | tgδ | Note 4 |  |  |  |
| Steady State Humidity (85/85) |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Note 1 |  |  |  |
| Final Measurements (1000 hours) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -1 |  | +1 | pF or |
|  |  |  | -2 |  | +2 | % |
|  |  |  |  |  |  | (Note 3) |
|  | Tangent of Loss Angle | tgδ | Note 4 |  |  |  |
|  | Insulation Resistance (Note 5) | RI | 10 |  | - | GΩ |
| Operating Life |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Notes 1, 2 |  |  |  |
| Intermediate Measurements (1000 hours) (Note 6) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -1 |  | +1 | pF or |
|  |  |  | -3 |  | +3 | % |
|  |  |  |  |  |  | (Note 3) |
|  | Insulation Resistance | RI | 10 |  | - | GΩ |
| Final Measurements (1000 or 2000 hours) (Note 7) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -1 |  | +1 | pF or |
|  |  |  | -3 |  | +3 | % |
|  |  |  |  |  |  | (Note 3) |
|  | Tangent of Loss Angle | tgδ | Note 4 |  |  |  |
|  | Insulation Resistance | RI | 10 |  | - | GΩ |
|  | Voltage Proof | VP | 2.5UR |  | - | V |
| Capacitance-Temperature Characteristics | Temperature Coefficient | TC | Note 8 |  |  |  |
| Robustness of Terminations |  |  |  |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |

NOTES:

As specified in Room Temperature Electrical Measurements.

Capacitance values recorded during Mounting may be used as initial measurements.

Whichever is greater.

Twice the value specified in Room Temperature Electrical Measurements.

Test conditions for Insulation Resistance shall be as specified in Steady State Humidity in the ESCC Generic Specification.

Intermediate measurements are optional at the Manufacturer’s discretion.

1000 hours is applicable to Periodic Testing for extension of qualification. 2000 hours is applicable to Qualification Testing, and to Periodic Testing for renewal of qualification after lapse.

As specified in High and Low Temperatures Electrical Measurements.

## BURN-IN

The requirements for Burn-in are specified in the ESCC Generic Specification. The following conditions shall also apply:

After Burn-in, the components shall be removed from the chamber and allowed to cool under normal atmospheric conditions for recovery for 24 hours minimum.

## APPENDIX A

AGREED DEVIATIONS FOR AVX/TPC (F)

| Items Affected | Description of Deviations |
| --- | --- |
| Deviations from Generic Specification: Screening Tests (Chart F3) | High and Low Temperatures Electrical Measurements: Temperature Coefficient may be replaced with data provided by the ceramic material supplier, using AVX/TPC production documents 1J-ICONTDIE-630L and 1J-ICONTDIE-900L (issues as per PID). |