Page 1 of 16

R.F. INDUCTORS, FIXED, MINIATURE, MOULDED, SMD

BASED ON SERIES MSCI 10K, 12K, 20K AND H01

ESCC Detail Specification No. 3201/008

| Issue 7 Draft B | June 2016 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2016. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| TBA | Specification upissued to incorporate changes per DCR. |

TABLE OF CONTENTS

1	General	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.1.1	Characteristics Codes	5

1.4.2	Component Type Variants and Range of Components	6

1.5	MAXIMUM RATINGS	10

1.6	PHYSICAL DIMENSIONS	11

1.7	FUNCTIONAL DIAGRAM	11

1.8	MATERIALS AND FINISHES	11

1.8.1	Case	11

1.8.2	Terminals	12

2	REQUIREMENTS	12

2.1	GENERAL	12

2.1.1	Deviations from the Generic Specification	12

2.1.1.1	Deviations from Qualification and Periodic Tests (Chart F4)	12

2.2	MARKING	12

2.3	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	13

2.3.1	Room Temperature Electrical Measurements	13

2.3.2	High and Low Temperatures Electrical Measurements	13

2.4	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	14

2.5	BURN-IN CONDITIONS	15

2.6	OPERATING LIFE CONDITIONS	15

# General

## SCOPE

This specification details the ratings, physical and electrical characteristics and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3201.

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 3201008014L7K

Detail Specification Reference: 3201008

Component Type Variant Number: 01 (as required)

Characteristic code: Inductance Value (4.7µH): 4L7 (as required)

Characteristic code: Inductance Tolerance (±10%): K (as required)

#### Characteristics Codes

Characteristics to be codified as part of the ESCC Component Number shall be as follows:

Inductance Value expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be microhenries (µH):

| Inductance Value L (µH) | Code |
| --- | --- |
| 0.0XX | L0XX |
| 0.XX | LXX |
| X.X | XLX |
| XX | XX0 |
| XX 101 | XX1 |
| XX 102 | XX2 |

Inductance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (± %) | Code Letter |
| --- | --- |
| 2 | G |
| 5 | J |
| 10 | K |
| 15 | L |

### Component Type Variants and Range of Components

The component type variants and range of components applicable to this specification are as follows:

| Variant Number | Type | Case Size (1) | Terminal Finish (2) | Weight Max (g) |
| --- | --- | --- | --- | --- |
| 01 | 10K | A | Au | 0.2 |
|  | 12K | B | Au | 0.2 |
| 02 | 10K | A | SnPb | 0.2 |
|  | 12K | B | SnPb | 0.2 |
| 03 | 20K | C | Au | 0.5 |
| 04 | 20K | C | SnPb | 0.5 |
| 05 | H01 | C | SnPb | 0.5 |

Range of Components – Variants 01, 02 (10K Series)

| Inductance L (µH) | Tolerance ± % | Q Min Q | L & Q Test Frequency ft (MHz) | Self- Resonant Frequency Min fr (MHz) | DC Resistance Max Rdc (Ω) | Rated DC Current IR (mA) | Case Size (1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.01 | 10 | 60 | 150 | 1000 | 0.025 | 750 | A |
| 0.012 | 10 | 60 | 150 | 1000 | 0.025 | 750 | A |
| 0.015 | 10 | 60 | 150 | 1000 | 0.025 | 750 | A |
| 0.018 | 10 | 60 | 150 | 1000 | 0.025 | 750 | A |
| 0.022 | 5, 10 | 51 | 100 | 1000 | 0.025 | 750 | A |
| 0.027 | 5, 10 | 51 | 100 | 1000 | 0.03 | 750 | A |
| 0.033 | 5, 10 | 47 | 100 | 1000 | 0.04 | 640 | A |
| 0.039 | 5, 10 | 47 | 100 | 1000 | 0.05 | 600 | A |
| 0.047 | 5, 10 | 47 | 100 | 1000 | 0.06 | 550 | A |
| 0.056 | 5, 10 | 47 | 100 | 900 | 0.065 | 520 | A |
| 0.068 | 5, 10 | 47 | 100 | 900 | 0.085 | 480 | A |
| 0.082 | 5, 10 | 47 | 100 | 750 | 0.115 | 470 | A |
| 0.1 | 10 | 47 | 50 | 620 | 0.07 | 470 | A |
| 0.12 | 10 | 47 | 50 | 540 | 0.07 | 470 | A |
| 0.15 | 10 | 47 | 50 | 450 | 0.075 | 450 | A |
| 0.18 | 10 | 51 | 50 | 400 | 0.095 | 430 | A |
| 0.22 | 10 | 51 | 50 | 380 | 0.155 | 350 | A |
| 0.27 | 10 | 51 | 50 | 340 | 0.18 | 310 | A |
| 0.33 | 10 | 51 | 50 | 280 | 0.195 | 280 | A |
| 0.39 | 10 | 47 | 50 | 240 | 0.21 | 240 | A |
| 0.47 | 5, 10 | 47 | 25 | 210 | 0.225 | 230 | A |
| 0.56 | 5, 10 | 52 | 25 | 180 | 0.245 | 220 | A |
| 0.68 | 5, 10 | 52 | 25 | 160 | 0.265 | 210 | A |
| 0.82 | 5, 10 | 52 | 25 | 130 | 0.29 | 200 | A |
| 1 | 5, 10 | 52 | 25 | 110 | 0.34 | 190 | A |
| 1.2 | 2, 5, 10 | 42 | 7.9 | 110 | 0.55 | 180 | A |
| 1.5 | 2, 5, 10 | 42 | 7.9 | 100 | 0.73 | 160 | A |
| 1.8 | 2, 5, 10 | 48 | 7.9 | 95 | 0.92 | 150 | A |
| 2.2 | 2, 5, 10 | 48 | 7.9 | 90 | 1.1 | 140 | A |
| 2.7 | 2, 5, 10 | 48 | 7.9 | 65 | 1.25 | 130 | A |
| 3.3 | 2, 5, 10 | 48 | 7.9 | 55 | 1.7 | 120 | A |
| 3.9 | 2, 5, 10 | 48 | 7.9 | 45 | 2 | 110 | A |
| 4.7 | 2, 5, 10 | 48 | 7.9 | 43 | 2.3 | 100 | A |
| 5.6 | 2, 5, 10 | 48 | 7.9 | 40 | 2.5 | 100 | A |
| 6.8 | 2, 5, 10 | 46 | 7.9 | 38 | 2.6 | 98 | A |
| 8.2 | 2, 5, 10 | 46 | 7.9 | 35 | 2.8 | 95 | A |
| 10 | 2, 5, 10 | 46 | 7.9 | 33 | 2.8 | 87 | A |

Range of Components – Variants 01, 02 (12K Series)

| Inductance L (µH) | Tolerance ± % | Q Min Q | Test Frequency ft (MHz) | Self- Resonant Frequency Min fr (MHz) | DC Resistance Max Rdc (Ω) | Rated DC Current IR (mA) | Case Size (1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 12 | 2, 5, 10 | 42 | 2.5 | 26 | 2 | 110 | B |
| 15 | 2, 5, 10 | 44 | 2.5 | 24 | 2.2 | 105 | B |
| 18 | 2, 5, 10 | 44 | 2.5 | 21 | 2.8 | 100 | B |
| 22 | 2, 5, 10 | 48 | 2.5 | 20 | 3.5 | 85 | B |
| 27 | 2, 5, 10 | 49 | 2.5 | 19 | 4.3 | 75 | B |
| 33 | 2, 5, 10 | 50 | 2.5 | 14 | 5.5 | 68 | B |
| 39 | 2, 5, 10 | 52 | 2.5 | 12 | 6.5 | 61 | B |
| 47 | 2, 5, 10 | 53 | 2.5 | 11 | 8.5 | 54 | B |
| 56 | 2, 5, 10 | 56 | 2.5 | 10 | 12 | 46 | B |
| 68 | 2, 5, 10 | 53 | 2.5 | 9 | 13 | 42 | B |
| 82 | 2, 5, 10 | 49 | 2.5 | 8 | 15 | 40 | B |
| 100 | 2, 5, 10 | 49 | 2.5 | 7 | 18 | 36 | B |
| 120 | 2, 5, 10 | 37 | 0.79 | 6 | 21 | 34 | B |
| 150 | 2, 5, 10 | 30 | 0.79 | 5 | 26 | 31 | B |
| 180 | 2, 5, 10 | 30 | 0.79 | 5 | 28 | 29 | B |
| 220 | 2, 5, 10 | 26 | 0.79 | 4.5 | 32 | 28 | B |
| 270 | 2, 5, 10 | 26 | 0.79 | 4 | 36 | 26 | B |
| 330 | 2, 5, 10 | 24 | 0.79 | 3.7 | 42 | 24 | B |
| 390 | 2, 5, 10 | 24 | 0.79 | 3.5 | 46 | 23 | B |
| 470 | 2, 5, 10 | 24 | 0.79 | 3 | 68 | 19 | B |
| 560 | 2, 5, 10 | 22 | 0.79 | 2.8 | 77 | 18 | B |
| 680 | 2, 5, 10 | 20 | 0.79 | 2.5 | 85 | 17 | B |
| 820 | 2, 5, 10 | 16 | 0.79 | 2 | 100 | 16 | B |
| 1000 | 2, 5, 10 | 12 | 0.79 | 1.5 | 120 | 15 | B |

Range of Components – Variants 03, 04 (20K Series)

| Inductance L (µH) | Tolerance ± % | Q Min Q | Test Frequency ft (MHz) | Self- Resonant Frequency Min fr (MHz) | DC Resistance Max Rdc (Ω) | Rated DC Current IR (mA) | Case Size (1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.010 | 10 | 60 | 150 | 1000 | 0.04 | 1000 | C |
| 0.012 | 10 | 70 | 150 | 1000 | 0.04 | 1000 | C |
| 0.015 | 10 | 75 | 150 | 1000 | 0.04 | 1000 | C |
| 0.018 | 10 | 75 | 150 | 1000 | 0.04 | 1000 | C |
| 0.022 | 10 | 60 | 100 | 1000 | 0.05 | 1000 | C |
| 0.027 | 10 | 60 | 100 | 1000 | 0.05 | 1000 | C |
| 0.033 | 10 | 60 | 100 | 1000 | 0.05 | 1000 | C |
| 0.039 | 10 | 60 | 100 | 1000 | 0.06 | 900 | C |
| 0.047 | 10 | 65 | 100 | 800 | 0.06 | 900 | C |
| 0.056 | 10 | 65 | 100 | 760 | 0.06 | 900 | C |
| 0.068 | 10 | 65 | 100 | 700 | 0.07 | 840 | C |
| 0.082 | 10 | 65 | 100 | 650 | 0.07 | 840 | C |
| 0.1 | 10 | 65 | 50 | 570 | 0.07 | 840 | C |
| 0.12 | 10 | 65 | 50 | 520 | 0.07 | 840 | C |
| 0.15 | 10 | 75 | 50 | 400 | 0.08 | 790 | C |
| 0.18 | 10 | 75 | 50 | 360 | 0.08 | 790 | C |
| 0.22 | 10 | 70 | 50 | 320 | 0.08 | 790 | C |
| 0.27 | 10 | 70 | 50 | 270 | 0.1 | 700 | C |
| 0.33 | 10 | 70 | 50 | 240 | 0.1 | 700 | C |
| 0.39 | 10 | 70 | 50 | 220 | 0.1 | 700 | C |
| 0.47 | 10 | 70 | 25 | 190 | 0.14 | 590 | C |
| 0.56 | 10 | 70 | 25 | 170 | 0.19 | 510 | C |
| 0.68 | 10 | 70 | 25 | 160 | 0.26 | 430 | C |
| 0.82 | 10 | 75 | 25 | 150 | 0.3 | 400 | C |
| 1 | 10 | 75 | 25 | 130 | 0.34 | 380 | C |
| 1.2 | 10 | 65 | 7.9 | 120 | 0.45 | 330 | C |
| 1.5 | 10 | 65 | 7.9 | 110 | 0.57 | 290 | C |
| 1.8 | 10 | 65 | 7.9 | 100 | 0.72 | 260 | C |
| 2.2 | 10 | 65 | 7.9 | 80 | 0.9 | 230 | C |
| 2.7 | 10 | 65 | 7.9 | 60 | 1.1 | 210 | C |
| 3.3 | 10 | 60 | 7.9 | 50 | 1.2 | 200 | C |
| 3.9 | 10 | 60 | 7.9 | 45 | 1.4 | 180 | C |
| 4.7 | 10 | 60 | 7.9 | 42 | 1.6 | 170 | C |
| 5.6 | 10 | 65 | 7.9 | 40 | 1.8 | 160 | C |
| 6.8 | 10 | 65 | 7.9 | 37 | 2.4 | 140 | C |
| 8.2 | 10 | 65 | 7.9 | 34 | 3 | 130 | C |
| 10 | 10 | 65 | 7.9 | 29 | 3.5 | 120 | C |
| 12 | 10 | 60 | 2.5 | 27 | 3.6 | 118 | C |
| 15 | 10 | 60 | 2.5 | 22 | 3.7 | 115 | C |
| 18 | 10 | 60 | 2.5 | 17 | 3.8 | 114 | C |
| 22 | 10 | 60 | 2.5 | 16 | 3.9 | 113 | C |
| 27 | 10 | 65 | 2.5 | 15 | 4 | 110 | C |
| 33 | 10 | 65 | 2.5 | 14 | 5 | 100 | C |
| 39 | 10 | 65 | 2.5 | 13 | 7 | 84 | C |
| 47 | 10 | 70 | 2.5 | 12 | 8 | 79 | C |
| 56 | 10 | 70 | 2.5 | 11 | 10 | 70 | C |
| 68 | 10 | 65 | 2.5 | 10 | 11 | 67 | C |
| 82 | 10 | 60 | 2.5 | 9 | 12 | 64 | C |
| 100 | 10 | 60 | 2.5 | 8 | 13 | 62 | C |
| 120 | 10 | 40 | 0.79 | 7 | 14 | 59 | C |
| 150 | 10 | 40 | 0.79 | 6 | 16 | 56 | C |
| 180 | 10 | 40 | 0.79 | 5 | 18 | 52 | C |
| 220 | 10 | 40 | 0.79 | 4 | 24 | 45 | C |
| 270 | 10 | 40 | 0.79 | 3.3 | 25 | 44 | C |
| 330 | 10 | 40 | 0.79 | 3.1 | 29 | 41 | C |
| 390 | 10 | 40 | 0.79 | 2.9 | 32 | 39 | C |
| 470 | 10 | 35 | 0.79 | 2.4 | 35 | 37 | C |
| 560 | 10 | 35 | 0.79 | 2.1 | 45 | 33 | C |
| 680 | 10 | 35 | 0.79 | 1.9 | 55 | 30 | C |
| 820 | 10 | 30 | 0.79 | 1.8 | 70 | 26 | C |
| 1000 | 10 | 30 | 0.79 | 1.7 | 80 | 25 | C |

Range of Components – Variant 05 (H01 Series)

| Inductance L (µH) | Tolerance ± % | Q Min Q | Test Frequency ft (MHz) | Self- Resonant Frequency Min fr (MHz) | DC Resistance Max Rdc (Ω) | Rated DC Current IR (mA) | Case Size (1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.38 | 15 | 30 | 1 | 8 | 0.029 | 1500 | C |
| 0.67 | 15 | 30 | 1 | 8 | 0.039 | 1250 | C |
| 1 | 15 | 30 | 1 | 8 | 0.054 | 1000 | C |
| 1.5 | 15 | 30 | 1 | 8 | 0.073 | 850 | C |
| 2 | 15 | 30 | 1 | 8 | 0.1 | 700 | C |
| 2.7 | 15 | 30 | 1 | 8 | 0.12 | 620 | C |
| 3.4 | 15 | 30 | 1 | 8 | 0.15 | 550 | C |
| 4.6 | 15 | 30 | 1 | 8 | 0.19 | 490 | C |
| 5.6 | 15 | 30 | 1 | 8 | 0.23 | 440 | C |
| 7.1 | 15 | 30 | 1 | 8 | 0.27 | 410 | C |
| 10 | 15 | 30 | 1 | 8 | 0.39 | 340 | C |
| 12 | 15 | 30 | 1 | 8 | 0.53 | 290 | C |
| 27 | 15 | 30 | 1 | 8 | 1.04 | 200 | C |
| 100 | 15 | 30 | 1 | 8 | 3.8 | 100 | C |

NOTES:

See Physical Dimensions.

See Materials and Finishes for details.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Rated DC Current | IR | Note 1 | mA |  |
| Dielectric Withstanding Voltage | DWV | 200 | Vrms |  |
| Operating Temperature Range | Top | -55 to +125 | °C | Tamb |
| Storage Temperature Range | Tstg | -55 to +125 | °C |  |
| Soldering Temperature | Tsol | +260 | °C | Note 2 |

NOTES:

See Component Type Variants and Range of Components for values.

Duration 5 seconds maximum, the same terminal shall not be resoldered until 3 minutes have elapsed.

## PHYSICAL DIMENSIONS

| Symbols | Dimensions (mm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Case Size A |  | Case Size B |  | Case Size C |  |
|  | Min | Max | Min | Max | Min | Max |
| A | - | 2.8 | - | 2.8 | 3.74 | 4.14 |
| B | - | 2.79 | - | 2.79 | 2.98 | 3.38 |
| C | - | 2.16 | - | 2.54 | - | 3.3 |
| D | 0.62 | 0.9 | 0.62 | 0.9 | 0.7 | 1.02 |
| F | 0.32 | 0.6 | 0.32 | 0.6 | 0.38 | 0.64 |
| G | 0.72 | 1.23 | 0.72 | 1.23 | 1.7 | - |

## FUNCTIONAL DIAGRAM

## MATERIALS AND FINISHES

### Case

As a minimum, a resin moulding shall ensure the inductor’s protection.

### Terminals

The terminal material shall be brass, plated with 2 to 3µm of copper, with either SnPb finish or further underplated with 2 to 3 µm of nickel with Au plated finish, as specified in Component Type Variants and Range of Components.

For Au finish, the gold thickness is dependent on inductance value as follows:

5µm for 0.01 to 1µH.

15µm for 1.2µH to 1mH.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Qualification and Periodic Tests (Chart F4)

Para. 8.11, Mechanical Shock: shall not be performed.

Para. 8.12, Vibration: shall not be performed.

Para. 8.13, Immersion: shall not be performed.

Para. 8.14, Moisture Resistance, Polarisation: there shall be no polarising voltage applied during test.

Para. 8.15, Operating Life, Operating conditions: No load shall be applied.

## MARKING

The marking of all components delivered to this specification shall be in accordance with the requirements of ESCC Basic Specification No. 21700. When the component is too small to accommodate all of the marking specified, as much as space permits shall be marked and the marking information, in full, shall accompany each component in its primary package.

The information to be marked and the order of precedence, shall be as follows:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3 ºC.

| Characteristics | Symbols | ESCC No. 3201 Test Method and Conditions | Tolerance (± %) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Inductance | L | Para. 8.3.1.1 f = ft (Note 1) I = 0Adc | 2 | 0.98 L (1) | 1.02 L (1) | µH |
|  |  |  | 5 | 0.95 L (1) | 1.05 L (1) |  |
|  |  |  | 10 | 0.9 L (1) | 1.1 L (1) |  |
|  |  |  | 15 | 0.85 L (1) | 1.15 L (1) |  |
| Quality Factor | Q | Para. 8.3.1.8 f = ft (Note 1) I = 0Adc | All | (1) | - | - |
| Self-Resonant Frequency | fr | Para. 8.3.1.13 Note 2 | All | (1) | - | MHz |
| DC Resistance | RDC | Para. 8.3.1.2 | All | - | (1) | Ω |
| Insulation Resistance | RI | Para. 8.3.1.3 | All | 1000 | - | MΩ |

NOTES:

See Component Type Variants and Range of Components for values.

Measurement shall be performed on a go-no-go basis.

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | ESCC No. 3201 Test Method and Conditions (Note 1) | Limits |  | Unit |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Inductance Change between -55 (+3 -0)ºC and +22 ± 3 ºC | ΔL/L | Para. 8.3.1.1 | -15 | +10 | % |
| Inductance Change between +125 (+0 -3)ºC and +22 ±3ºC | ΔL/L | Para. 8.3.1.1 | -10 | +15 | % |

NOTES:

Performed only for qualification or qualification maintenance. The measurements shall be performed on a sample of 5 components from the lot with 0 failures allowed. In the event of any failure a 100% inspection may be performed.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3ºC.

Unless otherwise specified the test methods and test conditions shall be as per the corresponding test defined in Room Temperature Electrical Measurements.

| Test Reference per ESCC No. 3201 | Characteristics | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Thermal Shock | DC Resistance | RDC | Note 1 |  | Ω |
| Barometric Pressure |  |  |  |  |  |
| Whilst at low pressure: | Dielectric Withstanding Voltage | DWV | 200 | - | V |
|  | DWV Leakage Current | IL | - | 100 | µA |
| Temperature Rise |  |  |  |  |  |
| Initial Measurements | DC Resistance (at 0.1IR) | RDC | Record Value |  | Ω |
| Final Measurements | DC Resistance (at IR) | RDC | Record Value |  | Ω |
|  | Temperature Rise | ΔT | - | 25 | °C |
| Overload | DC resistance | RDC | Note 1 |  | Ω |
|  | Insulation Resistance | RI | 1000 | - | MΩ |
|  | Dielectric Withstanding Voltage | DWV | 200 | - | V |
|  | DWV Leakage Current | IL | - | 100 | µA |
| Resistance to Soldering Heat | Inductance | L | Note 1 |  | µH |
|  | Quality Factor | Q | Note 1 |  | - |
|  | Self-Resonant Frequency | fr | Note 1 |  | MHz |
|  | DC resistance | RDC | Note 1 |  | Ω |
|  | Dielectric Withstanding Voltage | DWV | 200 | - | V |
|  | DWV Leakage Current | IL | - | 100 | µA |
| Moisture Resistance |  |  |  |  |  |
| Within 30 min of removal from conditioning: | Dielectric Withstanding Voltage | DWV | 200 | - | V |
|  | DWV Leakage Current | IL | - | 100 | µA |
|  | Insulation Resistance | RI | 100 | - | MΩ |
| Within 1 hour of previous measurements: | Inductance | L | Note 1 |  | µH |
|  | Quality Factor | Q | Note 1 |  | - |
|  | Self-Resonant Frequency | fr | Note 1 |  | MHz |
|  | DC resistance | RDC | Note 1 |  | Ω |
| Operating Life |  |  |  |  |  |
| Initial Measurement (0 hour) | Inductance | L | Note 1 |  | µH |
| Intermediate Measurements (1000 hours)(after 30 min recovery) | Dielectric Withstanding Voltage | DWV | 200 | - | V |
|  | DWV Leakage Current | IL | - | 100 | µA |
|  | Inductance Change | ΔL/L | -10 or (2) -5 | +10 or (2) +5 | % |
| Final Measurements (2000 hours)(after 30 min recovery) | Dielectric Withstanding Voltage | DWV | 200 | - | V |
|  | DWV Leakage Current | IL | - | 100 | µA |
|  | Inductance Change | ΔL/L | -10 or (2) -5 | +10 or (2) +5 | % |
|  | Quality Factor | Q | Note 1 |  | - |
|  | Self-Resonant Frequency | fr | Note 1 |  | MHz |
|  | DC resistance | RDC | Note 1 |  | Ω |
|  | Insulation Resistance | RI | 100 | - | MΩ |

NOTES:

See Component Type Variants and Range of Components for values.

L < 0.1μH or L ≥ 0.1 μH respectively.

## BURN-IN CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +125 (+0 -3) | ºC |

NOTES:

After Burn-in, the components shall be removed from the chamber and allowed to cool under normal atmospheric conditions for recovery for 24 hours minimum.

## OPERATING LIFE CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +125 (+0 -3) | ºC |
| DC Current | - | No Load | mA |

APPENDIX A

AGREED DEVIATIONS FOR EXXELIA MAGNETICS (F)

| Items Affected | Description of Deviations |
| --- | --- |
| Deviations from Generic Specification: Qualification and Periodic Tests (Chart F4) | Para. 8.17, Solderability: Final Examination: exposed base metal at the edge of the lead frame is permitted. |
| Characteristics Codes (Para. 1.4.1.1) | For Variants 01, 02, 03 and 04, in addition to the Inductance Value characteristic code used for the ESCC Component Number, Inductance Value may also be marked on the top of the body using three coloured bands as follows. The unit quantity shall be nanohenries (nH): Colour; Significant Figure; Multiplier (nH). Black; 0; 100. Brown; 1; 101. Red; 2; 102. Orange; 3; 103. Yellow; 4; 104. Green; 5; 105. Blue; 6; -. Violet; 7; -. Grey; 8; -. White; 9; -. NOTES: - The first, wider band represents the 1st significant figure. - The second, narrower band represents the 2nd significant figure. - The third, narrower band represents the multiplier. |