Page 1 of 19

CAPACITORS, LEADLESS SURFACE MOUNTED,

TANTALUM, SOLID ELECTROLYTE, ENCLOSED

ANODE CONNECTION,

BASED ON TYPE TAJ

ESCC Detail Specification No. 3012/001

| Issue 5 | March 2015 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

Legal Disclaimer and Copyright

European Space Agency, Copyright © 2015. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| 914 | Specification upissued to incorporate editorial changes per DCR. |

TABLE OF CONTENTS

1	GENERAL	6

1.1	SCOPE	6

1.2	TYPE VARIANTS AND RANGE OF COMPONENTS	6

1.3	MAXIMUM RATINGS	6

1.4	PARAMETER DERATING INFORMATION	6

1.5	PHYSICAL DIMENSIONS	6

1.6	FUNCTIONAL DIAGRAM	6

2	APPLICABLE DOCUMENTS	10

3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	10

4	REQUIREMENTS	10

4.1	GENERAL	10

4.2	DEVIATIONS FROM GENERIC SPECIFICATION	10

4.2.1	Deviations from Special In-process Controls	10

4.2.2	Deviations from Final Production Tests (Chart II)	10

4.2.3	Deviations from Burn-in and Electrical Measurements (Chart III)	10

4.2.4	Deviations from Qualification Tests (Chart IV)	10

4.2.5	Deviations from Lot Acceptance Tests (Chart V)	10

4.3	MECHANICAL REQUIREMENTS	10

4.3.1	Dimension Check	10

4.3.2	Weight	11

4.4	MATERIALS AND FINISHES	11

4.4.1	Terminations	11

4.5	MARKING	11

4.5.1	General	11

4.5.2	The ESCC Component Number	11

4.5.3	Electrical Characteristics and Ratings	11

4.5.4	Traceability Information	12

4.6	ELECTRICAL MEASUREMENTS	12

4.6.1	Electrical Measurements at Room Temperature	12

4.6.2	Electrical Measurements at High and Low Temperatures	12

4.6.3	Circuits for Electrical Measurements	12

4.7	BURN-IN TESTS	13

4.7.1	Parameter Drift Values	13

4.7.2	Conditions for Burn-in	13

4.7.3	Electrical Circuits for Burn-in	13

4.8	ENVIRONMENTAL AND ENDURANCE TESTS (CHARTS IV AND V OF ESCC GENERIC SPECIFICATION No. 3012)	15

4.8.1	Measurements and Inspections on Completion of Environmental Tests	15

4.8.2	Measurements and Inspections at Intermediate Points during Endurance Tests	15

4.8.3	Measurements and Inspections on Completion of Endurance Tests	15

4.8.4	Conditions for Operating Life Tests (Part of Endurance Testing)	15

4.8.5	Electrical Circuit for Operating Life Tests (Figure 5)	15

Appendix ‘A’	19

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, test and inspection data for Capacitors, Leadless Surface Mounted, Tantalum, Solid Electrolyte, Enclosed Anode Connection, based on Type TAJ.

It shall be read in conjunction with ESCC Generic Specification No. 3012, the requirements of which are supplemented herein.

## TYPE VARIANTS AND RANGE OF COMPONENTS

Variants of the basic type capacitors and the range of components covered by this specification are scheduled in Figure 2 and Table 1(a) respectively.

## MAXIMUM RATINGS

The maximum ratings, which shall not be exceeded at any time during use or storage, applicable to the capacitors specified herein, are as scheduled in Table 1(b).

## PARAMETER DERATING INFORMATION

The parameter derating information applicable to the capacitors specified herein is shown in Figure 1.

## PHYSICAL DIMENSIONS

The physical dimensions of the capacitors specified herein are shown in Figure 2.

## FUNCTIONAL DIAGRAM

The functional diagram of the capacitors specified herein is shown in Figure 3.

TABLE 1(a) - RANGE OF COMPONENTS

| CAP VALUE (μF) (2) | RATED VOLTAGE (V) (1) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 4 | 6.3 | 10 | 16 | 20 | 25 | 35 | 50 |
| 0.1 |  |  |  |  |  |  | A | A |
| 0.15 |  |  |  |  |  |  | A | B |
| 0.22 |  |  |  |  |  |  | A | B |
| 0.33 |  |  |  |  |  |  | A | B |
| 0.47 |  |  |  |  |  | A | A, B | C |
| 0.68 |  |  |  |  | A | A | A, B | C |
| 1 |  |  |  | A | A | A | B | C |
| 1.5 |  |  | A | A | A | B | B, C | D |
| 2.2 |  | A | A | A, B | B | B | B, C | D |
| 3.3 | A | A | A | A, B | B | B, C | C | D |
| 4.7 | A | A | A, B | B | B, C | C | C, D | D |
| 6.8 | A | A, B | B | B, C | C | C, D | D | D |
| 10 | A, B | B | B, C | C | C | C, D | D | E |
| 15 | B | B, C | C | C | C, D | D | D |  |
| 22 | B, C | C | C | C, D | D | D | E |  |
| 33 | C | C | C, D | D | D | E |  |  |
| 47 | C, D | C, D | C, D | D | E |  |  |  |
| 68 | C, D | D | D | D | E |  |  |  |
| 100 | D | D | D | E |  |  |  |  |
| 150 | D | D | E |  |  |  |  |  |
| 220 | E | E | E |  |  |  |  |  |

NOTES

Letters indicate case sizes (See Figure 2).

Tolerances of ±10% and ±20% are available.

TABLE 1(b) - MAXIMUM RATINGS

| No. | Characteristics | Symbol | Maximum Ratings |  | Units | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |  |
| 1 | Rated Voltage | UR | See Table 1(a) |  | Vdc |  |
| 2 | Surge Voltage | US | - | 1.3 x UR | Vdc | ≤ +85°C |
| 3 | Category Voltage | UC | - | 0.66 x UR | Vdc |  |
| 4 | Operating Temperature Range | Top | -55 | +125 | °C |  |
| 5 | Rated Temperature | Tr | - | +85 | °C |  |
| 6 | Category Temperature | Tc | - | +125 | °C |  |
| 7 | Storage Temperature Range | Tstg | -55 | +125 | °C |  |
| 8 | Soldering Temperature | Tsol | - | +260 | °C | Note 1 |

NOTES

            - Soldering time 5 seconds maximum for wave soldering and 10 seconds maximum for reflow soldering.

Figure 1 - Parameter derating information

FIGURE 2 - PHYSICAL DIMENSIONS

| Variant (1) | Case Size | Dimensions (mm) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | L |  | W |  | H | W1 |  | A |  | S | H1 |
|  |  | Min | Max | Min | Max | Max | Min | Max | Min | Max | Min | Min |
| 01 02 13 14 17 | A B C D E | 3 3.3 5.8 7.1 7.1 | 3.4 3.7 6.2 7.5 7.5 | 1.5 2.7 3.1 4.2 4.2 | 1.8 3 3.4 4.5 4.5 | 1.8 2.1 2.8 3.1 4.3 | 1.1 2.1 2.1 2.3 2.3 | 1.3 2.3 2.3 2.5 2.5 | 0.6 0.6 1.1 1.1 1.1 | 1.1 1.1 1.6 1.6 1.6 | 1.1 1.4 2.9 4.4 4.4 | 0.7 0.7 0.7 0.7 0.7 |

NOTE:

            - Variants 01 & 02 differ from Variants 13, 14 & 17 by their terminations (see Para. 4.4.1).

FIGURE 3 - FUNCTIONAL DIAGRAM

# APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3012 for Capacitors, Leadless Surface Mounted, Tantalum, Solid Electrolyte, Enclosed Anode Connection.

# TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein shall be as stated in this specification and ESCC Generic Specification No. 3012. Deviations from the Generic Specification, applicable to this Detail Specification only, are listed in Para. 4.2.

Deviations from the applicable Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirements and do not affect the components' reliability, are listed in the appendices attached to this specification.

## DEVIATIONS FROM GENERIC SPECIFICATION

### Deviations from Special In-process Controls

None.

### Deviations from Final Production Tests (Chart II)

None.

### Deviations from Burn-in and Electrical Measurements (Chart III)

None.

### Deviations from Qualification Tests (Chart IV)

Para. 9.19, Solderability: the solderable area is the termination 'pad' and up to 1/3 the height of the tab.

### Deviations from Lot Acceptance Tests (Chart V)

Para. 9.19, Solderability: the solderable area is the termination 'pad' and up to 1/3 the height of the tab.

## MECHANICAL REQUIREMENTS

### Dimension Check

The dimensions of the components specified herein shall be verified in accordance with the requirements set out in Para. 9.6 of ESCC Generic Specification No. 3012. They shall conform to those shown in Figure 2 of this specification.

### Weight

The maximum weight of the capacitors specified herein shall be as follows:

| Case Size 'A' | - 0.1 grammes |
| --- | --- |
| Case Size 'B' | - 0.2 grammes |
| Case Size 'C' | - 0.3 grammes |
| Case Size 'D' | - 0.5 grammes |
| Case Size 'E' | - 0.7 grammes |

## MATERIALS AND FINISHES

The materials and finishes shall be as specified herein. Where a definite material is not specified, a material which will enable the components specified herein to meet the performance requirements of this specification shall be used. Acceptance or approval of any constituent material does not guarantee acceptance of the finished product.

### Terminations

For Variants 01 & 02: the termination shall be Type 'G' with Type '16' finish in accordance with the requirements of ESCC Basic Specification No. 23500.

For Variants 13, 14 & 17: the termination shall be Type 'P' with Type '17' finish in accordance with the requirements of ESCC Basic Specification No. 23500.

## MARKING

### General

The marking of all components delivered to this specification shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and the following paragraphs. For those components too small to accommodate the marking as specified hereafter, the marking information in full shall accompany each component in its primary package. Such marking shall comprise:

The ESCC Component Number.

Characteristics and Ratings.

Traceability Information.

### The ESCC Component Number

Each component shall bear the ESCC Component Number which shall be constituted and marked as follows:

Example: 301200101B

Detail Specification Number	: 3012001

Type Variant (as applicable, see Figure 2): 01

Testing Level (B or C, as applicable): B

### Electrical Characteristics and Ratings

- The electrical characteristics and ratings to be marked, in the following order of precedence, are:

Polarity.

Numerical value.

Rated voltage.

Tolerance.

#### Polarity

The anode connection shall be indicated by a BAR on the coded surface.

NOTES:

For qualified devices, the ESCC qualified components symbol may be used to indicate the anode connection.

#### Capacitance

This shall be indicated by the value marked on the component.

#### Rated Voltage

This shall be indicated by the value marked on the component or, where the body size is too small, by the code letters specified hereafter:

| Rated Voltage (V) | Code Letter |
| --- | --- |
| 4 6.3 10 16 20 25 35 50 | G J A C D E V T |

#### Tolerance

The tolerance on numerical values shall be indicated by the code letters specified hereafter:

| Tolerance | Code Letter |
| --- | --- |
| ±10% | K |
| ±20% | M |

### Traceability Information

Traceability information shall be marked in accordance with the requirements of ESCC Basic Specification No. 21700. The information to be marked shall be as follows:

Manufacturing date code.

Serial number.

Manufacturer's name.

## ELECTRICAL MEASUREMENTS

### Electrical Measurements at Room Temperature

The parameters to be measured in respect of electrical characteristics are scheduled in Table 2. The measurements shall be performed at Tamb = +22 ±3°C.

### Electrical Measurements at High and Low Temperatures

The parameters to be measured at high and low temperatures are scheduled in Table 3.

### Circuits for Electrical Measurements

Not applicable.

## BURN-IN TESTS

### Parameter Drift Values

The parameter drift values applicable to burn-in are specified in Table 4 of this specification. Unless otherwise stated, measurements shall be performed at Tamb = +22 ±3°C. The parameter drift values (Δ) applicable to the scheduled parameters shall not be exceeded. In addition to these drift value requirements for a given parameter, the appropriate limit value specified in Table 2 shall not be exceeded.

### Conditions for Burn-in

The requirements for burn-in are specified in Section 7 of ESCC Generic Specification No. 3012. The conditions for burn-in shall be as specified in Table 5(a) of this specification.

### Electrical Circuits for Burn-in

Not applicable.

TABLE 2 - ELECTRICAL MEASUREMENTS AT ROOM TEMPERATURE

| No. | Characteristics | Symbol | Spec. and/or Test Method | Test Conditions | Limits |  | Unit |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Min | Max |  |
| 1 | Capacitance | C | ESCC 3012 Para. 9.4.1.1 |  | -10 -20 | +10 +20 | % |
| 2 | DC Leakage Current | IL | ESCC 3012 Para. 9.4.1.2 |  | - | 0.01 x C x UR or (1) 1 | µA |
| 3 | Dissipation Factor | DF | ESCC 3012 Para. 9.4.1.3 | UR < 10V UR ≥ 10V, C ≤ 1µF UR ≥ 10V, C > 1µF | - - - | 6 4 6 | % |

NOTES

Whichever is greater.

TABLE 3 - ELECTRICAL MEASUREMENTS AT HIGH and Low Temperature

| No. | Characteristics | Symbol | Spec. and/or Test Method | Test Conditions (Note 2) | Limits |  | Unit |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Min | Max |  |
| 1 | Capacitance Change | ΔC/C | ESCC 3012 Para. 9.4.1.1 | -55 (+3 -0)°C +85 ±3°C +125 (+0 -3)°C | -8 0 0 | 0 +8 +12 | % |
| 2 | DC Leakage Current | IL | ESCC 3012 Para. 9.4.1.2 | +85 ±3°C +125 (+0 -3)°C | - - | 0.1 x C x UR or (1) 1 0.125 x C x UR or (1) 1 (3) | µA |
| 3 | Dissipation Factor | DF | ESCC 3012 Para. 9.4.1.3 | -55 (+3 -0)°C +85 ±3°C +125 (+0 -3)°C | - - - | 9 7.2 9 | % |

NOTES

            - Whichever is greater.

            - Inspection level II single sampling, AQL 2.5% for each capacitance value. Each capacitance value shall be considered as constituting a complete lot.

            - Measured with category voltage.

Figure 4 – circuits for electrical measurements

Not applicable

TABLE 4 - PARAMETER DRIFT VALUES

| No. | Characteristics | Symbol | Spec. and/or Test Method | Test Conditions | Limits | Unit |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Capacitance Change | ΔC/C | As per Table 2 | As per Table 2 | ±5 | % |
| 2 | DC Leakage Current Change | ΔIL | As per Table 2 | As per Table 2 | 2 x Initial Value (1) or (2) (0.25 x Table 2 Item 2) +0.05µA | µA |

NOTES

            - Leakage currents ≤ 0.1µA are considered as a 0.1µA value.

            - Whichever is smaller.

TABLE 5(a) - CONDITIONS FOR BURN-IN

| No. | Characteristics | Symbol | Conditions | Unit |
| --- | --- | --- | --- | --- |
| 1 | Ambient Temperature | Tamb | +85 (+0 -3) | °C |
| 2 | Test Voltage | VT | UR | V |

TABLE 5(b) - CONDITIONS FOR OPERATING LIFE TESTS

| No. | Characteristics | Symbol | Conditions | Unit |
| --- | --- | --- | --- | --- |
| 1 | Ambient Temperature 1 | Tamb1 | +85 (+0 -3) | °C |
| 2 | Test Voltage 1 | VT1 | UR | V |
| 3 | Ambient Temperature 2 | Tamb2 | +125 (+0 -3) | °C |
| 4 | Test Voltage 2 | VT2 | UC | V |

FIGURE 5 - ELECTRICAL CIRCUIT FOR BURN-IN and operating life test

Not applicable.

## ENVIRONMENTAL AND ENDURANCE TESTS (CHARTS IV AND V OF ESCC GENERIC SPECIFICATION No. 3012)

### Measurements and Inspections on Completion of Environmental Tests

The parameters to be measured and inspections to be performed on completion of environmental tests are scheduled in Table 6. Unless otherwise stated, the measurements shall be performed at Tamb = +22 ±3°C.

### Measurements and Inspections at Intermediate Points during Endurance Tests

The parameters to be measured and inspections to be performed at intermediate points during endurance tests are scheduled in Table 6. The measurements shall be performed at 
the temperatures specified for the test.

### Measurements and Inspections on Completion of Endurance Tests

The parameters to be measured and inspections to be performed on completion of endurance tests are scheduled in Table 6. Unless otherwise stated, the measurements shall be performed at 
Tamb = +22 ±3°C.

### Conditions for Operating Life Tests (Part of Endurance Testing)

The requirements for operating life testing are specified in Section 9 of ESCC Generic Specification No. 3012. The conditions for operating life testing shall be as specified in Table 5(b) of this specification.

### Electrical Circuit for Operating Life Tests (Figure 5)

Not applicable.

TABLE 6 - MEASUREMENTS AND INSPECTIONS ON COMPLETION OF ENVIRONMENTAL TESTS AND AT INTERMEDIATE POINTS AND ON COMPLETION OF ENDURANCE TESTING

| No. | ESCC Generic Spec. No. 3012 |  | Measurements and Inspections |  | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Environmental and Endurance Tests (Note 1) | Test Methods and Conditions | Identification | Conditions |  | Min |  | Max |  |
| 01 | Mounting | Para. 9.9 | Final Examination |  |  |  |  |  |  |
|  |  |  | Terminals | Good tinning | - | - |  | - |  |
|  |  |  | Final Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Table 2 Item 1 | C | Table 2 |  |  | µF |
|  |  |  | Capacitance Change | Table 2 Item 1 | ΔC/C | -5 | +5 |  | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - |  | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - |  | Table 2 | % |
| 02 | Rapid Change of Temperature | Para. 9.3.2 | Initial Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  |  | µF |
|  |  |  | Final Measurements | Recovery period of 4 hours min. |  |  |  |  |  |
|  |  |  | Visual Examination | - | - | - |  | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | ΔC/C | -5 |  | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - |  | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - |  | Table 2 | % |
| 03 | External Visual Inspection | Para. 9.5 | Final Inspection |  |  |  |  |  |  |
|  |  |  | Visual Inspection | ESCC No. 20500 | - | - |  | - |  |
| 04 | Adhesion | Para. 9.10 | Initial Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table |  |  | µF |
|  |  |  | Final Measurements |  |  |  |  |  |  |
|  |  |  | Visual Examination | No damage or loosening from the substrate | - | - |  | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | ΔC/C | -5 |  | +5 | % |
| 05 | Vibration | Para. 9.11 | Measurements during test | During Last Cycle |  |  |  |  |  |
|  |  |  |  | No intermittent Contact >0.5ms, arcing or open or shorts | - | - |  | - |  |
|  |  |  | Final Examination |  |  |  |  |  |  |
|  |  |  | Visual Examination | No damage | - | - |  | - |  |
| 06 | Shock or Bump | Para. 9.12 | Final Examination |  |  |  |  |  |  |
|  |  |  | Visual Examination | No damage | - | - |  | - |  |
| 07 | Climatic Sequence | Para. 9.13 | Initial Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  |  | µF |
|  |  |  | Intermediate Measurements | After Dry Heat (2) |  |  |  |  |  |
|  |  |  | DC Leakage Current | Table 3 Item 2 | IL | - |  | Table 3 | µA |
|  |  |  | Final Measurements | After recovery of 1 to 24 hours |  |  |  |  |  |
|  |  |  | Visual Inspection | ESCC No. 20500 | - | - |  | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | ΔC/C | -5 |  | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - |  | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - |  | (3) | % |
| 08 | High and Low Temperature Stability | Para. 9.14 | Measurements during test |  |  |  |  |  |  |
|  |  |  | Electrical Measurements | Tables 2 & 3 | - | Tables 2 & 3 |  |  |  |
| 09 | Surge Voltage | Para. 9.15 | Final Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Table 2 Item 1 | C | Table 2 |  |  | µF |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - |  | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - |  | Table 2 | % |
| 10 | Damp Heat Steady State | Para. 9.16 | Initial Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  |  | µF |
|  |  |  | Final Measurements | After recovery of 1 to 2 hours |  |  |  |  |  |
|  |  |  | Visual Examination | - | - | - |  | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | ΔC/C | -5 |  | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - |  | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - |  | (3) | % |
| 11 | Operating Life | Para. 9.17 | Initial Measurements |  |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  |  | µF |
|  |  |  | Intermediate Measurements | At 250 and 1000 hrs |  |  |  |  |  |
|  |  |  | DC Leakage Current (2) | Table 3 Item 2 | IL | - |  | (4) | µA |
|  |  |  | Final Measurements | At 1000 and 2000 hrs and after recovery or 1 to 2 hours |  |  |  |  |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | ΔC/C | -5 |  | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - |  | (5) | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - |  | Table 2 | % |
|  |  |  | Visual Examination | No damage | - | - |  | - |  |
| 12 | Permanence of Marking | Para. 9.18 | Final Examination |  |  |  |  |  |  |
|  |  |  | Visual Examination | No corrosion or obliteration of marking | - | - |  | - |  |
| 13 | Solderability | Para. 9.19 and Paras. 4.2.4 and 4.2.5 of this spec | Final Examination |  |  |  |  |  |  |
|  |  |  | Visual Examination | No damage | - | - |  | - |  |

NOTES

The tests in this Table refer to either Chart IV or V and shall be used as applicable.

While still at the high temperature.

1.2x the value specified in Table 2 of this specification.

1.25x the value specified in Table 3 of this specification.

1.25x the value specified in Table 2 of this specification.

Appendix ‘A’

AGREED DEVIATIONS FOR AVX CZECH RePUBLIC S.R.O. (CZ)

| ITEMS AFFECTED | DESCRIPTION OF DEVIATIONS |
| --- | --- |
| Deviations from Final Production Tests (Chart II) | Para. 9.1, Internal Visual Inspection: Shall not be performed. |
|  | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |
| Deviations from Burn-in and Electrical Measurements (Chart III) | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |
| Deviations from Qualification Tests (Chart IV) | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |
| Deviations from Lot Acceptance Tests (Chart V) | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |