Page 1 of 21

CAPACITORS, LEADLESS SURFACE MOUNTED, TANTALUM, SOLID ELECTROLYTE, LOW EQUIVALENT SERIES RESISTANCE

BASED ON TYPE TES

ESCC Detail Specification No. 3012/004

| Issue 3 | April 2014 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

Legal Disclaimer and Copyright

European Space Agency, Copyright © 2014. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| 835 | Specification upissued to incorporate technical changes per DCR. |

TABLE OF CONTENTS

1	General	6

1.1	Scope	6

1.2	component type variants and Range of Components	6

1.3	Maximum Ratings	6

1.4	Parameter Derating Information	6

1.5	Physical Dimensions	6

1.6	Functional Diagram	6

2	Applicable Documents	6

3	Terms, Definitions, Abbreviations, Symbols and Units	6

4	REQUIREMENTS	12

4.1	GENERAL	12

4.2	DEVIATIONS FROM GENERIC SPECIFICATION	12

4.2.1	Deviations from Special In-Process Controls	12

4.2.2	Deviations from Final Production Tests (Chart II)	12

4.2.3	Deviations from Burn-in and Electrical Measurements (Chart III)	12

4.2.4	Deviations from Qualification Tests (Chart IV)	12

4.2.5	Deviations from Lot Acceptance Tests (Chart V)	12

4.3	MECHANICAL REQUIREMENTS	12

4.3.1	Dimension Check	12

4.3.2	Weight	12

4.4	MATERIALS AND FINISHES	12

4.4.1	Terminal Material and Finish	12

4.5	MARKING	13

4.5.1	General	13

4.5.2	The ESCC Component Number	13

4.5.3	Electrical Characteristics and Ratings	13

4.5.3.1	Polarity	13

4.5.3.2	Capacitance Value	14

4.5.3.3	Tolerance	14

4.5.3.4	Rated Voltage	14

4.5.3.5	Equivalent Series Resistance	14

4.5.4	Traceability Information	14

4.6	Electrical Measurements	15

4.6.1	Electrical Measurements at Room Temperature	15

4.6.2	Electrical Measurements at High and Low Temperatures	15

4.6.3	Circuits for Electrical Measurements (Figure 4)	15

4.7	Burn-in Tests	15

4.7.1	Parameter Drift Values	15

4.7.2	Conditions for Burn-in	15

4.7.3	Electrical Circuit for Burn-in (Figure 5)	15

4.8	Environmental and Endurance Tests (Charts IV and V of ESCC Generic Specification No. 3012)	17

4.8.1	Measurements and Inspections on Completion of Environmental Tests	17

4.8.2	Measurements and Inspections at Intermediate Points During Endurance Tests	17

4.8.3	Measurements and Inspections on Completion of Endurance Tests	17

4.8.4	Conditions for Operating Life (Part of Endurance Testing)	17

4.8.5	Electrical Circuit for Operating Life Tests (Figure 5)	17

APPENDIX ‘A’	21

# General

## Scope

This specification details the ratings, physical and electrical characteristics, test and inspection data for Capacitors, Leadless Surface Mounted, Tantalum, Solid Electrolyte, Low Equivalent Series Resistance, based on Type TES. It shall be read in conjunction with ESCC Generic Specification No. 3012, the requirements of which are supplemented herein.

## component type variants and Range of Components

The variants and the range of components covered by this specification are given in Table 1(a).

## Maximum Ratings

The maximum ratings, which shall not be exceeded at any time during use or storage, applicable to the components specified herein, are as scheduled in Table 1(b).

## Parameter Derating Information

The parameter derating information applicable to the capacitors specified herein is shown in Figure 1.

## Physical Dimensions

The physical dimensions of the capacitors specified herein are shown in Figure 2.

## Functional Diagram

The functional diagram for the capacitors specified herein is shown in Figure 3.

# Applicable Documents

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3012 for Capacitors, Leadless Surface Mounted, Tantalum, Solid Electrolyte, Enclosed Anode Connection

# Terms, Definitions, Abbreviations, Symbols and Units

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic specification No. 21300 shall apply.

Table 1(a) - TYPE VARIANTS AND RANGE OF COMPONENTS

| Variant Number | Case Code (Style) (Note 1) | Capacitance Range Cn (µF) (Notes 2, 3) | Rated Voltage UR (V) (Note 2) | Maximum Equivalent Series Resistance ESR (mΩ) (Note 2) | Terminal Material and Finish | Weight Max (g) |
| --- | --- | --- | --- | --- | --- | --- |
| 01 | A (1206) | 1 to 22 | 6.3 to 25 | 900 to 3000 | G16 | 0.1 |
| 02 | B (1210) | 1 to 47 | 6.3 to 50 | 500 to 2000 | G16 | 0.2 |
| 03 | C (2312) | 3.3 to 150 | 6.3 to 50 | 300 to 1000 | P17 | 0.3 |
| 04 | D (2917) | 4.7 to 330 | 6.3 to 50 | 35 to 200 | P17 | 0.5 |
| 05 | E (2917) | 33 to 470 | 6.3 to 35 | 30 to 65 | P17 | 0.7 |

NOTES:

See Figure 2.

The following rated Capacitance (Cn), maximum Rated Voltage (UR) and maximum Equivalent Series Resistance values (ESR) are available related to the Case Code (letters indicate Case Code; numbers indicate maximum ESR in mΩ):

| Capacitance Cn (F) | Rated Voltage UR |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 6.3V | 10V | 12V | 16V | 20V | 25V | 35V | 50V |
| 1 |  |  |  |  |  | A 3000 |  | B 2000 |
| 3.3 |  |  |  |  | A 2500 |  | B 1000 | C 1000 |
| 4.7 |  |  |  | A 2000 |  | B 1000 | C 600 | D 200 |
| 10 |  | A 1800 |  |  | B 1000 | C 600 | D 120 |  |
| 22 | A 900 |  |  | B 600 | C 400 |  | D 100 |  |
| 33 |  | B 650 |  |  | C 300 | D 65 | E 65 |  |
| 47 | B 500 |  |  | C 350 | D 55 | E 65 |  |  |
| 100 |  | C 200 |  | D 55 | E 45 |  |  |  |
| 150 | C 300 | D 45 |  | E 40 |  |  |  |  |
| 220 |  | D 35 | E 35 |  |  |  |  |  |
| 330 | D 35 | E 35 |  |  |  |  |  |  |
| 470 | E 30 |  |  |  |  |  |  |  |

The following Capacitance Tolerances are available:

- ±10% (K)

- ±20% (M)

Table 1(b) - MAXIMUM RATINGS

| No. | Characteristics | Symbols | Maximum Ratings |  | Units | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Rated Voltage | UR | See Table 1(a) |  | V | Note 1 |
| 2 | Surge Voltage | US | - | 1.3 x UR | V | Tamb ≤ +85°C |
| 3 | Category Voltage | UC | - | 0.66 x UR | V |  |
| 4 | Ripple Current | Iripple | - | See Note 2 | mA | f = 100kHz, Note 3 |
| 5 | Operating Temperature Range | Top | -55 to +125 |  | °C | Tamb |
| 6 | Rated Temperature | TR | - | +85 | °C |  |
| 7 | Upper Category Temperature | TC | - | +125 | °C |  |
| 8 | Storage Temperature Range | Tstg | -55 to +125 |  | °C |  |
| 9 | Soldering Temperature | Tsol | - | +260 | °C | Note 2 |

Notes:

            - At Tamb ≤ +85°C. For derating at Tamb > +85°C, see Figure 1(a).

            - Maximum Iripple, which depends on Cn and UR, shall be a follows:

| Capacitance Cn (µF) | Rated Voltage UR (V) | Maximum Ripple Current Iripple (mA) |
| --- | --- | --- |
| 22 | 6.3 | 290 |
| 47 | 6.3 | 410 |
| 150 | 6.3 | 610 |
| 330 | 6.3 | 2700 |
| 470 | 6.3 | 3000 |
| 10 | 10 | 200 |
| 33 | 10 | 360 |
| 100 | 10 | 740 |
| 150 | 10 | 2400 |
| 220 | 10 | 2700 |
| 330 | 50 | 2800 |
| 220 | 12 | 2800 |
| 4.7 | 16 | 190 |
| 22 | 16 | 380 |
| 47 | 16 | 560 |
| 100 | 16 | 2200 |
| 150 | 16 | 2600 |
| 3.3 | 20 | 170 |
| 10 | 20 | 290 |
| 22 | 20 | 520 |
| 33 | 20 | 610 |
| 47 | 20 | 2200 |
| 100 | 20 | 2500 |
| 1 | 25 | 160 |
| 4.7 | 25 | 290 |
| 10 | 25 | 430 |
| 33 | 25 | 2000 |
| 47 | 25 | 2000 |
| 3.3 | 35 | 290 |
| 4.7 | 35 | 430 |
| 10 | 35 | 1500 |
| 22 | 35 | 1600 |
| 33 | 35 | 2000 |
| 1 | 50 | 200 |
| 3.3 | 50 | 330 |
| 4.7 | 50 | 1100 |

            - At Tamb ≤ +25°C. For derating at Tamb > +25°C, see Figure 1(b).

            - Duration 5 seconds maximum for wave soldering and 10 seconds maximum for reflow soldering.

FIGURE 1 - PARAMETER DERATING INFORMATION

Figure 1(a) - Rated Voltage Versus Ambient Temperature

Figure 1(b) - Maximum Ripple Current versus Ambient Temperature

FIGURE 2 - PHYSICAL DIMENSIONS

| Variant Number | Case Code | Dimensions (mm) |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | L |  | W |  | H | W1 |  | A |  | S | H1 | W2 |  |
|  |  | Min | Max | Min | Max | Max | Min | Max | Min | Max | Min | Min | Min | Max |
| 01 | A | 3 | 3.4 | 1.5 | 1.8 | 1.8 | 1 | 1.4 | 0.6 | 1.1 | 1.1 | 0.7 | 0.05 | 0.4 |
| 02 | B | 3.3 | 3.7 | 2.7 | 3 | 2.1 | 2 | 2.4 | 0.6 | 1.1 | 1.4 | 0.7 | 0.15 | 0.5 |
| 03 | C | 5.8 | 6.2 | 3.1 | 3.4 | 2.8 | 2 | 2.4 | 1.1 | 1.6 | 2.9 | 0.7 | 0.35 | 0.7 |
| 04 | D | 7.1 | 7.5 | 4.2 | 4.5 | 3.1 | 2.2 | 2.6 | 1.1 | 1.6 | 4.4 | 0.7 | 0.8 | 1.15 |
| 05 | E | 7.1 | 7.5 | 4.2 | 4.5 | 4.3 | 2.2 | 2.6 | 1.1 | 1.6 | 4.4 | 0.7 | 0.8 | 1.15 |

Figure 3 - functional diagram

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are stated in this specification and ESCC Generic Specification No. 3012. Deviations from the Generic Specification, applicable to this specification only, are detailed in Para. 4.2.

Deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirements and do not affect the components’ reliability, are listed in the appendices attached to this specification.

## DEVIATIONS FROM GENERIC SPECIFICATION

### Deviations from Special In-Process Controls

None.

### Deviations from Final Production Tests (Chart II)

None.

### Deviations from Burn-in and Electrical Measurements (Chart III)

None

### Deviations from Qualification Tests (Chart IV)

Para. 9.19, Solderability: The solderable area is the termination pad and up to 1/3 the height of the tab.

### Deviations from Lot Acceptance Tests (Chart V)

Para. 9.19, Solderability: The solderable area is the termination pad and up to 1/3 the height of the tab.

## MECHANICAL REQUIREMENTS

### Dimension Check

The dimensions of the components specified herein shall be verified in accordance with the requirements set out in Para. 9.6 of ESCC Generic Specification No. 3012 and they shall conform to those shown in Figure 2 of this specification.

### Weight

The maximum weight of the components specified herein shall be as given in Table 1(a).

## MATERIALS AND FINISHES

The materials and finishes shall be as specified herein. Where a definite material is not specified, a material which will enable the capacitors specified herein to meet the performance requirements of this specification shall be used. Acceptance or approval of any constituent material does not guarantee acceptance of the finished product.

### Terminal Material and Finish

The terminal material and finish shall be as specified in Table 1(a) in accordance with the requirements of ESCC Basic Specification No. 23500.

## MARKING

### General

The marking of all components delivered to this specification shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and the following paragraphs. When the component is too small to accommodate all of the marking specified, as much as space permits shall be marked and the marking information, in full, shall accompany each component in its primary package.

The information to be marked and the order of precedence, shall be as follows:

The ESCC Component Number.

Electrical Characteristics and Ratings.

Traceability Information.

### The ESCC Component Number

The ESCC Component Number shall be constituted and marked as follows:

301200401B

Detail Specification Number: 3012004

Type Variant (see Table 1(a)): 01

Testing Level (B or C, as applicable): B

### Electrical Characteristics and Ratings

The electrical characteristics and ratings to be marked in the following order of precedence are:

Polarity.

Capacitance Value.

Tolerance.

Rated Voltage.

Equivalent Series Resistance.

The information shall be constituted and marked as follows:

Example: 106KE0600

Capacitance Value (10μF): 106

Tolerance (±10%): K

Rated Voltage (25V): E

Equivalent Series Resistance (600mΩ): 0600

#### Polarity

The anode terminal shall be indicated by a polarity stripe marked on the top surface of the component.

#### Capacitance Value

The capacitance value shall be indicated by the following codes. The unit quantity for marking shall be picofarad.

| Capacitance Cn (pF) | Code |
| --- | --- |
| XX105 | XX5 |
| XX106 | XX6 |
| XX107 | XX7 |

#### Tolerance

The tolerance on capacitance value shall be indicated by the following code letters.

| Tolerance (%) | Code Letter |
| --- | --- |
| ±10 | K |
| ±20 | M |

#### Rated Voltage

The rated voltage shall be indicated by the following code letters.

| Rated Voltage UR (V) | Code Letter |
| --- | --- |
| 6.3 | J |
| 10 | A |
| 12 | B |
| 16 | C |
| 20 | D |
| 25 | E |
| 35 | V |
| 50 | T |

#### Equivalent Series Resistance

The Equivalent Series Resistance maximum value shall be indicated by the following codes. The unit quantity for marking shall be milliohm.

| Equivalent Series Resistance ESR (mΩ) | Code |
| --- | --- |
| XX | 00XX |
| XXX | 0XXX |
| XXXX | XXXX |

### Traceability Information

Traceability information shall be marked in accordance with the requirements of ESCC Basic Specification No. 21700.

## Electrical Measurements

### Electrical Measurements at Room Temperature

The parameters to be measured at room temperature are scheduled in Table 2. Unless otherwise specified the measurements shall be performed at Tamb = +22 ±3°C.

### Electrical Measurements at High and Low Temperatures

The parameters to be measured at high and low temperatures are scheduled in Table 3.

### Circuits for Electrical Measurements (Figure 4)

Not applicable.

## Burn-in Tests

### Parameter Drift Values

The parameter drift values applicable to Burn-in are as specified in Table 4 of this specification. Unless otherwise stated, measurements shall be performed at Tamb = +22 ±3°C.

The parameter drift values (Δ) applicable to the parameters scheduled shall not be exceeded. In addition to these drift value requirements for a given parameter, the appropriate limit values specified in Table 2 shall not be exceeded.

### Conditions for Burn-in

The requirements for Burn-in are specified in Section 7 of ESCC Generic Specification No. 3012. The conditions for Burn-in shall be as specified in Table 5 of this specification.

### Electrical Circuit for Burn-in (Figure 5)

Not applicable

Table 2 – ELECTRICAL MEASUREMENTS AT ROOM TEMPERATURE

| No. | Characteristics | Symbols | ESCC 3012 Test Method | Rated Voltage | Tolerance | Limits |  | Unit |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Min | Max |  |
| 1 | Capacitance | C | Para. 9.4.1.1 | All | ±10% ±20% | 0.9Cn 0.8Cn | 1.1Cn 1.2Cn | µF |
| 2 | DC Leakage Current | IL | Para. 9.4.1.2 | All | All | - | 0.01Cn x UR or (Note 1) 1 | µA |
| 3 | Dissipation Factor | DF | Para. 9.4.1.3 | UR < 10V UR ≥ 10V | All | - | 10 6 | % |
| 4 | Equivalent Series Resistance | ESR | Para. 9.4.1.4 | All | All | - | Note 2 | mΩ |

NOTES:

            - Whichever is greater.

See Table 1(a) Note 2.

Table 3 - ELECTRICAL MEASUREMENTS AT HIGH AND LOW TEMPERATURES

| No. | Characteristics | Symbols | ESCC 3012 Test Method | Test Conditions (Note 1) | Limits |  | Unit |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Min | Max |  |
| 1 | Capacitance Change | C/C | Para. 9.4.1.1 | Tamb = -55 (+3 -0) °C | -10 | 0 | % (Note 2) |
|  |  |  |  | Tamb = +85 ±3°C | 0 | +10 |  |
|  |  |  |  | Tamb = +125 (+0 -3) °C | 0 | +12 |  |
| 2 | DC Leakage Current | IL | Para. 9.4.1.2 | Tamb = +85 ±3°C V = UR ±2% | - | 0.1Cn x UR or (Note 3) 1 | µA |
|  |  |  |  | Tamb = +125 (+0 -3) °C V = UC ±2% | - | 0.125Cn x UR or (Note 3) 1 |  |
| 3 | Dissipation Factor | DF | Para. 9.4.1.3 | Tamb = -55 (+3 -0) °C | - | +50 | % (Note 2) |
|  |  |  |  | Tamb = +85 ±3°C | - | +50 |  |
|  |  |  |  | Tamb = +125 (+0 -3) °C | - | +100 |  |
| 4 | Equivalent Series Resistance | ESR | Para. 9.4.1.4 | Tamb = -55 (+3 -0) °C | - | +150 | % (Note 2) |
|  |  |  |  | Tamb = +85 ±3°C | - | +50 |  |
|  |  |  |  | Tamb = +125 (+0 -3) °C | - | +50 |  |

NOTES:

            - Inspection level II single sampling, AQL 2.5% for each capacitance value. Each capacitance value shall be considered as constituting a complete lot.

            - Related to the value measured in Table 2.

            - Whichever is greater.

FIGURE 4 - CIRCUITS FOR ELECTRICAL MEASUREMENTS

Not applicable.

Table 4 - PARAMETER DRIFT VALUES

| No. | Characteristics | Symbol | Spec. and/or Test Method | Test Conditions | Change Limits () | Unit |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Capacitance Change | C/C | As per Table 2 | As per Table 2 | ±5 | % |
| 2 | DC Leakage Current Change | IL | As per Table 2 | As per Table 2 | 2 x Initial Value (Note 1) or (Note 2) 0.25 x Table 2 Item 2 + 0.05 | µA |

NOTES:

            - Leakage currents < 0.1μA shall be considered as a 0.1μA value.

            - Whichever is smaller.

Table 5(a) – CONDITIONS FOR BURN-IN

| No. | Characteristics | Symbol | Condition | Unit |
| --- | --- | --- | --- | --- |
| 1 | Ambient Temperature | Tamb | +85 (+0 -3) | °C |
| 2 | Test Voltage | VT | UR | V |

Table 5(b) – Conditions for Operating Life

| No. | Characteristics | Symbol | Condition | Unit |
| --- | --- | --- | --- | --- |
| 1 | Ambient Temperature 1 | Tamb1 | +85 (+0 -3) | °C |
| 2 | Test Voltage 1 | VT1 | UR | V |
| 3 | Ambient Temperature 2 | Tamb2 | +125 (+0 -3) | °C |
| 4 | Test Voltage 2 | VT2 | UC | V |

## Environmental and Endurance Tests (Charts IV and V of ESCC Generic Specification No. 3012)

### Measurements and Inspections on Completion of Environmental Tests

The parameters to be measured and inspections to be performed on completion of environmental tests are scheduled in Table 6. Unless otherwise stated, the measurements shall be performed at Tamb = +22 ±3°C.

### Measurements and Inspections at Intermediate Points During Endurance Tests

The parameters to be measured and inspections to be performed at intermediate points during endurance tests are scheduled in Table 6. Unless otherwise stated, the measurements shall be performed at Tamb = +22 ±3°C.

### Measurements and Inspections on Completion of Endurance Tests

The parameters to be measured and inspections to be performed on completion of endurance tests are scheduled in Table 6. Unless otherwise stated, the measurements shall be performed at Tamb = +22 ±3°C.

### Conditions for Operating Life (Part of Endurance Testing)

The requirements for Operating Life testing are specified in Section 9 of ESCC Generic Specification No. 3012. The conditions for Operating Life testing shall be as specified in Table 5(b) of this specification.

### Electrical Circuit for Operating Life Tests (Figure 5)

Not applicable.

Table 6 - MEASUREMENTS AND INSPECTIONS ON COMPLETION OF ENVIRONMENTAL TESTS AND AT INTERMEDIATE POINTS AND ON COMPLETION OF ENDURANCE TESTING

| No. | ESCC Generic Spec. No. 3012 |  | Measurements and Inspections |  | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Environmental and Endurance Tests (Note 1) | Test Methods and Conditions | Identification | Conditions |  | Min | Max |  |
| 01 | Mounting | Para. 9.9 | Final Examination |  |  |  |  |  |
|  |  |  | Terminals | Good tinning | - | - | - |  |
|  |  |  | Final Measurements |  |  |  |  |  |
|  |  |  | Capacitance | Table 2 Item 1 | C | Table 2 |  | µF |
|  |  |  | Capacitance Change | Table 2 Item 1 | C/C | -5 | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - | Table 2 | % |
|  |  |  | Equivalent Series Resistance | Table 2 Item 4 | ESR | - | 1.25 x Table 2 | mΩ |
| 02 | Rapid Change of Temperature | Para. 9.3.2 | Initial Measurements |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  | µF |
|  |  |  | Final Measurements | Recovery period of 4 hours min. |  |  |  |  |
|  |  |  | Visual Examination | No corrosion, no damage or obliteration of marking | - | - | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | C/C | -5 | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - | Table 2 | % |
|  |  |  | Equivalent Series Resistance | Table 2 Item 4 | ESR | - | 1.25 x Table 2 | mΩ |
| 03 | External Visual Inspection | Para. 9.5 | Final Inspection |  |  |  |  |  |
|  |  |  | External Visual Inspection | ESCC No. 20500 | - | - | - |  |
| 04 | Adhesion | Para. 9.10 | Initial Measurements |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  | µF |
|  |  |  | Final Measurements |  |  |  |  |  |
|  |  |  | Visual Examination | No damage or loosing from the substrate | - | - | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | C/C | -5 | +5 | % |
| 05 | Vibration | Para. 9.11 | Measurements during test | During Last Cycle |  |  |  |  |
|  |  |  |  | No intermittent Contact >0.5ms, arcing or open or shorts | - | - | - |  |
|  |  |  | Final Examination |  |  |  |  |  |
|  |  |  | Visual Examination | No damage | - | - | - |  |
| 06 | Shock or Bump | Para. 9.12 | Final Examination |  |  |  |  |  |
|  |  |  | Visual Examination | No damage | - | - | - |  |
| 07 | Climatic Sequence | Para. 9.13 | Initial Measurements |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  | µF |
|  |  |  | Intermediate Measurements | After Dry Heat |  |  |  |  |
|  |  |  | DC Leakage Current | Table 3 Item 2 (Note 2) | IL | - | Table 3 | µA |
|  |  |  | Final Measurements | After recovery of 1 to 24 tours |  |  |  |  |
|  |  |  | External Visual Inspection | ESCC No. 20500 | - | - | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | C/C | -5 | +5 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - | 1.25 x Table 2 | % |
|  |  |  | Equivalent Series Resistance | Table 2 Item 4 | ESR | - | 1.25 x Table 2 | mΩ |
| 08 | High and Low Temperature Stability | Para. 9.14 | Measurements during test |  |  |  |  |  |
|  |  |  | Electrical Measurements | Tables 2 & 3 |  | Tables 2 & 3 |  |  |
| 09 | Surge Voltage | Para. 9.15 | Final Measurements |  |  |  |  |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | C | Table 2 |  | µF |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - | Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - | Table 2 | % |
|  |  |  | Equivalent Series Resistance | Table 2 Item 4 | ESR | - | Table 2 | mΩ |
| 10 | Damp Heat Steady State | Para. 9.16 | Initial Measurements |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  | µF |
|  |  |  | Final Measurements | After recovery of 1 to 2 hours |  |  |  |  |
|  |  |  | Visual Examination | No damage | - | - | - |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | C/C | -10 | +10 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - | 1.5 x Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - | 1.2 x Table 2 | % |
|  |  |  | Equivalent Series Resistance | Table 2 Item 4 | ESR | - | 1.25 x Table 2 | mΩ |
| 11 | Operating Life | Para. 9.17 | Initial Measurements |  |  |  |  |  |
|  |  |  | Capacitance | Value recorded after Mounting | C | Table 2 |  | µF |
|  |  |  | Intermediate Measurements | At 250 and 1000 hrs |  |  |  |  |
|  |  |  | DC Leakage Current | Table 3 Item 2 (Note 2) | IL | - | 1.25 x Table 3 | µA |
|  |  |  | Final Measurements | At 1000 and 2000 hrs and after recovery or 1 to 2 hours |  |  |  |  |
|  |  |  | Capacitance Change | Table 2 Item 1 | C/C | -10 | +10 | % |
|  |  |  | DC Leakage Current | Table 2 Item 2 | IL | - | 1.25 x Table 2 | µA |
|  |  |  | Dissipation Factor | Table 2 Item 3 | DF | - | Table 2 | % |
|  |  |  | Equivalent Series Resistance | Table 2 Item 4 | ESR | - | 1.25 x Table 2 | mΩ |
|  |  |  | Visual Examination | No damage | - | - | - |  |
| 12 | Permanence of Marking | Para. 9.18 | Final Examination |  |  |  |  |  |
|  |  |  | Visual Examination | ESCC No. 24800 | - | - | - |  |
| 13 | Solderability | Para. 9.19, 4.2.4 and 4.2.5 of this spec | Final Examination |  |  |  |  |  |
|  |  |  | Visual Examination | ESCC No. 3012 Para. 9.13.3 and no damage | - | - | - |  |

NOTES:

The tests in this Table refer to either Chart IV or V and shall be used as applicable.

While still at the high temperature.

## APPENDIX ‘A’

Agreed Deviations for AVX Czech Republic s.r.o (CZ)

| Items Affected | Description of Deviations |
| --- | --- |
| Deviations from Final Production Tests (Chart II) | Para. 9.1, Internal Visual Inspection: Shall not be performed. Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |
| Deviations from Burn-in and Electrical Measurements (Chart III) | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |
| Deviations from Qualification Tests (Chart IV) | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |
| Deviations from Lot Acceptance Tests (Chart V) | Para. 9.5, External Visual Inspection: Visible base material is permitted on the edges of terminations (there is no plating on edges). |