DCR to ESCC 3009/039 issue 2

Addition to paragraph 1.4.1.1:

(c) Rated Voltage expressed by the following codes

| Rated Voltage (V) | Code Letter |
| --- | --- |
| 10 | Y |
| 16 | X |
| 25 | A |
| 50 | C |
| 100 | E |
| 200 | G |

Addition to paragraph 1.4.2:

| Variant Number | Style | Capacitance Range, Tolerance, Rated Voltage | Terminal Material and Finish |  | Weight Max (g) |
| --- | --- | --- | --- | --- | --- |
|  |  |  | End Terminations | Termination Finish |  |
| 01 | 0603 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.1 |
| 02 | 0805 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.1 |
| 03 | 1206 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 04 | 1210 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 05 | 1812 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.2 |
| 06 | 2220 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.3 |
| 07 | 0603 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.1 |
| 08 | 0805 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.1 |
| 09 | 1206 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.15 |
| 10 | 1210 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.15 |
| 11 | 1812 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.2 |
| 12 | 2220 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.3 |
| 13 (Note 4) | 0603 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.1 |
| 14 (Note 4) | 0805 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.1 |
| 15 (Note 4) | 1206 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 16 (Note 4) | 1210 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 17 (Note 4) | 1812 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.2 |
| 18 (Note 4) | 2220 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.3 |
| 19 (Note 4) | 0603 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.1 |
| 20 (Note 4) | 0805 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.1 |
| 21 (Note 4) | 1206 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.15 |
| 22 (Note 4) | 1210 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.15 |
| 23 (Note 4) | 1812 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.2 |
| 24 Note (4) | 2220 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.3 |
| 25 (Note 4) | 0402 | See Note 1 | Flexible + Ni barrier | Sn/Pb plating (Note 3) | 0.1 |
| 26 (Note 4) | 0402 | See Note 1 | Flexible + Ni barrier | Au plating (Note 2) | 0.1 |

Note 1.

            - Available rated voltages, capacitance values and tolerances are as follows:

| Variant Number | Style | Capacitance Range Cn (pF) |  | Rated Voltage UR (V) |
| --- | --- | --- | --- | --- |
|  |  | Min | Max |  |
| 01, 07 | 0603 | 10 | 1000 | 200 |
| 02, 08 | 0805 | 330 | 3900 |  |
| 03, 09 | 1206 | 470 | 12000 |  |
| 04, 10 | 1210 | 2200 | 27000 |  |
| 05, 11 | 1812 | 4700 | 47000 |  |
| 06, 12 | 2220 | 10000 | 120000 |  |
| 13, 19 | 0603 | 10 | 3900 |  |
| 14, 20 | 0805 | 330 | 15000 |  |
| 15, 21 | 1206 | 470 | 47000 |  |
| 16, 22 | 1210 | 2200 | 100000 |  |
| 17, 23 | 1812 | 4700 | 180000 |  |
| 18, 24 | 2220 | 10000 | 470000 |  |
| 01, 07 | 0603 | 10 | 2700 | 100 |
| 02, 08 | 0805 | 68 | 10000 |  |
| 03, 09 | 1206 | 470 | 27000 |  |
| 04, 10 | 1210 | 2200 | 56000 |  |
| 05, 11 | 1812 | 3900 | 120000 |  |
| 06, 12 | 2220 | 22000 | 270000 |  |
| 13, 19 | 0603 | 10 | 12000 |  |
| 14, 20 | 0805 | 68 | 47000 |  |
| 15, 21 | 1206 | 470 | 120000 |  |
| 16, 22 | 1210 | 2200 | 220000 |  |
| 17, 23 | 1812 | 3900 | 470000 |  |
| 18, 24 | 2220 | 22000 | 1000000 |  |
| 25, 26 | 0402 | 68 | 3300 | 50 |
| 01, 07 | 0603 | 10 | 10000 |  |
| 02, 08 | 0805 | 100 | 56000 |  |
| 03, 09 | 1206 | 470 | 82000 |  |
| 04, 10 | 1210 | 2200 | 220000 |  |
| 05, 11 | 1812 | 3900 | 470000 |  |
| 06, 12 | 2220 | 22000 | 1200000 |  |
| 13, 19 | 0603 | 10 | 22000 |  |
| 14, 20 | 0805 | 100 | 100000 |  |
| 15, 21 | 1206 | 470 | 180000 |  |
| 16, 22 | 1210 | 2200 | 390000 |  |
| 17, 23 | 1812 | 3900 | 820000 |  |
| 18, 24 | 2220 | 22000 | 1800000 |  |
| 25, 26 | 0402 | 68 | 5600 | 25 |
| 01, 07 | 0603 | 390 | 33000 |  |
| 02, 08 | 0805 | 6800 | 150000 |  |
| 03, 09 | 1206 | 10000 | 270000 |  |
| 04, 10 | 1210 | 33000 | 560000 |  |
| 05, 11 | 1812 | 100000 | 1200000 |  |
| 06, 12 | 2220 | 150000 | 2200000 |  |
| 13, 19 | 0603 | 390 | 33000 |  |
| 14, 20 | 0805 | 6800 | 150000 |  |
| 15, 21 | 1206 | 10000 | 270000 |  |
| 16, 22 | 1210 | 33000 | 560000 |  |
| 17, 23 | 1812 | 100000 | 1200000 |  |
| 18, 24 | 2220 | 150000 | 2200000 |  |
| 25, 26 | 0402 | 68 | 8200 | 16 |
| 01, 07 | 0603 | 390 | 100000 |  |
| 02, 08 | 0805 | 6800 | 390000 |  |
| 03, 09 | 1206 | 10000 | 1000000 |  |
| 04, 10 | 1210 | 33000 | 820000 |  |
| 05, 11 | 1812 | 100000 | 1200000 |  |
| 06, 12 | 2220 | 150000 | 2700000 |  |
| 13, 19 | 0603 | 390 | 100000 |  |
| 14, 20 | 0805 | 6800 | 390000 |  |
| 15, 21 | 1206 | 10000 | 1000000 |  |
| 16, 22 | 1210 | 33000 | 820000 |  |
| 17, 23 | 1812 | 100000 | 1800000 |  |
| 18, 24 | 2220 | 150000 | 3900000 |  |
| 25, 26 | 0402 | 10 | 12000 | 10 |
| 01, 07 | 0603 | 10 | 120000 |  |
| 02, 08 | 0805 | 68 | 470000 |  |
| 03, 09 | 1206 | 470 | 1500000 |  |
| 04, 10 | 1210 | 2200 | 2200000 |  |

Any capacitance value in the capacitance range may be available on request.

            - Variants 07 to 12 and 19 to 24 and 26 are not suitable for solder assembly methods. They shall be assembled using glue or wire bond techniques.

            - Sn/Pb plating, with typically 60% Sn, 40% Pb.

            - Variants 13 to 24 have X7R dielectric; see High and Low Temperature Electrical Measurements.

            - See Physical Dimensions.

Addition to paragraph 1.5 Maximum Ratings:

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Rated Voltage | UR | 10, 16, 25, 50, 100, 200 | V | Note 1 |
| Operating Temperature Range | Top | -55 to +125 | °C | Without derating. Tamb |
| Storage Temperature Range | Tstg | -55 to +125 | °C |  |
| Soldering Temperature | Tsol | +260 | °C | Note 2 |

NOTES:

            - As required; See Component Type Variants and Range of Components.

            - Duration 10 seconds maximum.

Addition to paragraph 1.6 Physical Dimensions:

| Symbols | Dimensions (mm) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Style 0402 Variants 25, 26 |  | Style 0603 Variants 01, 07, 13, 19 |  | Style 0805 Variants 02, 08, 14, 20 |  | Style 1206 Variants 03, 09, 15, 21 |  | Style 1210 Variants 04, 10, 16, 22 |  | Style 1812 Variants 05, 11, 17, 23 |  | Style 2220 Variants 06, 12, 18, 24 |  |
|  | Min | Max | Min | Max | Min | Max | Min | Max | Min | Max | Min | Max | Min | Max |
| L | 0.9 | 1.1 | 1.4 | 1.8 | 1.7 | 2.3 | 2.95 | 3.45 | 2.8 | 3.6 | 4 | 5 | 5.2 | 6.2 |
| I | 0.4 | 0.6 | 0.6 | 1 | 1.05 | 1.45 | 1.45 | 1.75 | 2.2 | 2.8 | 2.8 | 3.6 | 4.5 | 5.5 |
| e | - | 0.6 | - | 1 | - | 1.8 | - | 2.3 | - | 2.3 | - | 2.8 | - | 2.8 |
| M | 0.1 | 0.3 | 0.1 | 0.5 | 0.1 | 0.75 | 0.2 | 0.75 | 0.2 | 1 | 0.2 | 1 | 0.2 | 1 |

Addition to paragraph 2.1.1.1:

(a) Solderability: not applicable to variants 07 to 12, 19 to 24 and 26

Addition to paragraph 2.3.2:

| Characteristics | Symbols | Test Method and Conditions (Note 1) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Temperature Characteristic | TC | ESCC No. 3009 Tamb=-55±2°C, +20±2°C, +125±2°C Note 2 |  |  | % |
|  |  | For VT = no voltage applied All Variants: For VT = UR | -20 | +20 |  |
|  |  | Variants 01 to 12, 25 and 26: Variants 13 to 24: | -30 | +20 |  |
|  |  |  | Note 3 |  |  |