Page 1 of 20

CAPACITORS, FIXED, CERAMIC DIELECTRIC, TYPE II, HIGH CAPACITANCE, 50V TO 500V

BASED ON TYPES BR, CV AND CH

| ESCC Detail Specification No. 3001/030 Issue 8 Draft A | February 2017 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# LEGAL DISCLAIMER AND COPYRIGHT

European Space Agency, Copyright © 2017. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| TBA | Specification updated to incorporate changes per DCR. |

TABLE OF CONTENTS

1	GENERAL	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants and Range of Components	6

1.5	MAXIMUM RATINGS	9

1.6	PHYSICAL DIMENSIONS	10

1.6.1	Case Type BR with Radial Leads	10

1.6.2	Case Type CV with Radial Leads	11

1.6.3	Case Type CH with Straight DIL Leads	12

1.6.4	Case Type CH with L DIL Leads	14

1.7	FUNCTIONAL DIAGRAM	15

2	REQUIREMENTS	16

2.1	GENERAL	16

2.1.1	Deviations from the Generic Specification	16

2.2	MARKING	16

2.3	ROBUSTNESS OF TERMINATIONS	16

2.4	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	17

2.4.1	Room Temperature Electrical Measurements	17

2.4.2	High and Low Temperatures Electrical Measurements	17

2.5	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	18

2.6	BURN-IN	19

APPENDIX A	20

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3001.

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 300103001476KE

Detail Specification Reference: 3001030

Component Type Variant Number: 01 (as required)

Characteristic code: Capacitance Value (47μF): 476 (as required)

Characteristic code: Capacitance Tolerance (±10%): K (as required)

Rating code: Rated Voltage (100V): E (as required)

#### Characteristics and Ratings Codes

Characteristics and ratings to be codified as part of the ESCC Component Number shall be as follows:

Rated Capacitance Value Cn expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be picofarad (pF).

| Capacitance Value Cn (pF) | Code |
| --- | --- |
| XX 104 | XX4 |
| XX 105 | XX5 |
| XX 106 | XX6 |
| XX 107 | XX7 |

Capacitance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (± %) | Code Letter |
| --- | --- |
| 10 | K |
| 20 | M |

Rated Voltage expressed by the following codes:

| Rated Voltage UR (V) | Code Letter |
| --- | --- |
| 50 | C |
| 100 | E |
| 200 | G |
| 500 | L |

### Component Type Variants and Range of Components

The component type variants and range of components applicable to this specification are as follows:

| Variant Number | Package Details (Note 1) |  |  |  | Capacitance Range Cn (µF) (Note 4) |  |  |  | Weight Max (g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Case Type (Note 2) | Lead Type | No. of Leads | Lead Mat. & Fin. (Note 3) | Rated Voltage UR = 50V | Rated Voltage UR = 100V | Rated Voltage UR = 200V | Rated Voltage UR = 500V |  |
| 01 | BR40 | Radial | 2 | A3 | 1.8 to 3.3 | 1.2 to 2.7 | 0.33 to 0.56 | 0.12 to 0.22 | 2 |
| 02 | BR50 | Radial | 2 | A3 | 3.9 to 5.6 | 2.2 to 3.9 | 0.68 to 1 | 0.27 to 0.39 | 3 |
| 03 | BR66 | Radial | 2 | A3 | 6.8 to 10 | 4.7 to 8.2 | 1 to 2.2 | 0.47 to 1 | 5 |
| 04 | BR72 | Radial | 2 | A3 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 05 | BR84 | Radial | 2 | A3 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 06 | CV41 | Radial | 2 | A3 | 1.8 to 3.3 | 1.2 to 2.7 | 0.33 to 0.56 | 0.12 to 0.22 | 2 |
| 07 | CH41 | Straight DIL | 6 | N9 | 1.8 to 3.3 | 1.2 to 2.7 | 0.33 to 0.56 | 0.12 to 0.22 | 2 |
| 08 | CH41 | L DIL | 6 | N9 | 1.8 to 3.3 | 1.2 to 2.7 | 0.33 to 0.56 | 0.12 to 0.22 | 2 |
| 09 | CH42 | Straight DIL | 6 | N9 | 3.9 to 6.8 | 3.3 to 5.6 | 0.68 to 1.2 | 0.27 to 0.47 | 4 |
| 10 | CH42 | L DIL | 6 | N9 | 3.9 to 6.8 | 3.3 to 5.6 | 0.68 to 1.2 | 0.27 to 0.47 | 4 |
| 11 | CH43 | Straight DIL | 6 | N9 | 8.2 to 10 | 6.8 to 8.2 | 1.5 to 1.8 | 0.56 to 0.68 | 6 |
| 12 | CH43 | L DIL | 6 | N9 | 8.2 to 10 | 6.8 to 8.2 | 1.5 to 1.8 | 0.56 to 0.68 | 6 |
| 13 | CH44 | Straight DIL | 6 | N9 | 12 | 10 | 2.2 | 0.82 to 1 | 8 |
| 14 | CH44 | L DIL | 6 | N9 | 12 | 10 | 2.2 | 0.82 to 1 | 8 |
| 15 | CV51 | Radial | 2 | A3 | 3.9 to 5.6 | 2.2 to 3.9 | 0.68 to 1 | 0.27 to 0.39 | 3 |
| 16 | CH51 | Straight DIL | 8 | N9 | 3.9 to 5.6 | 2.2 to 3.9 | 0.68 to 1 | 0.27 to 0.39 | 3 |
| 17 | CH51 | L DIL | 8 | N9 | 3.9 to 5.6 | 2.2 to 3.9 | 0.68 to 1 | 0.27 to 0.39 | 3 |
| 18 | CH52 | Straight DIL | 8 | N9 | 6.8 to 10 | 4.7 to 8.2 | 1 to 2.2 | 0.47 to 0.82 | 6 |
| 19 | CH52 | L DIL | 8 | N9 | 6.8 to 10 | 4.7 to 8.2 | 1 to 2.2 | 0.47 to 0.82 | 6 |
| 20 | CH53 | Straight DIL | 8 | N9 | 12 to 15 | 10 to 12 | 2.7 to 3.3 | 1 to 1.2 | 9 |
| 21 | CH53 | L DIL | 8 | N9 | 12 to 15 | 10 to 12 | 2.7 to 3.3 | 1 to 1.2 | 9 |
| 22 | CH54 | Straight DIL | 8 | N9 | 18 to 22 | 15 | 3.9 | 1.5 | 12 |
| 23 | CH54 | L DIL | 8 | N9 | 18 to 22 | 15 | 3.9 | 1.5 | 12 |
| 24 | CV61 | Radial | 2 | A3 | 6.8 to 10 | 4.7 to 8.2 | 1 to 2.2 | 0.47 to 1 | 5 |
| 25 | CH61 | Straight DIL | 10 | N9 | 6.8 to 10 | 4.7 to 8.2 | 1 to 2.2 | 0.47 to 1 | 5 |
| 26 | CH61 | L DIL | 10 | N9 | 6.8 to 10 | 4.7 to 8.2 | 1 to 2.2 | 0.47 to 1 | 5 |
| 27 | CH62 | Straight DIL | 10 | N9 | 12 to 22 | 10 to 15 | 2.7 to 4.7 | 1 to 1.8 | 10 |
| 28 | CH62 | L DIL | 10 | N9 | 12 to 22 | 10 to 15 | 2.7 to 4.7 | 1 to 1.8 | 10 |
| 29 | CH63 | Straight DIL | 10 | N9 | 27 to 33 | 18 to 22 | 5.6 to 6.8 | 2.2 to 2.7 | 15 |
| 30 | CH63 | L DIL | 10 | N9 | 27 to 33 | 18 to 22 | 5.6 to 6.8 | 2.2 to 2.7 | 15 |
| 31 | CH64 | Straight DIL | 10 | N9 | 39 | 27 to 33 | 8.2 to 10 | 3.3 | 20 |
| 32 | CH64 | L DIL | 10 | N9 | 39 | 27 to 33 | 8.2 to 10 | 3.3 | 20 |
| 33 | CV71 | Radial | 2 | A3 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 34 | CH71 | Straight DIL | 14 | N9 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 35 | CH71 | L DIL | 14 | N9 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 36 | CH72 | Straight DIL | 14 | N9 | 22 to 39 | 18 to 27 | 3.9 to 6.8 | 1.8 to 3.3 | 16 |
| 37 | CH72 | L DIL | 14 | N9 | 22 to 39 | 18 to 27 | 3.9 to 6.8 | 1.8 to 3.3 | 16 |
| 38 | CH73 | Straight DIL | 14 | N9 | 47 to 56 | 33 to 39 | 8.2 to 10 | 3.9 to 4.7 | 24 |
| 39 | CH73 | L DIL | 14 | N9 | 47 to 56 | 33 to 39 | 8.2 to 10 | 3.9 to 4.7 | 24 |
| 40 | CH74 | Straight DIL | 14 | N9 | 68 | 47 | 12 | 5.6 | 32 |
| 41 | CH74 | L DIL | 14 | N9 | 68 | 47 | 12 | 5.6 | 32 |
| 42 | CV76 | Radial | 2 | A3 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 43 | CH76 | Straight DIL | 12 | N9 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 44 | CH76 | L DIL | 12 | N9 | 12 to 18 | 8.2 to 15 | 2.2 to 3.3 | 0.82 to 1.5 | 8 |
| 45 | CH77 | Straight DIL | 12 | N9 | 22 to 39 | 18 to 27 | 3.9 to 6.8 | 1.8 to 3.3 | 16 |
| 46 | CH77 | L DIL | 12 | N9 | 22 to 39 | 18 to 27 | 3.9 to 6.8 | 1.8 to 3.3 | 16 |
| 47 | CH78 | Straight DIL | 12 | N9 | 47 to 56 | 33 to 39 | 8.2 to 10 | 3.9 to 4.7 | 24 |
| 48 | CH78 | L DIL | 12 | N9 | 47 to 56 | 33 to 39 | 8.2 to 10 | 3.9 to 4.7 | 24 |
| 49 | CH79 | Straight DIL | 12 | N9 | 68 | 47 | 12 | 5.6 | 32 |
| 50 | CH79 | L DIL | 12 | N9 | 68 | 47 | 12 | 5.6 | 32 |
| 51 | CH81 | Straight DIL | 28 | N9 | 15 to 22 | 12 to 18 | 2.2 to 3.9 | 0.82 to 1.5 | 10 |
| 52 | CH81 | L DIL | 28 | N9 | 15 to 22 | 12 to 18 | 2.2 to 3.9 | 0.82 to 1.5 | 10 |
| 53 | CH82 | Straight DIL | 28 | N9 | 27 to 47 | 22 to 39 | 4.7 to 8.2 | 1.8 to 3.3 | 20 |
| 54 | CH82 | L DIL | 28 | N9 | 27 to 47 | 22 to 39 | 4.7 to 8.2 | 1.8 to 3.3 | 20 |
| 55 | CH83 | Straight DIL | 28 | N9 | 56 to 68 | 47 to 56 | 10 to 12 | 3.9 to 4.7 | 30 |
| 56 | CH83 | L DIL | 28 | N9 | 56 to 68 | 47 to 56 | 10 to 12 | 3.9 to 4.7 | 30 |
| 57 | CH84 | Straight DIL | 28 | N9 | 82 | 68 | 15 | 5.6 | 40 |
| 58 | CH84 | L DIL | 28 | N9 | 82 | 68 | 15 | 5.6 | 40 |
| 59 | CH86 | Straight DIL | 28 | N9 | 22 to 33 | 15 to 27 | 3.9 to 6.8 | 1.5 to 2.2 | 14 |
| 60 | CH86 | L DIL | 28 | N9 | 22 to 33 | 15 to 27 | 3.9 to 6.8 | 1.5 to 2.2 | 14 |
| 61 | CH87 | Straight DIL | 28 | N9 | 39 to 68 | 33 to 56 | 8.2 to 15 | 2.7 to 4.7 | 28 |
| 62 | CH87 | L DIL | 28 | N9 | 39 to 68 | 33 to 56 | 8.2 to 15 | 2.7 to 4.7 | 28 |
| 63 | CH88 | Straight DIL | 28 | N9 | 82 to 100 | 68 to 82 | 18 to 22 | 5.6 to 6.8 | 42 |
| 64 | CH88 | L DIL | 28 | N9 | 82 to 100 | 68 to 82 | 18 to 22 | 5.6 to 6.8 | 42 |
| 65 | CH89 | Straight DIL | 28 | N9 | 120 | 100 | 27 | 8.2 | 56 |
| 66 | CH89 | L DIL | 28 | N9 | 120 | 100 | 27 | 8.2 | 56 |
| 67 | CH91 | Straight DIL | 28 | N9 | 39 to 47 | 33 to 39 | 8.2 to 10 | 2.7 to 4.7 | 19 |
| 68 | CH91 | L DIL | 28 | N9 | 39 to 47 | 33 to 39 | 8.2 to 10 | 2.7 to 4.7 | 19 |
| 69 | CH92 | Straight DIL | 28 | N9 | 56 to 100 | 47 to 82 | 12 to 22 | 5.6 to 10 | 38 |
| 70 | CH92 | L DIL | 28 | N9 | 56 to 100 | 47 to 82 | 12 to 22 | 5.6 to 10 | 38 |
| 71 | CH93 | Straight DIL | 28 | N9 | 120 to 150 | 100 to 120 | 27 to 33 | 12 to 15 | 57 |
| 72 | CH93 | L DIL | 28 | N9 | 120 to 150 | 100 to 120 | 27 to 33 | 12 to 15 | 57 |
| 73 | CH94 | Straight DIL | 28 | N9 | 180 | 150 | 39 | 18 | 76 |
| 74 | CH94 | L DIL | 28 | N9 | 180 | 150 | 39 | 18 | 76 |

NOTES:

See Physical Dimensions.

For Variants 01 to 05 (case type BR) the body shall be coated with epoxy resin. Variants 06 to 74 (case types CV & CH) are classified as non-insulated.

The lead material and finishes shall be in accordance with the requirements of ESCC Basic Specification No. 23500.

Available capacitance values and tolerances are as follows:

Tolerance: ±10%; value series: E12

Tolerance: ±20%; value series: E12

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Rated Voltage | UR | 50, 100, 200, 500 | V | Note 1 |
| Operating Temperature Range | Top | -55 to +125 | °C | Without derating. Tamb |
| Storage Temperature Range | Tstg | -55 to +125 | °C |  |
| Soldering Temperature | Tsol | +260 | °C | Note 2 |

NOTES:

As required; See Component Type Variants and Range of Components.

Duration 5 seconds maximum at a distance of not less than 1.5mm from the body and the same lead shall not be resoldered until 3 minutes have elapsed.

## PHYSICAL DIMENSIONS

### Case Type BR with Radial Leads

| Variant Number | Case Type | Dimensions (mm) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | B Max | Ød (Note 1) |  | E |  | F Max | H Max | J Max | L Min (Note 1) |
|  |  |  | Min | Max | Min | Max |  |  |  |  |
| 01 | BR40 | 10.16 | 0.46 | 0.56 | 4.58 | 5.58 | 5 | 11.7 | 1.5 | 31.7 |
| 02 | BR50 | 12.7 | 0.59 | 0.69 | 9.66 | 10.66 | 5.1 | 14.2 | 1.5 | 31.7 |
| 03 | BR66 | 17.5 | 0.86 | 0.96 | 14.2 | 15.2 | 6.4 | 16.5 | 1.5 | 31.7 |
| 04 | BR72 | 19.3 | 0.86 | 0.96 | 14.74 | 15.74 | 6.4 | 24 | 1.5 | 31.7 |
| 05 | BR84 | 23.62 | 0.71 | 0.81 | 18.93 | 20.83 | 6.4 | 19.78 | 1.5 | 31.7 |

NOTES:

Both leads.

### Case Type CV with Radial Leads

| Variant Number | Case Type | Dimensions (mm) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | B Max | Ød (Note 1) |  | E |  | F Max | H Max | L (Note 1) |  |
|  |  |  | Min | Max | Min | Max |  |  | Min | Max |
| 06 | CV41 | 10.6 | 0.65 | 0.75 | 7.7 | 8.7 | 3.8 | 8.7 | 22 | 28 |
| 15 | CV51 | 11.9 | 0.85 | 0.95 | 9.66 | 10.66 | 3.8 | 10.7 | 22 | 28 |
| 24 | CV61 | 16.5 | 0.85 | 0.95 | 14.74 | 15.74 | 3.8 | 13.6 | 22 | 28 |
| 33 | CV71 | 17.8 | 0.85 | 0.95 | 14.74 | 15.74 | 3.8 | 21.6 | 22 | 28 |
| 42 | CV76 | 22.7 | 0.85 | 0.95 | 20.4 | 22 | 3.8 | 16.6 | 22 | 28 |

NOTES:

Both leads.

### Case Type CH with Straight DIL Leads

| Variant Number | Case Type | Dimensions (mm) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | A Max | a1 Max (Note 1) | b (Note 1) |  | b1 (Note 1) |  | D Max | E (Note 1) |  | e (Note 1) |  | F Max | L (Note 1) |  |
|  |  |  |  | Min | Max | Min | Max |  | Min | Max | Min | Max |  | Min | Max |
| 07 | CH41 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 12 | 14 |
| 09 | CH42 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 12 | 14 |
| 11 | CH43 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 12 | 14 |
| 13 | CH44 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 12 | 14 |
| 16 | CH51 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 12 | 14 |
| 18 | CH52 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 12 | 14 |
| 20 | CH53 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 12 | 14 |
| 22 | CH54 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 12 | 14 |
| 25 | CH61 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 12 | 14 |
| 27 | CH62 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 12 | 14 |
| 29 | CH63 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 12 | 14 |
| 31 | CH64 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 12 | 14 |
| 34 | CH71 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 12 | 14 |
| 36 | CH72 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 12 | 14 |
| 38 | CH73 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 12 | 14 |
| 40 | CH74 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 12 | 14 |
| 43 | CH76 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 12 | 14 |
| 45 | CH77 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 12 | 14 |
| 47 | CH78 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 12 | 14 |
| 49 | CH79 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 12 | 14 |
| 51 | CH81 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 12 | 14 |
| 53 | CH82 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 12 | 14 |
| 55 | CH83 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 12 | 14 |
| 57 | CH84 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 12 | 14 |
| 59 | CH86 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 12 | 14 |
| 61 | CH87 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 12 | 14 |
| 63 | CH88 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 12 | 14 |
| 65 | CH89 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 12 | 14 |
| 67 | CH91 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 12 | 14 |
| 69 | CH92 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 12 | 14 |
| 71 | CH93 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 12 | 14 |
| 73 | CH94 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 12 | 14 |

NOTES:

All leads.

### Case Type CH with L DIL Leads

| Variant Number | Case Type | Dimensions (mm) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | A Max | a1 Max (Note 1) | b (Note 1) |  | b1 (Note 1) |  | D Max | E (Note 1) |  | e (Note 1) |  | F Max | L (Note 1) |  |
|  |  |  |  | Min | Max | Min | Max |  | Min | Max | Min | Max |  | Min | Max |
| 08 | CH41 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 2.04 | 3.04 |
| 10 | CH42 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 2.04 | 3.04 |
| 12 | CH43 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 2.04 | 3.04 |
| 14 | CH44 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 8.7 | 7.7 | 8.7 | 2.49 | 2.59 | 9.2 | 2.04 | 3.04 |
| 17 | CH51 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 2.04 | 3.04 |
| 19 | CH52 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 2.04 | 3.04 |
| 21 | CH53 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 2.04 | 3.04 |
| 23 | CH54 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 10.7 | 9.66 | 10.66 | 2.49 | 2.59 | 10.7 | 2.04 | 3.04 |
| 26 | CH61 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 2.04 | 3.04 |
| 28 | CH62 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 2.04 | 3.04 |
| 30 | CH63 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 2.04 | 3.04 |
| 32 | CH64 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 13.6 | 13.5 | 14.5 | 2.49 | 2.59 | 14.9 | 2.04 | 3.04 |
| 35 | CH71 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 2.04 | 3.04 |
| 37 | CH72 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 2.04 | 3.04 |
| 39 | CH73 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 2.04 | 3.04 |
| 41 | CH74 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 21.6 | 14.74 | 15.74 | 2.49 | 2.59 | 16.8 | 2.04 | 3.04 |
| 44 | CH76 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 2.04 | 3.04 |
| 46 | CH77 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 2.04 | 3.04 |
| 48 | CH78 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 2.04 | 3.04 |
| 50 | CH79 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 16.6 | 19.52 | 21.12 | 2.49 | 2.59 | 21.6 | 2.04 | 3.04 |
| 52 | CH81 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 2.04 | 3.04 |
| 54 | CH82 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 2.04 | 3.04 |
| 56 | CH83 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 2.04 | 3.04 |
| 58 | CH84 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 9.66 | 10.66 | 2.49 | 2.59 | 12 | 2.04 | 3.04 |
| 60 | CH86 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 2.04 | 3.04 |
| 62 | CH87 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 2.04 | 3.04 |
| 64 | CH88 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 2.04 | 3.04 |
| 66 | CH89 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 38.2 | 14.74 | 15.74 | 2.49 | 2.59 | 18.9 | 2.04 | 3.04 |
| 68 | CH91 | 3.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 2.04 | 3.04 |
| 70 | CH92 | 7.4 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 2.04 | 3.04 |
| 72 | CH93 | 11.1 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 2.04 | 3.04 |
| 74 | CH94 | 14.8 | 2 | 0.45 | 0.55 | 0.204 | 0.304 | 40.6 | 19.52 | 21.12 | 2.49 | 2.59 | 24 | 2.04 | 3.04 |

NOTES:

All leads.

## FUNCTIONAL DIAGRAM

NOTES:

For case type CH, all leads on each side of the component are connected to the same capacitor terminal.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Special In-Process Controls (Chart F2)

Robustness of Terminations: Shall be replaced with a lead peel test as specified in Robustness of Terminations herein.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and as follows.

The information to be marked on the component shall be:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## ROBUSTNESS OF TERMINATIONS

The terminations of these devices are classified as rigid.

Robustness of Terminations shall be performed as a lead peel test on a sample of 5 components from each manufacturing lot with 0 failures allowed. The sample components shall be leaded but not encapsulated or coated. Where necessary, the leads of the component under test shall be bent through 90° in the plane of the joint such that a tensile force applied to the leads will result in a peeling force being applied to the leads’ joint.

A tensile force shall be applied evenly across the length, on the capacitor terminal, to all leads on that side of the component together, until the lead joint peels. All leads shall be tested.

The minimum peeling force shall be as follows:

For case types BR & CV: 8.9N

For case type CH: 22.25N

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

Electrical measurements shall be performed at room, high and low temperatures.

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | Test Method and Conditions | Tolerance (± %) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Capacitance (Note 1) | CA | ESCC No. 3001 |  |  |  | µF |
|  |  |  | 10 | 0.9Cn | 1.1Cn |  |
|  |  |  | 20 | 0.8Cn | 1.2Cn |  |
| Tangent of Loss Angle | tgδ | ESCC No. 3001 | All | - | 250 ×10-4 | - |
| Insulation Resistance (Dielectric) | RID | ESCC No. 3001 | All | 1000 | - | GΩ.nF |
| Insulation Resistance (Body Insulation) | RIB | ESCC No. 3001 Case type BR only Note 2 | All | 1000 | - | GΩ.nF |
| Voltage Proof (Dielectric) | VPD | ESCC No. 3001 | All |  |  | V |
|  |  | For UR < 500V |  | 2.5UR | - |  |
|  |  | For UR = 500V |  | 2UR | - |  |
| Voltage Proof (Body Insulation) | VPB | ESCC No. 3001 Case type BR only Note 2 | All |  |  | V |
|  |  | For UR < 500V |  | 2.5UR | - |  |
|  |  | For UR = 500V |  | 2UR | - |  |

NOTES:

Capacitance limits may be adjusted to take into account capacitance ageing, as specified in the Generic Specification.

The measurements shall be performed on a sample of 5 components from each manufacturing lot with 0 failures allowed. In the event of any failure a 100% inspection may be performed. In the case of a 100% inspection, a 1% total percent defective is allowed.

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | Test Method and Conditions (Note 1) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Temperature Characteristic | TC | ESCC No. 3001 Tamb = -55 ±2°C, +20 ±2°C, +125 ±2°C Note 2 |  |  | % |
|  |  | For VT = no voltage applied | -20 | +20 |  |
|  |  | For VT = UR | -50 | +30 |  |

NOTES:

The measurements shall be performed on a sample of 5 components from each manufacturing lot with 0 failures allowed. In the event of any failure a 100% inspection may be performed.

In the case of a 100% inspection, a 1% total percent defective is allowed.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

Unless otherwise specified the test methods and test conditions shall be as per the corresponding test defined in Room Temperature Electrical Measurements.

| Test Reference per ESCC No. 3001 | Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |  |
| Rapid Change of Temperature |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Note 1 |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -10 |  | +10 | % |
|  | Tangent of Loss Angle | tgδ | - |  | 500 ×10-4 | - |
| Steady State Humidity |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Note 1 |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -10 |  | +10 | % |
|  | Tangent of Loss Angle | tgδ | - |  | 500 ×10-4 | - |
|  | Insulation Resistance (Dielectric) Note 2 | RID | 30 |  | - | GΩ.nF |
|  | Insulation Resistance (Body Insulation) Notes 2, 3 | RIB | 30 |  | - | GΩ.nF |
| Operating Life |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Note 1 |  |  |  |
| Intermediate Measurements (1000 hours) (Note 4) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -15 |  | +15 | % |
|  | Insulation Resistance (Dielectric) Note 2 | RID | 100 |  | - | GΩ.nF |
|  | Insulation Resistance (Body Insulation) Notes 2, 3 | RIB | 100 |  | - | GΩ.nF |
| Final Measurements (1000 or 2000 hours) (Note 5) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -15 |  | +15 | % |
|  | Tangent of Loss Angle | tgδ | - |  | 500 ×10-4 | - |
|  | Insulation Resistance (Dielectric) Note 2 | RID | 100 |  | - | GΩ.nF |
|  | Insulation Resistance (Body Insulation) Notes 2, 3 | RIB | 100 |  | - | GΩ.nF |
|  | Voltage Proof (Dielectric) | VPD | Note 1 |  |  |  |
|  | Voltage Proof (Body Insulation) Note 3 | VPB | Note 1 |  |  |  |
| Capacitance-Temperature Characteristics | Temperature Characteristic | TC | Note 6 |  |  |  |
| Resistance to Soldering Heat |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Note 1 |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -15 |  | +15 | % |
|  | Insulation Resistance (Dielectric) Note 2 | RID | 1000 |  | - | GΩ.nF |
|  | Insulation Resistance (Body Insulation) Notes 2, 3 | RIB | 1000 |  | - | GΩ.nF |

NOTES:

As specified in Room Temperature Electrical Measurements.

Test conditions for Insulation Resistance shall be as specified in Steady State Humidity in the ESCC Generic Specification.

Case type BR only.

Intermediate measurements are optional at the Manufacturer’s discretion.

1000 hours is applicable to Periodic Testing for extension of qualification. 2000 hours is applicable to Qualification Testing, and to Periodic Testing for renewal of qualification after lapse.

As specified in High and Low Temperatures Electrical Measurements.

## BURN-IN

The requirements for Burn-in are specified in the ESCC Generic Specification. The following conditions shall also apply:

After Burn-in, the components shall be removed from the chamber and allowed to cool under normal atmospheric conditions for recovery for 24 hours minimum.

## APPENDIX A

AGREED DEVIATIONS FOR AVX LTD (GB)

| Items Affected | Description of Deviations |
| --- | --- |
| Deviations from Generic Specification: Special In-Process Controls (Chart F2) | Microsection Inspection: may be performed using AVX inspection document as per PID. |
|  | Internal Visual Inspection: may be performed using AVX inspection document as per PID. |
| Deviations from Generic Specification: Screening (Chart F3) | External Visual Inspection: may be performed using AVX inspection document as per PID. |
| Deviations from Generic Specification: Qualification and Periodic Tests (Chart F4) | External Visual Inspection: may be performed using AVX inspection document as per PID. |
| Room Temperature Electrical Measurements and Intermediate And End-Point Electrical Measurements | For UR = 200V, Insulation Resistance (Dielectric) and Insulation Resistance (Body Insulation) tested during Room Temperature Electrical Measurements, and Intermediate And End-Point Electrical Measurements for Operating Life and Resistance to Soldering Heat shall be measured with VT = UR. |