Page 1 of 24

DIODES, MICROWAVE, SILICON, HYPER-ABRUPT JUNCTION TUNING VARACTOR

BASED ON TYPES dh76XXX and EH76XXX

ESCC Detail Specification No. 5512/023

| Issue 5 Draft A | September 2017 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2017. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| tbc | Specification upissued to incorporate changes per DCR. |

TABLE OF CONTENTS

1	General	6

1.1	SCOPE	6

1.2	APPLICABLE DOCUMENTS	6

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	6

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	6

1.4.1	The ESCC Component Number	6

1.4.2	Component Type Variants	6

1.5	MAXIMUM RATINGS	9

1.6	Handling precautions	10

1.7	PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION	10

1.7.1	Ceramic Pill A (2 Leads) - Variants 01, 10, 19, 28, 37, 46, 55, 64	10

1.7.2	Ceramic Pill B - Variants 02, 11, 20, 29, 38, 47, 56, 65	11

1.7.3	Ceramic Pill C (Cathode Lead) - Variants 03, 12, 21, 30, 39, 48, 57, 66	12

1.7.4	Ceramic Pill D (Anode Lead) - Variants 04, 13, 22, 31, 40, 49, 58, 67	13

1.7.5	Ceramic Pill E (2 Leads) - Variants 05, 14, 23, 32, 41, 50, 59, 68	14

1.7.6	Ceramic Pill F (Anode Lead) - Variants 06, 15, 24, 33, 42, 51, 60, 69	15

1.7.7	Ceramic Pill G - Variants 07, 16, 25, 34, 43, 52, 61, 70	16

1.7.8	Ceramic Pill H - Variants 08, 17, 26, 35, 44, 53, 62, 71	17

1.7.9	Ceramic Pill I (2 Leads) - Variants 09, 18, 27, 36, 45, 54, 63, 72	18

1.7.10	Naked Die - Variants 73 to 80	19

1.8	FUNCTIONAL DIAGRAM	19

1.9	MATERIALS AND FINISHES	19

1.9.1	Materials and Finishes of Packaged Components	19

1.9.2	Materials and Finishes of Naked Die Components	20

2	REQUIREMENTS	20

2.1	GENERAL	20

2.1.1	Deviations from the Generic Specification	20

2.1.1.1	Deviations from Qualification and Periodic Testing – Chart F4	20

2.2	MARKING	20

2.3	Die Shear	20

2.4	TERMINAL STRENGTH	21

2.5	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	21

2.5.1	Room Temperature Electrical Measurements	21

2.5.2	High and Low Temperatures Electrical Measurements	22

2.6	PARAMETER DRIFT VALUES	22

2.7	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	23

2.8	BURN-IN 1 CONDITIONS	23

2.9	BURN-IN 2 CONDITIONS	23

2.10	OPERATING LIFE CONDITIONS	23

appendix ‘a’	24

# General

## SCOPE

This specification details the ratings, physical and electrical characteristics and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 5010

MIL-STD-750, Test Methods and Procedures for Semiconductor Devices

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 551202301

Detail Specification Reference: 5512023

Component Type Variant Number: 01 (as required)

### Component Type Variants

The component type variants applicable to this specification are as follows:

Packaged Components

| Variant Number | Based On Type | Package Type / Description | Total Capacitance CT (pF) |  | Tuning Ratio CT1/CT12 |  | Lead/Terminal Material and Finish (Note 1) |  | Weight Max (g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max | Min | Max | Anode | Cathode |  |
| 01 | DH76010 | Ceramic Pill A (2 Leads) | 0.9 | 1.34 | 3.8 | 5.1 | E2 | E2 | 0.02 |
| 02 | DH76010 | Ceramic Pill B | 0.9 | 1.34 | 3.8 | 5.1 | D7 | D7 | 0.02 |
| 03 | DH76010 | Ceramic Pill C (Cathode Lead) | 0.9 | 1.34 | 3.8 | 5.1 | D7 | E2 | 0.02 |
| 04 | DH76010 | Ceramic Pill D (Anode Lead) | 0.9 | 1.34 | 3.8 | 5.1 | E2 | D7 | 0.02 |
| 05 | DH76010 | Ceramic Pill E (2 Leads) | 0.9 | 1.34 | 3.8 | 5.1 | E2 | E2 | 0.02 |
| 06 | DH76010 | Ceramic Pill F (Anode Lead) | 0.9 | 1.34 | 3.8 | 5.1 | E2 | D7 | 0.02 |
| 07 | DH76010 | Ceramic Pill G | 0.94 | 1.42 | 3.5 | 4.7 | D7 | A7 | 0.15 |
| 08 | DH76010 | Ceramic Pill H | 1 | 1.5 | 3.3 | 4.4 | D7 | D7 | 0.06 |
| 09 | DH76010 | Ceramic Pill I (2 Leads) | 1 | 1.5 | 3.3 | 4.4 | E2 | E2 | 0.06 |
| 10 | DH76015 | Ceramic Pill A (2 Leads) | 1.3 | 1.94 | 4.1 | 5.5 | E2 | E2 | 0.02 |
| 11 | DH76015 | Ceramic Pill B | 1.3 | 1.94 | 4.1 | 5.5 | D7 | D7 | 0.02 |
| 12 | DH76015 | Ceramic Pill C (Cathode Lead) | 1.3 | 1.94 | 4.1 | 5.5 | D7 | E2 | 0.02 |
| 13 | DH76015 | Ceramic Pill D (Anode Lead) | 1.3 | 1.94 | 4.1 | 5.5 | E2 | D7 | 0.02 |
| 14 | DH76015 | Ceramic Pill E (2 Leads) | 1.3 | 1.94 | 4.1 | 5.5 | E2 | E2 | 0.02 |
| 15 | DH76015 | Ceramic Pill F (Anode Lead) | 1.3 | 1.94 | 4.1 | 5.5 | E2 | D7 | 0.02 |
| 16 | DH76015 | Ceramic Pill G | 1.34 | 2.02 | 3.9 | 5.2 | D7 | A7 | 0.15 |
| 17 | DH76015 | Ceramic Pill H | 1.4 | 2.1 | 3.7 | 4.9 | D7 | D7 | 0.06 |
| 18 | DH76015 | Ceramic Pill I (2 Leads) | 1.4 | 2.1 | 3.7 | 4.9 | E2 | E2 | 0.06 |
| 19 | DH76022 | Ceramic Pill A (2 Leads) | 1.86 | 2.78 | 4.3 | 5.7 | E2 | E2 | 0.02 |
| 20 | DH76022 | Ceramic Pill B | 1.86 | 2.78 | 4.3 | 5.7 | D7 | D7 | 0.02 |
| 21 | DH76022 | Ceramic Pill C (Cathode Lead) | 1.86 | 2.78 | 4.3 | 5.7 | D7 | E2 | 0.02 |
| 22 | DH76022 | Ceramic Pill D (Anode Lead) | 1.86 | 2.78 | 4.3 | 5.7 | E2 | D7 | 0.02 |
| 23 | DH76022 | Ceramic Pill E (2 Leads) | 1.86 | 2.78 | 4.3 | 5.7 | E2 | E2 | 0.02 |
| 24 | DH76022 | Ceramic Pill F (Anode Lead) | 1.86 | 2.78 | 4.3 | 5.7 | E2 | D7 | 0.02 |
| 25 | DH76022 | Ceramic Pill G | 1.9 | 2.86 | 4.1 | 5.5 | D7 | A7 | 0.15 |
| 26 | DH76022 | Ceramic Pill H | 1.96 | 2.94 | 3.9 | 5.3 | D7 | D7 | 0.06 |
| 27 | DH76022 | Ceramic Pill I (2 Leads) | 1.96 | 2.94 | 3.9 | 5.3 | E2 | E2 | 0.06 |
| 28 | DH76033 | Ceramic Pill A (2 Leads) | 2.74 | 4.1 | 4.5 | 6 | E2 | E2 | 0.02 |
| 29 | DH76033 | Ceramic Pill B | 2.74 | 4.1 | 4.5 | 6 | D7 | D7 | 0.02 |
| 30 | DH76033 | Ceramic Pill C (Cathode Lead) | 2.74 | 4.1 | 4.5 | 6 | D7 | E2 | 0.02 |
| 31 | DH76033 | Ceramic Pill D (Anode Lead) | 2.74 | 4.1 | 4.5 | 6 | E2 | D7 | 0.02 |
| 32 | DH76033 | Ceramic Pill E (2 Leads) | 2.74 | 4.1 | 4.5 | 6 | E2 | E2 | 0.02 |
| 33 | DH76033 | Ceramic Pill F (Anode Lead) | 2.74 | 4.1 | 4.5 | 6 | E2 | D7 | 0.02 |
| 34 | DH76033 | Ceramic Pill G | 2.74 | 4.18 | 4.3 | 5.8 | D7 | A7 | 0.15 |
| 35 | DH76033 | Ceramic Pill H | 2.84 | 4.26 | 4.2 | 5.6 | D7 | D7 | 0.06 |
| 36 | DH76033 | Ceramic Pill I (2 Leads) | 2.84 | 4.26 | 4.2 | 5.6 | E2 | E2 | 0.06 |
| 37 | DH76047 | Ceramic Pill A (2 Leads) | 3.86 | 5.78 | 4.6 | 6.1 | E2 | E2 | 0.02 |
| 38 | DH76047 | Ceramic Pill B | 3.86 | 5.78 | 4.6 | 6.1 | D7 | D7 | 0.02 |
| 39 | DH76047 | Ceramic Pill C (Cathode Lead) | 3.86 | 5.78 | 4.6 | 6.1 | D7 | E2 | 0.02 |
| 40 | DH76047 | Ceramic Pill D (Anode Lead) | 3.86 | 5.78 | 4.6 | 6.1 | E2 | D7 | 0.02 |
| 41 | DH76047 | Ceramic Pill E (2 Leads) | 3.86 | 5.78 | 4.6 | 6.1 | E2 | E2 | 0.02 |
| 42 | DH76047 | Ceramic Pill F (Anode Lead) | 3.86 | 5.78 | 4.6 | 6.1 | E2 | D7 | 0.02 |
| 43 | DH76047 | Ceramic Pill G | 3.9 | 5.86 | 4.5 | 6 | D7 | A7 | 0.15 |
| 44 | DH76047 | Ceramic Pill H | 3.96 | 5.94 | 4.4 | 5.8 | D7 | D7 | 0.06 |
| 45 | DH76047 | Ceramic Pill I (2 Leads) | 3.96 | 5.94 | 4.4 | 5.8 | E2 | E2 | 0.06 |
| 46 | DH76068 | Ceramic Pill A (2 Leads) | 5.54 | 8.3 | 4.6 | 6.2 | E2 | E2 | 0.02 |
| 47 | DH76068 | Ceramic Pill B | 5.54 | 8.3 | 4.6 | 6.2 | D7 | D7 | 0.02 |
| 48 | DH76068 | Ceramic Pill C (Cathode Lead) | 5.54 | 8.3 | 4.6 | 6.2 | D7 | E2 | 0.02 |
| 49 | DH76068 | Ceramic Pill D (Anode Lead) | 5.54 | 8.3 | 4.6 | 6.2 | E2 | D7 | 0.02 |
| 50 | DH76068 | Ceramic Pill E (2 Leads) | 5.54 | 8.3 | 4.6 | 6.2 | E2 | E2 | 0.02 |
| 51 | DH76068 | Ceramic Pill F (Anode Lead) | 5.54 | 8.3 | 4.6 | 6.2 | E2 | D7 | 0.02 |
| 52 | DH76068 | Ceramic Pill G | 5.58 | 8.38 | 4.6 | 6.1 | D7 | A7 | 0.15 |
| 53 | DH76068 | Ceramic Pill H | 5.64 | 8.46 | 4.5 | 6 | D7 | D7 | 0.06 |
| 54 | DH76068 | Ceramic Pill I (2 Leads) | 5.64 | 8.46 | 4.5 | 6 | E2 | E2 | 0.06 |
| 55 | DH76100 | Ceramic Pill A (2 Leads) | 8.1 | 12.14 | 4.7 | 6.3 | E2 | E2 | 0.02 |
| 56 | DH76100 | Ceramic Pill B | 8.1 | 12.14 | 4.7 | 6.3 | D7 | D7 | 0.02 |
| 57 | DH76100 | Ceramic Pill C (Cathode Lead) | 8.1 | 12.14 | 4.7 | 6.3 | D7 | E2 | 0.02 |
| 58 | DH76100 | Ceramic Pill D (Anode Lead) | 8.1 | 12.14 | 4.7 | 6.3 | E2 | D7 | 0.02 |
| 59 | DH76100 | Ceramic Pill E (2 Leads) | 8.1 | 12.14 | 4.7 | 6.3 | E2 | E2 | 0.02 |
| 60 | DH76100 | Ceramic Pill F (Anode Lead) | 8.1 | 12.14 | 4.7 | 6.3 | E2 | D7 | 0.02 |
| 61 | DH76100 | Ceramic Pill G | 8.14 | 12.22 | 4.2 | 6.2 | D7 | A7 | 0.15 |
| 62 | DH76100 | Ceramic Pill H | 8.2 | 12.3 | 4.6 | 6.1 | D7 | D7 | 0.06 |
| 63 | DH76100 | Ceramic Pill I (2 Leads) | 8.2 | 12.3 | 4.6 | 6.1 | E2 | E2 | 0.06 |
| 64 | DH76150 | Ceramic Pill A (2 Leads) | 12.1 | 18.14 | 4.7 | 6.3 | E2 | E2 | 0.02 |
| 65 | DH76150 | Ceramic Pill B | 12.1 | 18.14 | 4.7 | 6.3 | D7 | D7 | 0.02 |
| 66 | DH76150 | Ceramic Pill C (Cathode Lead) | 12.1 | 18.14 | 4.7 | 6.3 | D7 | E2 | 0.02 |
| 67 | DH76150 | Ceramic Pill D (Anode Lead) | 12.1 | 18.14 | 4.7 | 6.3 | E2 | D7 | 0.02 |
| 68 | DH76150 | Ceramic Pill E (2 Leads) | 12.1 | 18.14 | 4.7 | 6.3 | E2 | E2 | 0.02 |
| 69 | DH76150 | Ceramic Pill F (Anode Lead) | 12.1 | 18.14 | 4.7 | 6.3 | E2 | D7 | 0.02 |
| 70 | DH76150 | Ceramic Pill G | 12.1 | 18.22 | 4.7 | 6.3 | D7 | A7 | 0.15 |
| 71 | DH76150 | Ceramic Pill H | 12.2 | 18.3 | 4.7 | 6.2 | D7 | D7 | 0.06 |
| 72 | DH76150 | Ceramic Pill I (2 Leads) | 12.2 | 18.3 | 4.7 | 6.2 | E2 | E2 | 0.06 |

Naked Die Components (Note 2)

| Variant Number | Based On Type | Junction Capacitance CJ (pF) |  | Tuning Ratio CJ1/CJ12 |  | Total Capacitance CT (pF) (Note 3) |  | Tuning Ratio CT1/CT12 (Note 3) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min | Max | Min | Max | Min | Max | Min | Max |
| 73 | EH76010 | 0.8 | 1.2 | 4.6 | 6.1 | 0.94 | 1.42 | 3.5 | 4.7 |
| 74 | EH76015 | 1.2 | 1.8 | 4.7 | 6.3 | 1.34 | 2.02 | 3.9 | 5.2 |
| 75 | EH76022 | 1.76 | 2.64 | 4.7 | 6.3 | 1.9 | 2.86 | 4.1 | 5.5 |
| 76 | EH76033 | 2.64 | 3.96 | 4.8 | 6.4 | 2.74 | 4.18 | 4.3 | 5.8 |
| 77 | EH76047 | 3.76 | 5.64 | 4.8 | 6.4 | 3.9 | 5.86 | 4.5 | 6 |
| 78 | EH76068 | 5.44 | 8.16 | 4.8 | 6.4 | 5.58 | 8.38 | 4.6 | 6.1 |
| 79 | EH76100 | 8 | 12 | 4.8 | 6.4 | 8.14 | 12.22 | 4.2 | 6.2 |
| 80 | EH76150 | 12 | 18 | 4.8 | 6.4 | 12.1 | 18.22 | 4.7 | 6.3 |

notes:

The lead/terminal material and finish shall be in accordance with the requirements of ESCC Basic Specification No. 23500.

For Naked Die Components, Variants 73 to 80, the default package selected for assembly of the Packaged Test Sublot shall be Ceramic Pill G. At the Manufacturer’s option, any of the other packages specified herein with a Variant for the same die may be selected. The die applicable to each Variant is indicated by the based on type number.

In cases where the default package is not selected for the Packaged Test Sublot, the Total Capacitance and Tuning Ratio limits of the selected package shall apply.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Unit | Remarks |
| --- | --- | --- | --- | --- |
| Reverse Voltage | VRmax | -20 | V | IR = 10µA Note 1 |
| Operating Temperature Range | Top | -55 to +150 | °C | Tamb |
| Storage Temperature Range | Tstg | -65 to +175 | °C |  |
| Soldering Temperature | Tsol | +230 | °C | Note 2 |

NOTES:

At Tamb ≤ +25°C. For Tamb > +25°C, derate linearly to -16V at Tamb = +150°C.

Duration 5 seconds maximum and the same terminal shall not be resoldered until 3 minutes have elapsed. Only applicable to Variants 01 to 72 (Packaged Components).

## Handling precautions

These devices are susceptible to damage by electrostatic discharge. Therefore, suitable precautions shall be employed for protection during all phases of manufacture, testing, packaging, shipment and any handling.

Variants 01 to 45, 55 to 77, 79 and 80 are categorised as Class 2 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 2500V.

Variants 46 to 54 and 78 are categorised as Class 3 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 5000V.

## PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION

### Ceramic Pill A (2 Leads) - Variants 01, 10, 19, 28, 37, 46, 55, 64

| Symbols | Dimensions mm |  | Remarks |
| --- | --- | --- | --- |
|  | Min | Max |  |
| ØA | 1.07 | 1.47 |  |
| B | 0.95 | 1.35 |  |
| C | 1.3 | 1.9 | Both terminals |
| D | 2.5 | - |  |
| E | 0.55 | 0.65 | Both terminals |
| F | 0.06 | 0.1 | Both terminals |
| G | 0.1 | 0.5 | Both terminals |

NOTES:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill B - Variants 02, 11, 20, 29, 38, 47, 56, 65

| Symbols | Dimensions mm |  |
| --- | --- | --- |
|  | Min | Max |
| ØA | 1.07 | 1.47 |
| B | 0.95 | 1.35 |

NOTES:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill C (Cathode Lead) - Variants 03, 12, 21, 30, 39, 48, 57, 66

|  | Symbols | Dimensions mm |  |
| --- | --- | --- | --- |
|  |  | Min | Max |
|  | ØA | 1.07 | 1.47 |
|  | B | 0.95 | 1.35 |
|  | C | 5 | - |
|  | D | 0.55 | 0.65 |
|  | E | 0.06 | 0.1 |

notes:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill D (Anode Lead) - Variants 04, 13, 22, 31, 40, 49, 58, 67

|  | Symbols | Dimensions mm |  |
| --- | --- | --- | --- |
|  |  | Min | Max |
|  | ØA | 1.07 | 1.47 |
|  | B | 0.95 | 1.35 |
|  | C | 5 | - |
|  | D | 0.55 | 0.65 |
|  | E | 0.06 | 0.1 |

notes:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill E (2 Leads) - Variants 05, 14, 23, 32, 41, 50, 59, 68

| Symbols | Dimensions mm |  | Remarks |
| --- | --- | --- | --- |
|  | Min | Max |  |
| ØA | 1.07 | 1.47 |  |
| B | 0.95 | 1.35 |  |
| C | 5 | - |  |
| D | 0.55 | 0.65 | Both terminals |
| E | 0.06 | 0.1 | Both terminals |

notes:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill F (Anode Lead) - Variants 06, 15, 24, 33, 42, 51, 60, 69

|  | Symbols | Dimensions mm |  |
| --- | --- | --- | --- |
|  |  | Min | Max |
|  | ØA | 1.07 | 1.47 |
|  | B | 0.95 | 1.35 |
|  | C | 10 | 10.4 |
|  | D | 5 | - |
|  | E | 0.55 | 0.65 |
|  | F | 0.06 | 0.1 |

notes:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill G - Variants 07, 16, 25, 34, 43, 52, 61, 70

|  | Symbols | Dimensions mm |  |
| --- | --- | --- | --- |
|  |  | Min | Max |
|  | A | 1.52 | 1.63 |
|  | B | 1.75 | 1.85 |
|  | D | 5.2 | 5.72 |
|  | ØE | 1.52 | 1.63 |
|  | ØG | 3 | 3.23 |
|  | ØH | 1.95 | 2.11 |

notes:

Terminal identification shall be by means of the physical configuration of the package.

### Ceramic Pill H - Variants 08, 17, 26, 35, 44, 53, 62, 71

| Symbols | Dimensions mm |  |
| --- | --- | --- |
|  | Min | Max |
| A | 1.4 | 1.6 |
| ØD | 2.94 | 3.14 |
| ØD1 | 1.93 | 2.13 |

notes:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Ceramic Pill I (2 Leads) - Variants 09, 18, 27, 36, 45, 54, 63, 72

| Symbols | Dimensions mm |  | Remarks |
| --- | --- | --- | --- |
|  | Min | Max |  |
| B | 1.38 | 1.73 |  |
| d | 0.07 | 0.08 |  |
| d1 | 0.95 | 1.05 | Both terminals |
| ØD | 2.95 | 3.15 |  |
| ØD1 | 1.93 | 2.13 |  |
| L | 9 | - |  |

notes:

Terminal identification: The body shall be marked at a suitable location near the cathode terminal with a black dot.

### Naked Die - Variants 73 to 80

| Symbols | Dimensions mm |  | Remarks |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 0.34 | 0.4 |  |
| B | 0.16 | 0.26 |  |
| ØC | 0.03 0.05 0.07 0.09 0.11 0.13 0.15 0.18 | 0.06 0.08 0.1 0.12 0.14 0.16 0.19 0.23 | Variant 73 Variant 74 Variant 75 Variant 76 Variant 77 Variant 78 Variant 79 Variant 80 |

notes:

Terminal identification shall be by means of the physical configuration.

## FUNCTIONAL DIAGRAM

## MATERIALS AND FINISHES

### Materials and Finishes of Packaged Components

For Variants 01 to 72, the materials and finishes shall be as follows:

Case

- The case shall be hermetically sealed and have a ceramic body with a metal base and lid.

Leads/Terminals

- As specified in Para. 1.4.2.

### Materials and Finishes of Naked Die Components

For Variants 73 to 80, the materials and finishes shall be as follows:

Bond pad

- The bond pad metallisation shall be TiPtAu with a layer of vacuum-deposited gold of thickness 0.7µm minimum.

Die backface

- The die backface metallisation shall be TiPtAu with a layer of gold of thickness 0.7µm minimum.

Glassivation

- The glassivation material shall be silicon oxide or silicon nitride of thickness 0.25µm typical.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Qualification and Periodic Testing – Chart F4

Mechanical Shock: Shall not be performed.

Vibration: Shall not be performed.

Constant Acceleration: Shall not be performed.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and as follows.

The information to be marked on the component shall be:

Terminal identification, as specified in Para. 1.7.

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## Die Shear

In those cases where package clearances are such that a die shear test is not practicable, the die shall be pushed away with a suitable tool. The force required to remove the die need not be recorded. The die attachment area shall be inspected and the component shall be considered acceptable if more than 50% of the semiconductor material remains.

## TERMINAL STRENGTH

The test conditions for terminal strength, tested as specified in the ESCC Generic Specification, shall be as follows:

For Variants 01, 03 to 06, 09, 10, 12 to 15, 18, 19, 21 to 24, 27, 28, 30 to 33, 36, 37, 39 to 42,

- 45, 46, 48 to 51, 54, 55, 57 to 60, 63, 64, 66 to 69, 72: Test Condition A, tension, with a force of 1.25N for duration 10s.

For Variants 02, 07, 08, 11, 16, 17, 20, 25, 26, 29, 34, 35, 38, 43, 44, 47, 52, 53, 56, 61, 62, 65, 70, 71: shall not be performed.

For Variants 73 to 80: not applicable.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Reverse Current 1 (Note 1) | IR1 | 4016 | VR = -20V | - | 10 | µA |
| Reverse Current 2 (Note 1) | IR2 | 4016 | VR = -16V | - | 50 | nA |
| Forward Voltage (Note 1) | VF | 4011 | IF = 10mA | - | 1 | V |
| Total Capacitance (Note 2) | CT | 4001 | VR = -4V, f = 1MHz | Note 3 | Note 3 | pF |
| Junction Capacitance (Note 4) | CJ | 4001 | VR = -4V, f = 1MHz | Note 3 | Note 3 | pF |
| Tuning Ratio (Notes 2, 5) | CT1/CT12 | 4001 | VR = -1V and -12V f = 1MHz | Note 3 | Note 3 | - |
| Tuning Ratio (Notes 4, 6) | CJ1/CJ12 | 4001 | VR = -1V and -12V f = 1MHz | Note 3 | Note 3 | - |
| Quality Factor (Note 7) | Q | - | VR = -4V, f = 1GHz |  |  | - |
| Variants 01 to 09, 73: Variants 10 to 18, 74: Variants 19 to 27, 75: Variants 28 to 36, 76: Variants 37 to 45, 77: Variants 46 to 54, 78: Variants 55 to 63, 79: Variants 64 to 72, 80: |  |  |  | 100 90 75 58 40 25 12 4 | - - - - - - - - |  |

NOTES:

This characteristic applies to all Variants tested during Charts F2 and F3 of the Generic Specification.

This characteristic applies to Variants 01 to 72 (Packaged Components) and Variants 73 to 80 (Packaged Test Sublot samples for Naked Die Components), tested only during Chart F3 of the Generic Specification.

See Para. 1.4.2 for the applicable limits.

This characteristic applies only to Variants 73 to 80 (Naked Die Components), tested only during Chart F2 of the Generic Specification.

For Variants 01 to 72 (Packaged Components) and Variants 73 to 80 (Packaged Test Sublot samples for Naked Die Components) tested during Chart F3 of the Generic Specification, the Tuning Ratio is determined by dividing the Total Capacitance at VR = -1V by the Total Capacitance at VR = -12V.

For Variants 73 to 80 (Naked Die Components) tested during Chart F2 of the Generic Specification, the Tuning Ratio is determined by dividing the Junction Capacitance at VR = -1V by the Junction Capacitance at VR = -12V.

Guaranteed but not tested.

### High and Low Temperatures Electrical Measurements

The measurements shall be performed only at Tamb = +150 (+0 -3)°C.

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions Note 1 | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Reverse Current 2 (Note 2) | IR2 | 4016 | VR = -16V | - | 10 | µA |

NOTES:

Measurements shall be performed on a sample basis as specified in the Generic Specification.

This characteristic applies to all Variants tested during Charts F2 and F3 of the Generic Specification.

## PARAMETER DRIFT VALUES

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.5.1.

The drift values (Δ) shall not be exceeded for each characteristic specified. The corresponding absolute limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  | Drift Value (1) Δ | Absolute |  |  |
|  |  |  | Min | Max |  |
| Reverse Current 2 | IR2 | ±10 or (2) ±100% | - | 50 | nA |
| Forward Voltage | VF | ±5% | - | 1 | V |
| Total Capacitance (Note 3) | CT | ±5% | Note 4 | Note 4 | pF |

NOTES:

Δ1 = Δ2.

Whichever is the greater referred to the initial value.

This characteristic applies to Variants 01 to 72 (Packaged Components) and Variants 73 to 80 (Packaged Test Sublot samples for Naked Die Components).

See Para. 1.4.2 for the applicable limits.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.5.1.

The limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- |
|  |  | Min | Max |  |
| Reverse Current 2 | IR2 | - | 20 | µA |
| Forward Voltage | VF | - | 1 | V |
| Total Capacitance (Note 1) | CT | Note 2 | Note 2 | pF |

NOTES:

This characteristic applies to Variants 01 to 72 (Packaged Components) and Variants 73 to 80 (Packaged Test Sublot samples for Naked Die Components).

See Para. 1.4.2 for the applicable limits.

## BURN-IN 1 CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +150 (+0 -3) | °C |
| Reverse Voltage | VR | -16 | V |

## BURN-IN 2 CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +125 (+0 -3) | °C |
| Forward Current | IF | 50 | mA |

## OPERATING LIFE CONDITIONS

The conditions shall be as specified in Para. 2.8.

## appendix ‘a’

agreed deviations for cobham microwave (f)

| Items Affected | Description of Deviations |
| --- | --- |
| Para. 2.1.1, Deviations from the Generic Specification: Deviations from Special In-Process Controls – Chart F2 | SEM Inspection: SEM inspection shall be performed on three dice from one wafer per metallisation run, selected after die separation. |
|  | Bond Strength: The following pre-seal bond strength shall apply: 0.03N minimum |
| Para. 2.1.1, Deviations from the Generic Specification: Deviations from Screening Tests for Packaged Components – Chart F3A | Radiographic Inspection: Shall not be performed on Packaged Test Sublot samples for Naked Die Components. May be performed without serialisation and at any point during Chart F3A. Any components found to fail Radiographic Inspection shall be removed from the lot. May be performed in the X and Z axes only. |
| Para. 2.1.1.1, Deviations from Qualification and Periodic Testing – Chart F4 | For the De-encapsulation Subgroup, the Internal Visual Inspection, Bond Strength and Die Shear tests may be replaced by measurements verifying the die solder integrity and wire integrity, as follows: Thermal Impedance test in accordance with MIL-STD-750, Test Method 3101. PD = 0.25W. - The Thermal Impedance shall be measured and shall not exceed 150°C/W. Forward Voltage test in accordance with MIL-STD-750, Test Method 4011. IF =100mA. - The Forward Voltage shall be measured and shall not exceed 1.2V. |