Page 1 of 17

CAPACITORS, MICROWAVE, SILICON, MOS, NAKED DIE

BASED ON TYPEs 101m, 201m, 400m and 401m

ESCC Detail Specification No. 5711/002

| Issue 4 Draft A | September 2017 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2017. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| tbc | Specification upissued to incorporate changes per DCR. |

TABLE OF CONTENTS

1	General	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.1.1	Characteristics and Ratings Codes	5

1.4.2	Component Type Variants and Range of Components	6

1.5	MAXIMUM RATINGS	7

1.6	handling precautions	8

1.7	PHYSICAL DIMENSIONS	8

1.7.1	Variants 01 to 10	8

1.7.2	Variants 11 to 23	8

1.7.3	Variants 24, 25, 26	9

1.7.4	Variants 27, 28 and 29	10

1.7.5	Variant 30	11

1.7.6	Variant 31	12

1.8	FUNCTIONAL DIAGRAM	12

1.9	MATERIALS AND FINISHES	12

2	REQUIREMENTS	13

2.1	GENERAL	13

2.1.1	Deviations from the Generic Specification	13

2.1.1.1	Deviations from Production Control (Chart F2)	13

2.1.1.2	Deviations from Screening Tests for Die Components – Chart F3B	13

2.2	MARKING	13

2.3	die shear	13

2.4	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	14

2.4.1	Room Temperature Electrical Measurements	14

2.4.2	High and Low Temperatures Electrical Measurements	14

2.5	PARAMETER DRIFT VALUES	15

2.6	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	15

2.7	BURN-IN 2 CONDITIONS	16

2.8	OPERATING LIFE CONDITIONS	16

APPENDIX A	17

# General

## SCOPE

This specification details the ratings, physical and electrical characteristics and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 5010

MIL-STD-750, Test Methods and Procedures for Semiconductor Devices

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 5711002012C2KG

Detail Specification Reference: 5711002

Component Type Variant Number: 01 (as required)

Characteristic code: Capacitance Value (2.2pF): 2C2 (as required)

Characteristic code: Tolerance (±10%): K (as required)

Rating code: Rated Voltage (200V): G (as required)

#### Characteristics and Ratings Codes

Characteristics and ratings to be codified as part of the ESCC Component Number shall be as follows:

Rated Capacitance Value Cn expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be picofarads (pF):

| Capacitance Value Cn (pF) | Code |
| --- | --- |
| 0.XX | CXX |
| X.X | XCX |
| XX | XX0 |
| XX101 | XX1 |

Capacitance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (± %) | Code Letter |
| --- | --- |
| 10 | K |
| 20 | M |

Rated Voltage expressed by the following codes:

| Rated Voltage UR (V) | Code Letter |
| --- | --- |
| 40 | B |
| 100 | E |
| 200 | G |
| 400 | K |

### Component Type Variants and Range of Components

The component type variants and the associated range of components applicable to this specification are as follows:

| Variant Number | Based on Type | Capacitance Values Cn (pF) | Capacitance Tolerance (± %) | Rated Voltage UR (V) |
| --- | --- | --- | --- | --- |
| 01 | 201M106C | 2.2, 2.7, 3.3 | 10, 20 | 200 |
| 02 | 101M106C | 3.9, 4.7, 5.6, 6.8 | 10, 20 | 100 |
| 03 | 400M106C | 8.2, 10, 12, 15 | 10, 20 | 40 |
| 04 | 201M107C | 3.9, 4.7, 5.6, 6.8, 8.2 | 10, 20 | 200 |
| 05 | 101M107C | 10, 12, 15 | 10, 20 | 100 |
| 06 | 400M107C | 18, 22, 27, 33, 39 | 10, 20 | 40 |
| 07 | 201M108C | 10, 12, 15, 18 | 10, 20 | 200 |
| 08 | 101M108C | 22, 27, 33, 39 | 10, 20 | 100 |
| 09 | 400M108C | 47, 56, 68 | 10, 20 | 40 |
| 10 | 400M110C | 82, 100 | 10, 20 | 40 |
| 11 | 201M106A | 0.22, 0.27, 0.33, 0.39, 0.47, 0.56, 0.68, 0.82, 1, 1.2, 1.5, 1.8, 2.2, 2.7, 3.3 | 10, 20 | 200 |
| 12 | 101M106A | 3.9, 4.7, 5.6, 6.8 | 10, 20 | 100 |
| 13 | 400M106A | 8.2, 10, 12, 15 | 10, 20 | 40 |
| 14 | 201M104A | 3.9, 4.7, 5.6, 6.8 | 10, 20 | 200 |
| 15 | 101M104A | 10, 12 | 10, 20 | 100 |
| 16 | 400M104A | 18, 22, 27 | 10, 20 | 40 |
| 17 | 201M107A | 8.2 | 10, 20 | 200 |
| 18 | 101M107A | 15 | 10, 20 | 100 |
| 19 | 400M107A | 33, 39 | 10, 20 | 40 |
| 20 | 201M108A | 10, 12, 15, 18 | 10, 20 | 200 |
| 21 | 101M108A | 22, 27, 33, 39 | 10, 20 | 100 |
| 22 | 400M108A | 47, 56, 68 | 10, 20 | 40 |
| 23 | 400M110A | 82, 100 | 10, 20 | 40 |
| 24 | 401M111J | 0.125 (Note 1) | 10, 20 | 400 |
| 25 | 201M111J | 0.25 (Note 1) | 10, 20 | 200 |
| 26 | 101M111J | 0.5 (Note 1) | 10, 20 | 100 |
| 27 | 401M112J | 0.2 (Note 1) | 10, 20 | 400 |
| 28 | 201M112J | 0.4 (Note 1) | 10, 20 | 200 |
| 29 | 101M112J | 0.8 (Note 1) | 10, 20 | 100 |
| 30 | 400M113J | 10 (Note 1) | 10, 20 | 40 |
| 31 | 400M114J | 10 (Note 1) | 10, 20 | 40 |

Notes:

Capacitor arrays with several bond pads. The capacitance value refers to Cn, the smallest individual rated capacitance value available on the die. Multiples of Cn also available on the die shall be as specified in Para. 1.7 for the particular Variant.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Unit | Remarks |
| --- | --- | --- | --- | --- |
| Rated Voltage | UR | See Para. 1.4.2 | V |  |
| Breakdown Voltage | VBR | 1.5UR | V | Minimum |
| Operating Temperature Range | Top | -55 to +150 | °C | Tamb |
| Storage Temperature Range | Tstg | -55 to +175 | °C |  |
| Die Attach Temperature | Tdie | +320 | °C | Note 1 |

NOTES:

Duration 30 seconds maximum.

## handling precautions

These devices are susceptible to damage by electrostatic discharge. Therefore suitable precautions shall be employed for protection during all phases of manufacture, test, packaging, shipping and handling.

These components are categorised as Class 1 per ESCC Basic Specification No. 23800 with a minimum Critical Path Failure Voltage of 1000V.

## PHYSICAL DIMENSIONS

### Variants 01 to 10

|  | Symbols | Dimensions mm |  | Variant Number |
| --- | --- | --- | --- | --- |
|  |  | Min | Max |  |
|  | A | 0.34 | 0.4 | 01, 02, 03 |
|  |  | 0.54 | 0.6 | 04, 05, 06 |
|  |  | 0.74 | 0.8 | 07, 08, 09 |
|  |  | 0.94 | 1 | 10 |
|  | ØC | 0.145 | 0.31 | 01, 02, 03 |
|  |  | 0.31 | 0.49 | 04, 05, 06 |
|  |  | 0.54 | 0.66 | 07, 08, 09 |
|  |  | 0.72 | 0.78 | 10 |
|  | E | 0.16 | 0.22 | All |

### Variants 11 to 23

|  | Symbols | Dimensions mm |  | Variant Number |
| --- | --- | --- | --- | --- |
|  |  | Min | Max |  |
|  | A | 0.3 | 0.4 | 11, 12, 13 |
|  |  | 0.44 | 0.54 | 14, 15, 16 |
|  |  | 0.5 | 0.6 | 17, 18, 19 |
|  |  | 0.7 | 0.8 | 20, 21, 22 |
|  |  | 0.9 | 1 | 23 |
|  | D | 0.22 | 0.28 | 11, 12, 13 |
|  |  | 0.34 | 0.38 | 14, 15, 16 |
|  |  | 0.4 | 0.44 | 17, 18, 19 |
|  |  | 0.54 | 0.64 | 20, 21, 22 |
|  |  | 0.68 | 0.78 | 23 |
|  | E | 0.16 | 0.22 | All |

### Variants 24, 25, 26

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 0.4 | 0.5 |  |
| D | 0.06 | 0.08 | 1 |
| E | 0.16 | 0.22 |  |

notes:

Dimension of the smallest bond pad area, specified for bonding purposes.

### Variants 27, 28 and 29

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 0.4 | 0.5 |  |
| D | 0.08 | 0.1 | 1 |
| E | 0.16 | 0.22 |  |

notes:

Dimension of the smallest bond pad area, specified for bonding purposes.

### Variant 30

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 0.4 | 0.5 |  |
| D | 0.06 | 0.08 | 1 |
| E | 0.16 | 0.22 |  |
| F | 0.26 | 0.28 | 1 |

notes:

Dimension of the smallest bond pad area, specified for bonding purposes.

### Variant 31

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 0.4 | 0.5 |  |
| D | 0.06 | 0.08 | 1 |
| E | 0.16 | 0.22 |  |
| F | 0.26 | 0.28 | 1 |

notes:

Dimension of the smallest bond pad area, specified for bonding purposes.

## FUNCTIONAL DIAGRAM

## MATERIALS AND FINISHES

Materials and finishes shall be as follows:

Bond Pad

- The bond pad metallisation shall be TiAu with a layer of vacuum-deposited gold, thickness ≥ 0.25µm and a final layer of electrolytic gold, thickness ≥ 2.7µm.

Die Backface

- The die backface metallisation shall be TiAu with a layer of gold, thickness ≥ 0.5µm.

Glassivation

- The material of the capacitor dielectric shall be oxide. The thickness of the oxide varies as required for each component’s Cn and UR.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Production Control (Chart F2)

A Metallisation Adhesion test shall be performed on a randomly selected sample of 5 naked die from each wafer lot, after Die Visual Inspection during Wafer Lot Acceptance.

- Samples shall be subjected to a high temperature bake of +320 (+5 -0)°C for a period of 5 minutes minimum. The samples shall then be visually inspected.

- Any evidence of lifting or peeling metallisation shall be cause for wafer lot failure.

- This test is considered as destructive and therefore components so tested shall not form part of the delivery lot.

#### Deviations from Screening Tests for Die Components – Chart F3B

Burn-in 1: Not applicable.

Parameter Drift Values Δ1: Not applicable.

Check for Lot Failure for Burn-in 1: Not applicable.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700.

The information to be marked and the order of precedence shall be as follows:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## die shear

In those cases where package clearances are such that a die shear test is not practicable, the die shall be pushed away with a suitable tool. The force required to remove the die need not be recorded. The die attachment area shall be inspected and the component shall be considered acceptable if more than 50% of the semiconductor material remains.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions | Tolerance (± %) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Min | Max |  |
| Capacitance | C | 4001 | VT = 0V, f = 1MHz | 10 20 | 0.9Cn 0.8Cn | 1.1Cn 1.2Cn | pF |
| Leakage Current | IL1 | 4016 | VT = UR | All | - | 50 | nA |
| Voltage Proof Leakage Current | IL2 | 4016 | VT = 1.5UR | All | - | 100 | nA |

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions Note 1 | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Leakage Current | IL1 | 4016 | Tamb = +150 (+0 -3)°C VT = UR | - | 100 | nA |

NOTES:

Measurements shall be performed on a sample basis as specified in the Generic Specification.

## PARAMETER DRIFT VALUES

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.4.1.

The drift values (Δ) shall not be exceeded for each characteristic specified. The corresponding absolute limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  | Drift Value Δ | Absolute |  |  |
|  |  |  | Min | Max |  |
| Capacitance | C | ±0.2 or (1) ±2% | Note 2 |  | pF |
| Leakage Current | IL1 | ±5 or (1) ±100% | - | 50 | nA |

NOTES:

Whichever is the greater referred to the initial value.

As specified in Para. 2.4.1.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.4.1.

The limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- |
|  |  | Min | Max |  |
| Capacitance | C | Note 1 |  | pF |
| Leakage Current | IL1 | - | 50 | nA |
| Voltage Proof Leakage Current | IL2 | - | 100 | nA |

NOTES:

As specified in Para. 2.4.1.

## BURN-IN 2 CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +150 (+0 -3) | °C |
| Test Voltage | VT | UR | V |

## OPERATING LIFE CONDITIONS

The conditions shall be as specified in Para. 2.7.

## APPENDIX A

AGREED DEVIATIONS FOR Cobham Microwave (F)

| Items Affected | Description of Deviations |
| --- | --- |
| Para. 2.1.1.1, Deviations from Production Control – Chart F2 | - Assembly (Assembly of the Packaged Test Sublot for Naked Die Components): - A minimum of 5 dice per wafer and 20 dice per wafer lot shall be assembled to make up the Packaged Test Sublot. |
|  | Encapsulation: Encapsulation of the Packaged Test Sublot samples is optional at the Manufacturer’s discretion. |
| Deviations from Generic Specification: Screening Tests (Chart F3) | Particle Impact Noise Detection (PIND): Not applicable. |
|  | Radiographic Inspection: Not applicable. |
|  | Seal (Fine and Gross Leak): Not applicable. |
|  | External Visual Inspection: Not applicable. |