Page 1 of 16

TRANSISTORS, MICROWAVE, SILICON, BIPOLAR, SMALL SIGNAL

BASED ON TYPE BFY740B

ESCC Detail Specification No. 5611/011

| Issue 4 Draft B | April 2018 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2018. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| TBA | Specification upissued to incorporate changes per DCR. |

TABLE OF CONTENTS

1	General	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants	5

1.5	MAXIMUM RATINGS	6

1.6	handling precautions	6

1.7	PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION	7

1.8	FUNCTIONAL DIAGRAM	8

1.9	MATERIALS AND FINISHES	8

2	REQUIREMENTS	8

2.1	GENERAL	8

2.1.1	Deviations from the Generic Specification	8

2.1.1.1	Deviations from Screening Tests for Packaged Components – Chart F3A	8

2.1.1.2	Deviations from Qualification and Periodic Tests for Packaged Components - Chart F4A	8

2.2	MARKING	9

2.3	Die Shear	9

2.4	TERMINAL STRENGTH	9

2.5	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	10

2.5.1	Room Temperature Electrical Measurements	10

2.5.2	High and Low Temperatures Electrical Measurements	11

2.6	PARAMETER DRIFT VALUES	12

2.7	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	13

2.8	BURN-IN 1 CONDITIONS	14

2.9	BURN-IN 2 CONDITIONS	14

2.10	OPERATING LIFE CONDITIONS	14

APPENDIX A	15

# General

## SCOPE

This specification details the ratings, physical and electrical characteristics and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 5010

MIL-STD-750, Test Methods and Procedures for Semiconductor Devices

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 561101101

Detail Specification Reference: 5611011

Component Type Variant Number: 01

### Component Type Variants

The component type variants applicable to this specification are as follows:

| Variant Number | Based on Type | Die Metallisation | Case | Lead Material and Finish | Weight max g |
| --- | --- | --- | --- | --- | --- |
| 01 | BFY740B | NiPPdAu | Micro-X | G2 | 0.03 |
| 02 | BFY740B | TiPtAu | Micro-X | G2 | 0.03 |

The lead material and finish shall be in accordance with the requirements of ESCC Basic Specification No. 23500.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Collector-Emitter Voltage | VCEO | 4 3.5 | V | Tamb > 0°C Tamb ≤ 0°C |
| Collector-Emitter Voltage | VCES | 13 | V |  |
| Collector-Base Voltage | VCBO | 13 | V |  |
| Emitter-Base Voltage | VEBO | 1.2 | V |  |
| Collector Current | IC | 30 | mA |  |
| Base Current | IB | 3 | mA | Note 1 |
| Power Dissipation | Ptot | 120 | mW | TS ≤ +125°C Note 2 |
| Operating Temperature Range | Top | -65 to +175 | °C | TS |
| Storage Temperature Range | Tstg | -65 to +175 | °C |  |
| Junction Temperature | Tj | +175 | °C |  |
| Thermal Resistance, Junction-to-Soldering Point | Rth(j-s) | 417 | °C/W |  |
| Soldering Temperature | Tsol | +250 | °C | Note 3 |

NOTES:

Maximum ratings must not be exceeded under any combination of DC ratings and RF voltage/current swings except as specified in Para. 2.5.1 herein.

TS is measured on the collector lead at the soldering point to the PCB. For TS greater than specified, Ptot derates linearly to 0W at TS = +175°C.

Duration 5 seconds maximum at a distance of not less than 0.5mm from the device body and the same lead shall not be resoldered until 3 minutes have elapsed.

## handling precautions

These devices are susceptible to damage by electrostatic discharge. Therefore suitable precautions shall be employed for protection during all phases of manufacture test, packaging, shipping and handling.

These components are categorised as Class 1 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 100V.

## PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION

Micro-x Package

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| B | 1.68 | 1.88 | 2 |
| d | 0.07 | 0.15 | 3 |
| d1 | 0.4 | 0.6 | 2 |
| d2 | 0.92 | 1.12 | 2 |
| ØD | 1.55 | 1.85 |  |
| E | 0.85 | 1.25 | 3 |
| E1 | 0.66 | 0.86 | 3 |
| H | 4 | 4.4 | 2 |
| S | 0.08 | 0.3 | 4 |

NOTES:

The Collector terminal is identified by means of a black dot marked on the lid, with the three other terminals identifiable by the component’s geometry.

Applies in two places.

Applies to all leads.

Applies in four places.

## FUNCTIONAL DIAGRAM

NOTES:

The lid is connected to the Emitter terminal.

## MATERIALS AND FINISHES

Materials and finishes shall be as follows:

Case

- The case shall be hermetically sealed and have a ceramic body with a metal lid.

Leads

- As specified in Para. 1.4.2 Component Type Variants.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Screening Tests for Packaged Components – Chart F3A

Radiographic Inspection: shall be performed in the X and Z axes only.

#### Deviations from Qualification and Periodic Tests for Packaged Components - Chart F4A

Mechanical Shock: Not applicable.

Vibration: Not applicable.

Constant Acceleration: Not applicable.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700. The information to be marked and the order of precedence shall be as follows:

Terminal identification.

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number.

Traceability information.

## Die Shear

In those cases where package clearances are such that a die shear test is not practicable, the die shall be pushed away with a suitable tool. The force required to remove the die need not be recorded. The die attachment area shall be inspected and the component shall be considered acceptable if more than 50% of the semiconductor material remains.

## TERMINAL STRENGTH

The test conditions for terminal strength, tested as specified in the ESCC Generic Specification, shall be as follows:

Test Condition A, tension, with a force of 2.23N and a duration of 5s.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +25 ±3°C.

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Collector-Emitter Cut-off Current 1 | ICES1 | 3041 | Bias Condition C VCE = 13V | - | 1000 | nA |
| Collector-Emitter Cut-off Current 2 | ICES2 | 3041 | Bias Condition C VCE = 10.5V | - | 100 | nA |
| Collector-Emitter Cut-off Current 3 | ICES3 | 3041 | Bias Condition C VCE = 5V | - | 20 | nA |
| Collector-Emitter Cut-off Current 4 | ICEX | 3041 | VCE = 4V, IB = 100nA Variant 01: Variant 02: | 20 20 | 100 150 | µA |
| Emitter-Base Cut-off Current 1 | IEBO1 | 3061 | Bias Condition D VEB = 1.2V | - | 5 | µA |
| Emitter-Base Cut-off Current 2 | IEBO2 | 3061 | Bias Condition D VEB = 500mV | - | 100 | nA |
| Forward-Current Transfer Ratio 1 | hFE1 | 3076 | VCE = 3V, IC = 20mA | 185 | 380 | - |
| Forward-Current Transfer Ratio 2 | hFE2 | 3076 | VCE = 3V, IC = 20µA | 240 | 690 | - |
| Base-Emitter Forward Voltage | VFBE | 4011 | IB = 12mA, IC = 0A Note 1 | - | 960 | mV |
| Collector-Emitter Capacitance | CCE | 3236 | VCE = 2V, IB = 0A, f = 1MHz Common Base Configuration | - | 0.5 | pF |
| Collector-Base Capacitance | CCB | 3236 | VCB = 2V, IE = 0A, f = 1MHz Common Emitter Configuration | - | 0.12 | pF |
| Emitter-Base Capacitance | CEB | 3236 | VEB = 500mV, IC = 0A, f = 1MHz Common Collector Configuration | - | 0.8 | pF |
| Insertion Power Gain at 1.8GHz | ¦S21¦21.8 | - | f = 1.8GHz, VCE = 3V, IC = 20mA Notes 2, 3 | 22 | - | dB |
| Insertion Power Gain at 6GHz | ¦S21¦26 | - | f = 6GHz, VCE = 3V, IC = 20mA Notes 2, 3 | 12 | - | dB |
| Maximum Available / Stable Gain at 1.8GHz | MAG / MSG1.8 | - | f = 1.8GHz, VCE = 3V, IC = 20mA Notes 2, 3, 4 | 24 | - | dB |
| Maximum Available / Stable Gain at 6GHz | MAG / MSG6 | - | f = 6GHz, VCE = 3V, IC = 20mA Notes 2, 3, 4 | 17 | - | dB |
| Noise Figure at 1.8GHz | NF1.8 | - | f = 1.8GHz, VCE = 3V, IC = 8mA Notes 3, 5, 6 | - | 0.75 | dB |
| Noise Figure at 6GHz | NF6 | - | f = 6GHz, VCE = 3V, IC = 8mA Notes 3, 5, 6 | - | 1.15 | dB |

NOTES:

Pulsed measurement, pulse duration < 1s, single pulse. IB may exceed that specified in Para. 1.5 Maximum Ratings.

Measured in a 50Ω system using a suitable network analyser.

Small signal measurement.

MAG if K ≥ 1; MSG if K < 1.

Input tuned for NFmin.

Measurements shall be performed on a sample of 15 components with the maximum allowed limit reduced by 0.07dB. In the event of any failure a 100% inspection shall be performed and the specified limit shall apply.

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Collector-Emitter Cut-off Current 2 | ICES2 | 3041 | Tamb = +150 (+0 -5)°C Bias Condition C VCE = 10.5V, Note 1 | - | 5 | µA |
| Collector-Emitter Cut-off Current 3 | ICES3 | 3041 | Tamb = +150 (+0 -5)°C Bias Condition C VCE = 5V, Note 1 | - | 1 | µA |
| Emitter-Base Cut-off Current 1 | IEBO1 | 3061 | Tamb = +150 (+0 -5)°C Bias Condition D VEB = 1.2V, Note 1 | - | 50 | µA |
|  |  |  | Tamb = -55 (+5 -0)°C Bias Condition D VEB = 1.2V, Note 2 | - | 5 | µA |
| Emitter-Base Cut-off Current 2 | IEBO2 | 3061 | Tamb = +150 (+0 -5)°C Bias Condition D VEB = 500mV, Note 1 | - | 1 | µA |
| Forward-Current Transfer Ratio 1 | hFE1 | 3076 | Tamb = +150 (+0 -5)°C VCE = 3V, IC = 20mA, Note 1 | 85 | 250 | - |
|  |  |  | Tamb = -55 (+5 -0)°C VCE = 3V, IC = 20mA, Note 2 | 150 | 400 | - |

NOTES:

Measurements shall be performed on a sample of 5 components. In the event of any failure, a 100% inspection shall be performed.

Measurements shall be performed on a sample of 5 assembled components per wafer. In the event of any failure, a 100% inspection shall be performed.

## PARAMETER DRIFT VALUES

Unless otherwise specified, the measurements shall be performed at Tamb = +25 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.5.1 Room Temperature Electrical Measurements.

The drift values (Δ) shall not be exceeded for each characteristic specified. The corresponding absolute limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  | Drift Value (1) Δ | Absolute |  |  |
|  |  |  | Min | Max |  |
| Collector-Emitter Cut-off Current 2 | ICES2 | ±20 or (2) +100/-50% | - | 100 | nA |
| Collector-Emitter Cut-off Current 3 | ICES3 | ±5 or (2) +100/-50% | - | 20 | nA |
| Emitter-Base Cut-off Current 1 | IEBO1 | ±0.5 or (2) +100/-50% | - | 5 | µA |
| Emitter-Base Cut-off Current 2 | IEBO2 | ±20 or (2) +100/-50% | - | 100 | nA |
| Forward-Current Transfer Ratio 1 | hFE1 | ±10% | 185 | 380 | - |
| Base-Emitter Forward Voltage | VFBE | ±20 (3) | - | 960 | mV |

NOTES:

Δ1 = Δ2.

Whichever is greater.

The total change over both Burn-in 1 and Burn-in 2 referred to the initial value made prior to Burn-in 1.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +25 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.5.1 Room Temperature Electrical Measurements.

The limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  | Drift Value Δ | Absolute |  |  |
|  |  |  | Min | Max |  |
| Collector-Emitter Cut-off Current 2 | ICES2 | ±20 or (1) +100/-50% | - | 100 | nA |
| Collector-Emitter Cut-off Current 3 | ICES3 | ±5 or (1) +100/-50% | - | 20 | nA |
| Emitter-Base Cut-off Current 1 | IEBO1 | ±0.5 or (1) +100/-50% | - | 5 | µA |
| Emitter-Base Cut-off Current 2 | IEBO2 | ±20 or (1) +100/-50% | - | 100 | nA |
| Forward-Current Transfer Ratio 1 | hFE1 | ±10% | 185 | 380 | - |
| Base-Emitter Forward Voltage | VFBE | ±20 | - | 960 | mV |

notes:

Whichever is greater.

## BURN-IN 1 CONDITIONS

| Characteristics | Symbols | Test Conditions (Note 1) | Units |
| --- | --- | --- | --- |
| Soldering Point Temperature | TS | +150 (+0 -5) | °C |
| Collector-Emitter Voltage | VCES | 10.5 | V |
| Base-Emitter Voltage | VBE | 0 | V |

notes:

Maximum ratings shall not be exceeded during power up and power down sequences.

## BURN-IN 2 CONDITIONS

| Characteristics | Symbols | Test Conditions (Notes 1, 2) | Units |
| --- | --- | --- | --- |
| Soldering Point Temperature | TS | ≥ +125 | °C |
| Junction Temperature | Tj | +175 (+0 -5) | °C |
| Power Dissipation | Ptot | ≤ Ptot (see Para. 1.5) | mW |
| Collector-Emitter Voltage | VCE | 3.5 | V |

notes:

Maximum ratings shall not be exceeded during power up and power down sequences.

TS and/or Ptot shall be adjusted to attain the specified Tj.

## OPERATING LIFE CONDITIONS

The conditions shall be as specified in Para. 2.9 Burn-in 2 Conditions.

## APPENDIX A

AGREED DEVIATIONS FOR INFINEON Technologies AG (D)

| Items Affected | Description of Deviations |
| --- | --- |
| Para. 2.1.1 Deviations from Generic Specification: Special In-Process Controls - Chart F2 | Internal Visual Inspection: shall include verification of the length, height and shape of the wire bonding. |
|  | Bond Strength: the following pre-seal bond strength shall apply: - 0.015N minimum |
|  | Die Shear: if Para. 2.3 does not apply, the following shear strength may be applied: - 0.4N minimum |
|  | Dimension Check: may be performed during Chart F3A testing. |
| Para. 2.1.1 Deviations from Generic Specification: Screening Tests for Packaged Components - Chart F3A | Temperature Cycling: shall be replaced by a Thermal Shock test in accordance with MIL-STD-202, Test Method 107, Test Condition B, 20 cycles. |
|  | Radiographic Inspection: shall not be performed. |
| Para. 2.1.1 Deviations from Generic Specification: Qualification and Periodic Tests for Packaged Components - Chart F4A | Temperature Cycling: shall be replaced by a Thermal Shock test in accordance with MIL-STD-202, Test Method 107, Test Condition B, 100 cycles. |
|  | - Assembly Capability Subgroup tests: in addition to the permitted use of empty packages or electrical rejects as test samples, components rejected during the following Screening Tests: Radiographic Inspection Seal External Visual Inspection may be used on the condition that the cause for rejection has no possible impact on the tests, and they have been subjected to the same screening as the packages of the assembly lot with which they are associated. |
|  | Bond Strength: the following post–seal bond strength shall apply: - 0.012N minimum |
|  | Die Shear: if Para. 2.3 does not apply, the following shear strength may be applied: - 0.4N minimum |
| Para. 2.1.1 Deviations from Generic Specification: Final Customer Source Inspection | Final Customer Source Inspection shall be limited to witnessing of the DC and 1MHz parameters specified in Para. 2.5.1 Room Temperature Electrical Measurements. |
| Para. 2.1.1 Deviations from Generic Specification: Data Documentation | Additional Documentation and Wafer Lot Acceptance Data: if Wafer Lot Acceptance Data is stipulated in the Purchase Order, such data will not be delivered but will be available for review at lnfineon Technologies AG. |