Page 1 of 13

DIODES, MICROWAVE, SILICON, SCHOTTKY, GENERAL PURPOSE

BASED ON TYPEs bas40 and baS70

ESCC Detail Specification No. 5512/020

| Issue 5 Draft B | October 2019 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2019. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| tba | Specification upissued to incorporate changes per DCR. |

TABLE OF CONTENTS

1	General	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants	5

1.5	MAXIMUM RATINGS	6

1.6	handling precautions	6

1.7	PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION	7

1.8	FUNCTIONAL DIAGRAM	7

1.9	MATERIALS AND FINISHES	8

2	REQUIREMENTS	8

2.1	GENERAL	8

2.1.1	Deviations from the Generic Specification	8

2.1.1.1	Deviations from Screening Tests - Chart F3	8

2.1.1.2	Deviations from Qualification and Periodic Tests - Chart F4	8

2.2	MARKING	8

2.3	Die Shear	8

2.4	TERMINAL STRENGTH	8

2.5	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	9

2.5.1	Room Temperature Electrical Measurements	9

2.5.2	High and Low Temperatures Electrical Measurements	9

2.6	PARAMETER DRIFT VALUES	10

2.7	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	11

2.8	BURN-IN 1 CONDITIONS	11

2.9	BURN-IN 2 CONDITIONS	12

2.10	OPERATING LIFE CONDITIONS	12

APPENDIX A	13

# General

## SCOPE

This specification details the ratings, physical and electrical characteristics and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 5010

MIL-STD-750, Test Methods and Procedures for Semiconductor Devices

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 551202001

Detail Specification Reference: 5512020

Component Type Variant Number: 01 (as required)

### Component Type Variants

The component type variants applicable to this specification are as follows:

| Variant Number | Based on Type | Case | Terminal Material and Finish | Weight max g |
| --- | --- | --- | --- | --- |
| 01 | BAS70 | T1 | E2 | 0.02 |
| 03 | BAS40 | T1 | E2 | 0.02 |

The terminal material and finish shall be in accordance with the requirements of ESCC Basic Specification No. 23500.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| DC Reverse Voltage Variant 01 Variant 03 | VR | 70 40 | V |  |
| DC Forward Current Variant 01 Variant 03 | IF | 70 120 | mA |  |
| Surge Forward Current Variant 01 Variant 03 | IFSM | 85 170 | mAp-p | Note 1 |
| Power Dissipation | PD | 250 | mW | Tcase ≤ +125°C Note 2 |
| Operating Temperature Range | Top | -55 to +150 | °C | Tcase |
| Storage Temperature Range | Tstg | -55 to +150 | °C |  |
| Soldering Temperature | Tsol | +250 | °C | Note 3 |
| Junction Temperature | Tj | +150 | °C |  |
| Thermal Resistance, Junction-to-Case | Rth(j-c) | 100 | °C/W |  |

NOTES:

Duration ≤ 10ms, duty cycle = 10%.

For Tcase > +125°C, derate linearly to 0W at Tcase = +150°C.

Duration 5 seconds maximum at a distance of not less than 0.5mm from the device body and the same termination shall not be resoldered until 3 minutes have elapsed.

## handling precautions

These devices are susceptible to damage by electrostatic discharge. Therefore suitable precautions shall be employed for protection during all phases of manufacture test, packaging, shipping and handling.

These components are categorised as Class 1 per ESCC Basic Specification No. 23800 with a Minimum Critical Path Failure Voltage of 1000V.

## PHYSICAL DIMENSIONS AND TERMINAL IDENTIFICATION

Case Type T1

| Symbols | Dimensions mm |  | Notes |
| --- | --- | --- | --- |
|  | Min | Max |  |
| A | 1.4 | 1.95 |  |
| A1 | 1.05 | 1.25 |  |
| B | 1.15 | 1.35 |  |
| B1 | - | 0.4 | 1 |
| d | 0.06 | 0.1 |  |
| d1 | 0.4 | 0.6 |  |
| ØD | 1.3 | 1.45 |  |
| G | 0.1 | 0.5 |  |
| ØH | - | 0.3 |  |
| L | 5.5 | - |  |

NOTES:

The anode terminal is identified by the sealing ring and lid (dimension B1).

## FUNCTIONAL DIAGRAM

## MATERIALS AND FINISHES

Materials and finishes shall be as follows:

Case

- The case shall be hermetically sealed, have a ceramic body and a metal sealing ring and lid.

Terminals

- As specified in Para. 1.4.2 Component Type Variants.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Screening Tests - Chart F3

Radiographic Inspection: shall be performed in the X and Z axes only.

#### Deviations from Qualification and Periodic Tests - Chart F4

Mechanical Shock: Not applicable.

Vibration: Not applicable.

Constant Acceleration: Not applicable.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700. The information to be marked and the order of precedence shall be as follows:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number (see Para. 1.4.1).

Traceability information.

## Die Shear

In those cases where package clearances are such that a die shear test is not practicable, the die shall be pushed away with a suitable tool. The force required to remove the die need not be recorded. The die attachment area shall be inspected and the component shall be considered acceptable if more than 50% of the semiconductor material remains.

## TERMINAL STRENGTH

The test conditions for Terminal Strength, tested as specified in the ESCC Generic Specification, shall be as follows:

Test Condition A, tension, with a force of 1.5N and a duration of 5s.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +25 ±3°C.

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Reverse Current 1 | IR1 | 4016 | Variant 01, VR = 70V Variant 03, VR = 40V | - - | 2 2 | µA |
| Reverse Current 2 | IR2 | 4016 | Variant 01, VR = 56V Variant 03, VR = 32V | - - | 100 100 | nA |
| Forward Voltage 1 | VF1 | 4011 | IF = 1mA Variant 01 Variant 03 | 300 290 | 440 390 | mV |
| Forward Voltage 2 | VF2 | 4011 | IF = 10mA Variant 01 Variant 03 | 600 410 | 780 540 | mV |
| Forward Voltage 3 | VF3 | 4011 | Variant 01, IF = 15mA Variant 03, IF = 40mA | 0.8 0.65 | 1 0.85 | V |
| Differential Forward Resistance (Note 1) | RFD | - | IF1 = 10mA, IF2 = 15mA Variant 01 Variant 03 | 26 8 | 34 12 | Ω |
| Total Capacitance | CT | 4001 | VR = 0V, f = 1MHz Vin = 15mV Variant 01 Variant 03 | 1.2 2.4 | 2 4 | pF |

NOTES:

RFD = ΔVF/ΔIF.

### High and Low Temperatures Electrical Measurements

The measurements shall be performed only at Tamb = +145 (+0 -5)°C.

| Characteristics | Symbols | MIL-STD-750 Test Method | Test Conditions (Note 1) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Reverse Current 2 | IR2 | 4016 | Variant 01, VR = 56V Variant 03, VR = 32V | - - | 100 200 | µA |
| Forward Voltage 3 | VF3 | 4011 | Variant 01, IF = 15mA Variant 03, IF = 40mA | - - | 950 800 | mV |

NOTES:

Measurements shall be performed on a sample of 5 components. In the event of any failure, a 100% inspection shall be performed.

## PARAMETER DRIFT VALUES

Unless otherwise specified, the measurements shall be performed at Tamb = +25 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.5.1 Room Temperature Electrical Measurements.

The drift values (Δ) shall not be exceeded for each characteristic specified. The corresponding absolute limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  | Drift Value (1) Δ | Absolute |  |  |
|  |  |  | Min | Max |  |
| Reverse Current 2 | IR2 | ±10 or (2) +50%, -33% | - | 100 | nA |
| Forward Voltage 3 Variant 01 Variant 03 | VF3 | ±5% | 0.8 0.65 | 1 0.85 | V |

NOTES:

Δ1 = Δ2.

Whichever is greater.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +25 ±3°C.

The test methods and test conditions shall be as per the corresponding test defined in Para. 2.5.1 Room Temperature Electrical Measurements.

The limit values for each characteristic shall not be exceeded.

| Characteristics | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- |
|  |  | Min | Max |  |
| Reverse Current 1 | IR1 | - | 2.2 | µA |
| Reverse Current 2 | IR2 | - | 110 | nA |
| Forward Voltage 1 Variant 01 Variant 03 | VF1 | 290 280 | 450 400 | mV |
| Forward Voltage 2 Variant 01 Variant 03 | VF2 | 580 390 | 800 560 | mV |
| Forward Voltage 3 Variant 01 Variant 03 | VF3 | 0.78 0.63 | 1.02 0.87 | V |
| Differential Forward Resistance Variant 01 Variant 03 | RFD | 25 7.5 | 35 12.5 | Ω |
| Total Capacitance Variant 01 Variant 03 | CT | 1.1 2.3 | 2.1 4.1 | pF |

## BURN-IN 1 CONDITIONS

| Characteristics | Symbols | Test Conditions | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +145 (+0 -5) | °C |
| Reverse Voltage Variant 01 Variant 03 | VR | 56 (+0 -3) 32 (+0 -2) Note 1 | V |

NOTES:

After the burn-in period, the components shall be allowed to cool until Tamb = +25 ±3°C; the VR bias shall be maintained until Tamb < +35°C.

## BURN-IN 2 CONDITIONS

| Characteristics | Symbols | Test Conditions (Note 1) | Units |
| --- | --- | --- | --- |
| Junction Temperature | Tj | +150 (+0 -5) | °C |
| Power Dissipation | PD | ≤ PD given in Para. 1.5 Maximum Ratings | mW |

notes:

Tcase shall be adjusted to attain the specified Tj.

## OPERATING LIFE CONDITIONS

The conditions shall be as specified in Para. 2.9 for Burn-in 2.

## APPENDIX A

AGREED DEVIATIONS FOR INFINEON Technologies AG (D)

| Items Affected | Description of Deviations |
| --- | --- |
| Para. 2.1.1 Deviations from Generic Specification: Special In-Process Controls - Chart F2 | Bond Strength: The following pre-seal bond strength shall apply: - 0.05N minimum |
|  | Die Shear: The following shear strength shall apply: - 0.5N minimum |
|  | Dimension Check: May be performed during Chart F3 testing. |
| Para. 2.1.1 Deviations from Generic Specification: Final Customer Source Inspection | Final Customer Source Inspection shall be limited to witnessing of the DC parameters specified in Para. 2.5.1 Room Temperature Electrical Measurements. |
| Para. 2.1.1 Deviations from Generic Specification: Data Documentation | Additional Documentation and Wafer Lot Acceptance Data: If Wafer Lot Acceptance Data is stipulated in the Purchase Order, such data will not be delivered but will be available for review at lnfineon Technologies AG. |
| Para. 2.1.1.1 Deviations from Screening Tests - Chart F3 | Temperature Cycling: Shall be replaced by a Thermal Shock test in accordance with MIL-STD-202, Test Method 107, Test Condition B, 20 cycles. |
| Para. 2.1.1.2 Deviations from Qualification and Periodic Tests - Chart F4 | Temperature Cycling: Shall be replaced by a Thermal Shock test in accordance with MIL-STD-202, Test Method 107, Test Condition B, 100 cycles. |
|  | - Assembly Capability Subgroup tests: - In addition to the permitted use of empty packages or electrical rejects as test samples, components rejected during the following Screening Tests: Radiographic Inspection Seal External Visual Inspection may be used on the condition that the cause for rejection has no possible impact on the tests, and they have been subjected to the same screening as the packages of the assembly lot with which they are associated. |
|  | Bond Strength: The following post–seal bond strength shall apply: - 0.04N minimum |
|  | Die Shear: The following shear strength shall apply: - 0.5N minimum |