Page 1 of 18

CAPACITORS, FIXED, RECONSTITUTED MICA, HIGH VOLTAGE

BASED ON TYPE HT86PS

ESCC Detail Specification No. 3006/022

| Issue 4 Draft B | January 2020 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# LEGAL DISCLAIMER AND COPYRIGHT

European Space Agency, Copyright © 2020. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| TBD | Specification updated to incorporate changes per DCR. |

TABLE OF CONTENTS

1	GENERAL	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND range of COMPONENTs	5

1.4.1	The ESCC Component Number	5

1.4.1.1	Characteristics and Ratings Codes	5

1.4.2	Range of Components	6

1.5	MAXIMUM RATINGS	12

1.6	PHYSICAL DIMENSIONS and terminal identification	13

1.7	FUNCTIONAL DIAGRAM	13

2	REQUIREMENTS	13

2.1	GENERAL	13

2.1.1	Deviations from the Generic Specification	13

2.1.1.1	Deviations from Screening Tests (Chart F3)	13

2.1.1.2	Deviations from Qualification and Periodic Tests – Chart F4	14

2.2	MARKING	14

2.3	Robustness of terminations	14

2.4	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	15

2.4.1	Room Temperature Electrical Measurements	15

2.4.2	High and Low Temperatures Electrical Measurements	16

2.5	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	16

2.6	BURN-IN conditions	18

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3006.

IEC Publication No. 60270, High-voltage test techniques – Partial discharge measurements

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND range of COMPONENTs

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 300602201222MH

Detail Specification Reference: 3006022

Component Type Variant Number (mandatory): 01

Characteristic code: Capacitance Value (2200pF): 222 (as required)

Characteristic code: Capacitance Tolerance (±20%): M (as required)

Rating code: Rated Voltage (10000V): H (as required)

#### Characteristics and Ratings Codes

Characteristics and ratings to be codified as part of the ESCC Component Number shall be as follows:

Capacitance Value, C, expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be picofarads (pF).

| Capacitance Value C (pF) | Code |
| --- | --- |
| XX101 | XX1 |
| XX102 | XX2 |
| XX103 | XX3 |
| XX104 | XX4 |
| XX105 | XX5 |

Capacitance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (± %) | Code Letter |
| --- | --- |
| 10 | K |
| 20 | M |

Rated Voltage, UR, expressed by the following codes:

| Rated Voltage UR (V) | Code Letter |
| --- | --- |
| 1500 | C |
| 2500 | D |
| 3500 | E |
| 5000 | F |
| 7500 | G |
| 10000 | H |
| 12500 | J |
| 15000 | K |
| 20000 | L |

### Range of Components

The range of components applicable to this specification are as follows:

| Capacitance Value (C) (pF) | Capacitance Tolerance (± %) | Rated Voltage (UR) (V) | Dimensions (mm) (Note 1) |  |  |  | Lead Material & Finish (Note 2) | Weight Max (g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | L (±1) | h (±1) | e (±1) | ØW (+10%, -0.05) |  |  |
| 33000 | 10, 20 | 1500 | 35 | 10 | 4 | 1 | A3 or A4 | 4 |
| 39000 | 10 | 1500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 47000 | 10, 20 | 1500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 56000 | 10 | 1500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 68000 | 10, 20 | 1500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 82000 | 10 | 1500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 100000 | 10, 20 | 1500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 120000 | 10 | 1500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 150000 | 10, 20 | 1500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 180000 | 10 | 1500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 220000 | 10, 20 | 1500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 270000 | 10 | 1500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 330000 | 10, 20 | 1500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 390000 | 10 | 1500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 470000 | 10, 20 | 1500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 560000 | 10 | 1500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 820000 | 10, 20 | 1500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 1000000 | 10 | 1500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 1200000 | 10, 20 | 1500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 1500000 | 10 | 1500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 1800000 | 10, 20 | 1500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 2200000 | 10 | 1500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 15000 | 10, 20 | 2500 | 25 | 12 | 4 | 1 | A3 or A4 | 4 |
| 22000 | 10, 20 | 2500 | 35 | 10 | 4 | 1 | A3 or A4 | 4 |
| 27000 | 10 | 2500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 33000 | 10, 20 | 2500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 39000 | 10 | 2500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 47000 | 10, 20 | 2500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 56000 | 10 | 2500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 68000 | 10, 20 | 2500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 82000 | 10 | 2500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 100000 | 10, 20 | 2500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 120000 | 10 | 2500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 150000 | 10, 20 | 2500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 180000 | 10 | 2500 | 61 | 38 | 8 | 1 | A3 or A4 | 28 |
| 220000 | 10, 20 | 2500 | 61 | 38 | 8 | 1 | A3 or A4 | 28 |
| 270000 | 10 | 2500 | 61 | 45 | 8 | 1 | A3 or A4 | 44 |
| 330000 | 10, 20 | 2500 | 61 | 45 | 8 | 1 | A3 or A4 | 44 |
| 390000 | 10 | 2500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 470000 | 10, 20 | 2500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 560000 | 10 | 2500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 680000 | 10, 20 | 2500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 820000 | 10 | 2500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 1000000 | 10, 20 | 2500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 1200000 | 10 | 2500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 1500000 | 10, 20 | 2500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 15000 | 10, 20 | 3500 | 35 | 10 | 4 | 1 | A3 or A4 | 4 |
| 18000 | 10 | 3500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 22000 | 10, 20 | 3500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 27000 | 10 | 3500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 33000 | 10, 20 | 3500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 39000 | 10 | 3500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 47000 | 10, 20 | 3500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 56000 | 10 | 3500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 68000 | 10, 20 | 3500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 82000 | 10 | 3500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 100000 | 10, 20 | 3500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 120000 | 10 | 3500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 150000 | 10, 20 | 3500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 180000 | 10 | 3500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 220000 | 10, 20 | 3500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 270000 | 10 | 3500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 330000 | 10, 20 | 3500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 390000 | 10 | 3500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 470000 | 10, 20 | 3500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 560000 | 10 | 3500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 680000 | 10, 20 | 3500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 820000 | 10 | 3500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 1000000 | 10, 20 | 3500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 6800 | 10, 20 | 5000 | 35 | 10 | 4 | 1 | A3 or A4 | 4 |
| 8200 | 10 | 5000 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 10000 | 10, 20 | 5000 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 12000 | 10 | 5000 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 15000 | 10, 20 | 5000 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 18000 | 10 | 5000 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 22000 | 10, 20 | 5000 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 27000 | 10 | 5000 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 33000 | 10, 20 | 5000 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 39000 | 10 | 5000 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 47000 | 10, 20 | 5000 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 56000 | 10 | 5000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 68000 | 10, 20 | 5000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 82000 | 10 | 5000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 100000 | 10, 20 | 5000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 120000 | 10 | 5000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 150000 | 10, 20 | 5000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 180000 | 10 | 5000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 220000 | 10, 20 | 5000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 270000 | 10 | 5000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 330000 | 10, 20 | 5000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 390000 | 10 | 5000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 470000 | 10, 20 | 5000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 2200 | 10, 20 | 7500 | 35 | 10 | 4 | 1 | A3 or A4 | 4 |
| 2700 | 10 | 7500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 3300 | 10, 20 | 7500 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 3900 | 10 | 7500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 4700 | 10, 20 | 7500 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 5600 | 10 | 7500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 6800 | 10, 20 | 7500 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 8200 | 10 | 7500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 10000 | 10, 20 | 7500 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 12000 | 10 | 7500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 15000 | 10, 20 | 7500 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 18000 | 10 | 7500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 22000 | 10, 20 | 7500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 27000 | 10 | 7500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 33000 | 10, 20 | 7500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 39000 | 10 | 7500 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 47000 | 10, 20 | 7500 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 56000 | 10 | 7500 | 79 | 47 | 8 | 1.2 | A3 or A4 | 67 |
| 68000 | 10, 20 | 7500 | 79 | 47 | 8 | 1.2 | A3 or A4 | 67 |
| 82000 | 10 | 7500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 100000 | 10, 20 | 7500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 120000 | 10 | 7500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 150000 | 10, 20 | 7500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 180000 | 10 | 7500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 220000 | 10, 20 | 7500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 1000 | 10, 20 | 10000 | 35 | 10 | 4 | 1 | A3 or A4 | 4 |
| 1200 | 10 | 10000 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 1500 | 10, 20 | 10000 | 35 | 12 | 6 | 1 | A3 or A4 | 6.5 |
| 1800 | 10 | 10000 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 2200 | 10, 20 | 10000 | 35 | 16 | 6 | 1 | A3 or A4 | 8.5 |
| 2700 | 10 | 10000 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 3300 | 10, 20 | 10000 | 35 | 24 | 6 | 1 | A3 or A4 | 12.5 |
| 3900 | 10 | 10000 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 4700 | 10, 20 | 10000 | 35 | 30 | 8 | 1 | A3 or A4 | 20 |
| 5600 | 10 | 10000 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 6800 | 10, 20 | 10000 | 35 | 40 | 8 | 1 | A3 or A4 | 26.5 |
| 8200 | 10 | 10000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 10000 | 10, 20 | 10000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 12000 | 10 | 10000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 15000 | 10, 20 | 10000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 18000 | 10 | 10000 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 22000 | 10, 20 | 10000 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 27000 | 10 | 10000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 33000 | 10, 20 | 10000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 39000 | 10 | 10000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 47000 | 10, 20 | 10000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 56000 | 10 | 10000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 68000 | 10, 20 | 10000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 82000 | 10 | 10000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 100000 | 10, 20 | 10000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 3300 | 10, 20 | 12500 | 61 | 20 | 4 | 1 | A3 or A4 | 14 |
| 3900 | 10 | 12500 | 61 | 22 | 6 | 1 | A3 or A4 | 21 |
| 4700 | 10, 20 | 12500 | 61 | 22 | 6 | 1 | A3 or A4 | 21 |
| 5600 | 10 | 12500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 6800 | 10, 20 | 12500 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 8200 | 10 | 12500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 10000 | 10, 20 | 12500 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 12000 | 10 | 12500 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 15000 | 10, 20 | 12500 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 18000 | 10 | 12500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 22000 | 10, 20 | 12500 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 27000 | 10 | 12500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 33000 | 10, 20 | 12500 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 39000 | 10 | 12500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 47000 | 10, 20 | 12500 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 56000 | 10 | 12500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 68000 | 10, 20 | 12500 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 1500 | 10, 20 | 15000 | 61 | 20 | 4 | 1 | A3 or A4 | 14 |
| 1800 | 10 | 15000 | 61 | 22 | 6 | 1 | A3 or A4 | 21 |
| 2200 | 10, 20 | 15000 | 61 | 22 | 6 | 1 | A3 or A4 | 21 |
| 2700 | 10 | 15000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 3300 | 10, 20 | 15000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 3900 | 10 | 15000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 4700 | 10, 20 | 15000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 5600 | 10 | 15000 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 6800 | 10, 20 | 15000 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 8200 | 10 | 15000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 10000 | 10, 20 | 15000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 12000 | 10 | 15000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 15000 | 10, 20 | 15000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 18000 | 10 | 15000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 22000 | 10, 20 | 15000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 27000 | 10 | 15000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 33000 | 10, 20 | 15000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 680 | 10, 20 | 20000 | 61 | 20 | 4 | 1 | A3 or A4 | 14 |
| 820 | 10 | 20000 | 61 | 22 | 6 | 1 | A3 or A4 | 21 |
| 1000 | 10, 20 | 20000 | 61 | 22 | 6 | 1 | A3 or A4 | 21 |
| 1200 | 10 | 20000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 1500 | 10, 20 | 20000 | 61 | 24 | 8 | 1 | A3 or A4 | 28 |
| 1800 | 10 | 20000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 2200 | 10, 20 | 20000 | 61 | 38 | 8 | 1 | A3 or A4 | 44 |
| 2700 | 10 | 20000 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 3300 | 10, 20 | 20000 | 61 | 45 | 8 | 1 | A3 or A4 | 52 |
| 3900 | 10 | 20000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 4700 | 10, 20 | 20000 | 79 | 45 | 8 | 1.2 | A3 or A4 | 67 |
| 5600 | 10 | 20000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 6800 | 10, 20 | 20000 | 79 | 47 | 10 | 1.2 | A3 or A4 | 85 |
| 8200 | 10 | 20000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 10000 | 10, 20 | 20000 | 105 | 47 | 10 | 1.2 | A3 or A4 | 115 |
| 12000 | 10 | 20000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |
| 15000 | 10, 20 | 20000 | 105 | 50 | 14 | 1.2 | A3 or A4 | 175 |

NOTES:

See Para. 1.6.

Lead material and finishes shall be in accordance with the requirements of ESCC Basic Specification No. 23500.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Rated Voltage | UR | 1500, 2500, 3500, 5000, 7500, 10000, 12500, 15000, 20000 | V | Note 1 |
| Ripple Voltage, peak-to-peak (Note 2) | URip | 0.2×UR 0.15×UR 0.04×UR 0.01×UR | Vpp | At 50Hz At 100Hz At 1000Hz At 10000Hz |
| Operating Air Pressure Range | Pop | Less than 0.1 or greater than 75000 | Pa | Note 3 |
| Operating Temperature Range | Top | -55 to +125 | °C | Without derating. Tamb |
| Storage Temperature Range | Tstg | -55 to +125 | °C |  |
| Soldering Temperature | Tsol | +260 | °C | Note 4 |

NOTES:

As required; See Para. 1.4.2.

Ripple voltage plus applied DC voltage shall never exceed UR.

Components are designed for dielectric fluid use or encapsulation.

Duration 5 seconds maximum at 4mm from the device body and the same terminal shall not be resoldered until 3 minutes have elapsed.

## PHYSICAL DIMENSIONS and terminal identification

NOTES:

The limits of Dimensions L, h, e and ØW are defined in Para. 1.4.2.

The difference between dimensions E and F shall be < 2mm. The difference between dimensions G and H shall be < 1mm.

Terminal identification: A voltage polarity “” symbol shall be marked on the body to indicate the lead which should be connected to the lowest potential.

## FUNCTIONAL DIAGRAM

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Screening Tests (Chart F3)

Rapid Change of Temperature:

Test Condition (d), Exposure time (each cycle, each temperature): 3 hours minimum.

Test Condition (e), Transition time: 1 hour ±5 minutes.

#### Deviations from Qualification and Periodic Tests – Chart F4

Rapid Change of Temperature:

Test Condition (d), Exposure time (each cycle, each temperature): 3 hours minimum.

Test Condition (e), Transition time: 1 hour ±5 minutes.

Vibration:

Test Condition (c), Applied voltage: no voltage shall be applied.

Data Points: no monitoring during the last cycle.

Shock:

Test Condition (d), Applied voltage: no voltage shall be applied.

Data Points: no monitoring during the last cycle.

Climatic Sequence (Damp Heat, Accelerated, First Cycle and Damp Heat, Accelerated, Remaining Cycles): the applied voltage shall be 100V.

Climatic Sequence (Low Air Pressure): For Qualification Testing only, Low Air Pressure shall be performed under the following conditions:

1 hour minimum at 1×10-5 mbar maximum.

Temperature: +50 (+5 -0)°C

Applied voltage: 1.25×UR applied for the last 5 minutes of the period of low pressure.

Operating Life:

Test Condition (c), Applied voltage: 1.15×UR.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and as follows.

The information to be marked on the component shall be:

Terminal Identification (see Para. 1.6).

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number (see Para. 1.4.1).

Traceability information.

## Robustness of terminations

The test conditions for Robustness of Terminations shall be as specified in the ESCC Generic Specification and as follows:

Test Ua1 (tensile):

- Applied force: 20N

- Duration: 10 ±1s

Test Uc Method 1, Severity 2 (torsion, 2 successive rotations of 180°)

Test Ub Method 1 (bending, 2 consecutive bends):

- Applied force: 10N

The number of terminals to be tested is as follows: All terminals for test Ua1; one-half of the terminals for test Uc Method 1, Severity 2; the remaining terminals for test Ub Method 1.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

Electrical measurements shall be performed at room, high and low temperatures.

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | Test Method and Conditions | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Capacitance | C | ESCC No. 3006 | Note 1 | Note 2 | pF |
| Tangent of Loss Angle | tgδ | ESCC No. 3006 VT = 1V Test Frequency = 1kHz | - | 50×10-4 | - |
| Insulation Resistance, Dielectric | RI | ESCC No. 3006 |  |  |  |
|  |  | For C ≤ 220000pF For C > 220000pF | 25 5000 | - - | GΩ GΩ.nF |
| Insulation Resistance, Body Insulation | RIB | ESCC No. 3006 | 25 | - | GΩ |
| Voltage Proof, Terminal-to-Terminal | VP | ESCC No. 3006 (Note 3) | 1.6×UR (Note 4) | - | V |
| Voltage Proof, Terminal-to-Case | VPB | ESCC No. 3006 (Note 3) | 1.6×UR (Note 4) | - | V |
| Partial Discharge (AC) | QAC | IEC 60270 |  |  |  |
|  |  | Vrms = 5%UR Vrms = 10%UR (Note 5) | - - | 0 1000 | pC pC |

NOTES:

Capacitance Value of the component minus the applicable Tolerance (see Para. 1.4.2).

Capacitance Value of the component plus the applicable Tolerance (see Para. 1.4.2).

Voltage application time: 5s

For the applicable Rated Voltage (UR) see Para. 1.4.2.

Partial Discharge shall be measured at two different levels of voltage. For the applicable Rated Voltage (UR) see Para. 1.4.2.

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | Test Method and Conditions (Note 1) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Temperature Coefficient | ΔC/C | ESCC No. 3006 |  |  |  |
|  |  | Tamb = -55 (+3 -0)°C | -3 (Note 2) | - | % |
|  |  | Tamb = +125 (+0 -5)°C | - | +10 (Note 2) | % |
| Insulation Resistance, Dielectric | RI | ESCC No. 3006 Tamb = +125 (+0 -5)°C |  |  |  |
|  |  | For C ≤ 220000pF For C > 220000pF | 250 50 | - - | MΩ GΩ.nF |
| Leakage Current | IL | Tamb = +125 (+0 -5)°C | - | Note 4 | nA |
|  |  | VT = 1×UR (Note 3) |  |  |  |

NOTES:

The measurements shall be performed on a sample of 5 components from each manufacturing lot with 0 failures allowed. In the event of any failure a 100% inspection may be performed.

The Temperature Coefficient limits are with respect to the capacitance at +22 ±2°C (reference point temperature).

For the applicable Rated Voltage (UR) see Para. 1.4.2.

The maximum Leakage Current limit, in nA, is: UR (in V) × C (in pF) / 100000.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

Unless otherwise specified the test methods and test conditions shall be as per the corresponding test defined in Para. 2.4.1, Room Temperature Electrical Measurements.

| Test Reference per ESCC No. 3006 | Characteristics | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Resistance to Soldering Heat |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Note 1 |  | pF |
| Final Measurements | Capacitance | C | Note 1 |  | pF |
|  | Change in Capacitance | ΔC/C | -1 | +1 | % |
|  | Insulation Resistance (Terminal-to-Terminal) | RI |  |  |  |
|  | For C ≤ 220000pF For C > 220000pF |  | Note 1 Note 1 | - - | GΩ GΩ.nF |
|  | Tangent of Loss Angle | tgδ | - | Note 1 | - |
| Temperature Coefficient | Temperature Coefficient (Note 2) | ΔC/C | Note 3 |  | % |
| Rapid Change of Temperature |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Note 1 |  | pF |
| Final Measurements | Capacitance | C | Note 1 |  | pF |
|  | Change in Capacitance | ΔC/C | -1 | +1 | % |
|  | Tangent of Loss Angle | tgδ | - | 60×10-4 | - |
| Climatic Sequence |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Note 1 |  | pF |
| Final Measurements | Capacitance | C | Note 1 |  | pF |
|  | Change in Capacitance | ΔC/C | -3 | +3 | % |
|  | Tangent of Loss Angle | tgδ | - | 60×10-4 | - |
|  | Voltage Proof, Terminal-to-Terminal | VP | 1×UR (Note 4) | - | V |
|  | Voltage Proof, Terminal-to-Case | VPB | 1×UR (Note 4) | - | V |
|  | Insulation Resistance, Dielectric | RI |  |  |  |
|  | For C ≤ 220000pF For C > 220000pF |  | Note 5 Note 5 | - - | GΩ GΩ.nF |
|  | Insulation Resistance, Body Insulation | RIB | 5 | - | GΩ |
|  | Partial Discharge (AC) | QAC |  |  |  |
|  | Vrms = 10%UR |  | - | 2000 | pC |
| Operating Life |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Note 1 |  | pF |
| Intermediate Measurements (1000 hours) | Capacitance | C | Note 1 |  | pF |
|  | Change in Capacitance | ΔC/C | -5 | +5 | % |
| Final Measurements (1000 or 2000 hours) (Note 6) | Capacitance | C | Note 1 |  | pF |
|  | Change in Capacitance | ΔC/C | -5 | +5 | % |
|  | Tangent of Loss Angle | tgδ | - | 60×10-4 | - |
|  | Insulation Resistance, Dielectric | RI |  |  |  |
|  | For C ≤ 220000pF For C > 220000pF |  | Note 5 Note 5 | - - | GΩ GΩ.nF |
|  | Insulation Resistance, Body Insulation | RIB | 5 | - | GΩ |
|  | Partial Discharge (AC) | QAC |  |  | pC |
|  | Vrms = 5%UR Vrms = 10%UR |  | - - | 0 2000 |  |

NOTES:

As specified in Para. 2.4.1.

The test method and test conditions shall be as specified in Para. 2.4.2.

As specified in Para. 2.4.2.

For the applicable Rated Voltage (UR) see Para. 1.4.2.

50% of the limit specified in Para. 2.4.1.

1000 hours is applicable to Periodic Testing for extension of qualification. 2000 hours is applicable to Qualification Testing, and to Periodic Testing for renewal of qualification after lapse.

## BURN-IN conditions

| Characteristics | Symbols | Conditions (Note 1) | Units |
| --- | --- | --- | --- |
| Ambient Temperature | Tamb | +125 (+0 -5) | °C |
| Test Voltage | VT | 1.15×UR (Note 2) | V |

NOTES:

1MΩ resistors shall be connected in series with the components subjected to Burn-in. On completion of Burn-in the components shall be removed from the burn-in chamber and allowed to cool, under normal atmospheric conditions, for recovery for 24 ±2 hours.

For the applicable Rated Voltage (UR) see Para. 1.4.2.