Page 1 of 18

POLYIMIDE INSULATED FINISHED WIRES AND CABLES, LOW FREQUENCY, 600V, -100 TO +200°C

ESCC Detail Specification No. 3901/001

| Issue 3 Draft C | March 2024 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# Legal Disclaimer and Copyright

European Space Agency, Copyright © 2024. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| 1616 | Specification upissued to incorporate changes per DCR. |
| Draft 3A 01/12/23 S.Thacker | Proposed revision based on DCR1616 with modifications; see herein with all proposed changes from issue 2 highlighted yellow. Note: It is usual within ESCC to have a unique ordering code for any available particular specified component option i.e. using a unique ESCC component Number. The proposed modifications to DCR1616 as herein, facilitate component identification, traceability, and reordering of a particular component design option. My proposal also allows any Manufacturer who does not support this new custom colour option to still supply ESCC components without any impacting change. |
| Draft 3B 13/12/23 Draft 3B+ 15/12/23 Draft 3B++ 04/03/24 Draft 3B+++ 06/03/24 S.Thacker | New revision based on modifications proposed by Axon-Cable in email dated 11/12/23 & based around the colour coding already implemented in several 3901/xxx specs (e.g. 3901/012). See herein with all new proposed changes from issue 2 & Draft 3A highlighted blue. Other changes remain highlighted yellow. Draft 3B+: modification to Para. 4.4.6(b) & 4.5.2.2(b) to correct/clarify the 6 available insulation colours Draft 3B++: modification to Paras. 4.4.6(b) & 4.5.2 in response to comments from Draka (highlighted green) Draft 3B+++: modification to Paras. 4.5.1 in response to comments from Axon (highlighted pink) |
| Draft 3C 08/03//24 S.Thacker | New revision based on all modifications per Draft 3B+++ agreed with both supporting Manufacturers Axon-Cable & Prysmian/Draka. See herein with all changes from issue 2 highlighted blue. Note: several additional minor editorial changes are also included for the purposes of consistency & clarification; these are highlighted yellow. |

TABLE OF CONTENTS

1	GENERAL	6

1.1	SCOPE	6

1.2	COMPONENT TYPE VARIANTS	6

1.3	MAXIMUM RATINGS	6

1.4	PARAMETER DERATING INFORMATION	6

1.5	PHYSICAL CHARACTERISTICS	6

1.6	FUNCTIONAL DIAGRAM	6

2	APPLICABLE DOCUMENTS	10

3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	10

4	REQUIREMENTS	10

4.1	GENERAL	10

4.2	DEVIATIONS FROM GENERIC SPECIFICATION	10

4.2.1	Deviations from Special In-process Controls	10

4.2.2	Deviations from Final Production Tests - Chart II	10

4.2.3	Deviations from Burn-in and Electrical Measurements - Chart III	10

4.2.4	Deviations from Qualification Tests - Chart IV	10

4.2.5	Deviations from Lot Acceptance Tests - Chart V	10

4.3	MECHANICAL REQUIREMENTS	11

4.3.1	Dimension Check	11

4.3.2	Weight	11

4.4	MATERIALS AND FINISHES	12

4.4.1	Conductor	12

4.4.2	Finished Wire/Core Insulation	12

4.4.3	Cable  Assembly	12

4.4.4	Shield	13

4.4.5	Jacket	13

4.4.6	Colour Codes	14

4.5	MARKING	14

4.5.1	General	14

4.5.2	The ESCC Component Number	15

4.5.3	Traceability Information	16

4.5.4	Additional Marking	16

4.6	ELECTRICAL MEASUREMENTS	16

4.6.1	Electrical Measurements at Room Temperature	16

4.6.2	Electrical Measurements at High and Low Temperatures	16

4.6.3	Circuits for Electrical Measurements (Figure 4)	16

4.7	BURN-IN TESTS	16

4.8	ENVIRONMENTAL AND ENDURANCE TESTS	16

4.8.1	Mechanical Properties of Conductor	16

4.8.2	Accelerated Ageing	16

4.8.3	Wrap Test at Ambient Temperature	17

4.8.4	Voltage Test	17

4.8.5	Shrinkage	17

4.8.6	Blocking	17

4.8.7	Cold Bend Test	17

4.8.8	Cut-through Resistance	17

4.8.9	Notch Resistance	18

4.8.10	Flammability	18

4.8.11	Resistance to Fluids	18

4.8.12	Surface Resistance	18

4.8.13	Abrasion Resistance	18

4.8.14	Soldering	18

4.8.15	Solderability (applicable to the shield only)	18

4.8.16	Radiation Resistance	18

4.8.17	Overload Resistance	18

4.8.18	Long-term Ageing Test	18

4.8.19	Anthony & Brown Test	18

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, test and inspection data for Polyimide Insulated, Finished Wires and Cables, Low Frequency, 600V, -100°C to +200°C. It shall be read in conjunction with ESCC Generic Specification No. 3901, the requirements of which are supplemented herein.

NOTES:

These finished wires and cables shall not be used in the presence or vicinity of hydrazine or nitrogen tetroxide.

## COMPONENT TYPE VARIANTS

Variants of the basic types of finished wires and cables specified herein, which are also covered by this specification, are listed in Table 1(a).

## MAXIMUM RATINGS

The maximum ratings, applicable to the finished wires and cables specified herein, which shall not be exceeded at any time during use or storage in controlled space environment, are scheduled in Table 1(b).

## PARAMETER DERATING INFORMATION

The derating information applicable to the finished wires and cables specified herein is as follows:

The maximum current for each core used in a cable shall be:

IBmax= Imax × 29 - n28 (for 1 < n < 15)

IBmax = Imax2 for n > 15

where n = number of cores in the cable.

The temperature derating information is shown in Figure 1 with maximum current Imax for a single wire/core.

The derating factors contained herein indicate maximum stress values and do not preclude further derating.

## PHYSICAL CHARACTERISTICS

The physical characteristics of the finished wires and cables specified herein are shown in Figures 2(a), 2(b) and 2(c) and their dimensions in Table 1(a).

## FUNCTIONAL DIAGRAM

Not applicable.

TABLE 1(a) – COMPONENT TYPE VARIANTS

| Variant No. | Shielded | Un-shielded | No. of Cores | Wire Size AWG | Stranding No of Strands × Diameter (mm) | Conductor Characteristics |  |  | Shield Strand Ø (mm) | Core Max Ø (mm) | Finished Wire/Cable |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Max Ø (mm) | Nom Sect. (mm2) | Max Ohmic Resistance (Ω/km) |  |  | Characteristics |  |
|  |  |  |  |  |  |  |  |  |  |  | Max Ø (mm) | Max Weight (kg/km) |
| Variants 01 through 23 deleted, not to be used |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 24 |  | X | 1 | 26 | 19×0.1 (1) | 0.53 | 0.15 | 148 | - | - | 0.84 | 2.05 |
| 25 |  | X | 1 | 24 | 19×0.12 (1) | 0.64 | 0.21 | 105 | - | - | 0.95 | 2.75 |
| 26 |  | X | 1 | 22 | 19×0.16 | 0.85 | 0.38 | 50.9 | - | - | 1.15 | 4.4 |
| 27 |  | X | 1 | 20 | 19×0.2 | 1.04 | 0.6 | 32.2 | - | - | 1.35 | 6.65 |
| 28 |  | X | 1 | 18 | 19×0.25 | 1.29 | 0.93 | 20.6 | - | - | 1.6 | 9.98 |
| 29 |  | X | 1 | 16 | 19×0.3 | 1.53 | 1.3 | 14.3 | - | - | 1.85 | 14 |
| 30 |  | X | 1 | 14 | 27×0.3 | 1.87 | 1.9 | 10.1 | - | - | 2.19 | 19.6 |
| 31 |  | X | 1 | 12 | 45×0.3 | 2.5 | 3.2 | 6.03 | - | - | 2.8 | 32.1 |
| 32 |  | X | 2 | 16 | 19×0.3 | 1.53 | 1.3 | 15 | - | 1.85 | 3.8 | 30.7 |
| 33 |  | X | 2 | 14 | 27×0.3 | 1.87 | 1.9 | 10.6 | - | 2.19 | 4.48 | 43.1 |
| 34 |  | X | 2 | 12 | 45×0.3 | 2.4 | 3.2 | 6.33 | - | 2.8 | 5.7 | 70.6 |
| 35 |  | X | 3 | 16 | 19×0.3 | 1.53 | 1.3 | 15 | - | 1.85 | 4.08 | 46.1 |
| 36 |  | X | 3 | 14 | 27×0.3 | 1.87 | 1.9 | 10.6 | - | 2.19 | 4.82 | 64.6 |
| 37 |  | X | 3 | 12 | 45×0.3 | 2.4 | 3.2 | 6.33 | - | 2.8 | 6.15 | 106 |
| 38 | X |  | 1 | 16 | 19×0.3 | 1.53 | 1.3 | 14.3 | 0.1 | 1.85 | 2.23 | 18.8 |
| 39 | X |  | 1 | 14 | 27×0.3 | 1.87 | 1.9 | 10.1 | 0.12 | 2.19 | 2.63 | 27 |
| 40 | X |  | 1 | 12 | 45×0.3 | 2.4 | 3.2 | 6.03 | 0.15 | 2.8 | 3.3 | 43.3 |
| 41 | X |  | 2 | 16 | 19×0.3 | 1.53 | 1.3 | 15 | 0.15 | 1.85 | 4.26 | 41.8 |
| 42 | X |  | 2 | 14 | 27×0.3 | 1.87 | 1.9 | 10.6 | 0.15 | 2.19 | 5.07 | 55.6 |
| 43 | X |  | 2 | 12 | 45×0.3 | 2.4 | 3.2 | 6.33 | 0.2 | 2.8 | 6.3 | 90.5 |
| 44 | X |  | 3 | 16 | 19×0.3 | 1.53 | 1.3 | 15 | 0.15 | 1.85 | 4.54 | 58.2 |
| 45 | X |  | 3 | 14 | 27×0.3 | 1.87 | 1.9 | 10.6 | 0.2 | 2.19 | 5.4 | 83.3 |
| 46 | X |  | 3 | 12 | 45×0.3 | 2.4 | 3.2 | 6.33 | 0.2 | 2.8 | 6.72 | 127.3 |
| 47 |  | X | 1 | 28 | 19×0.08 (1) | 0.43 | 0.1 | 242 | - | - | 0.73 | 1.37 |

NOTES:

Copper alloy.

TABLE 1(b) – MAXIMUM RATINGS

| No. | Characteristics | Symbol | Maximum Rating | Unit | Remarks |
| --- | --- | --- | --- | --- | --- |
| 1 | Voltage | VP | 600 | Vrms |  |
| 2 | Maximum Current (each finished wire/core) (Note 1) | Imax | 1.5 2.5 3.5 5 7.5 10 13 17 23 | A | For AWG : 28 26 24 22 20 18 16 14 12 |
| 3 | Operating Temperature Range | Tamb | -100 to +200 | °C |  |
| 4 | Storage Temperature Range | Tstg | -100 to +200 | °C |  |

NOTES:

            - The above specified current will generate a temperature rise of approximately 50°C above ambient temperature in a vacuum environment. Precautions shall be taken to prevent the total temperature of the wire (ambient plus rise) exceeding the continuous operating temperature of the wire.

Figure 1 – PARAMETER Derating Information

Figure 2 – Physical CHARACTERISTICS

Dimensions are given in Table 1(a)

FIGURE 2(a) – finished Wire / CORE

FIGURE 2(b) – SHIELDED AND JACKETED CABLES

FIGURE 2(c) – SHIELDED AND JACKETED CABLES

# APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3901, Wires and Cables, Electrical, 600V, Low Frequency.

MIL-DTL-81381, Wire, Electric, Polyimide-Insulated, Copper or Copper Alloy.

# TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 and ESCC Generic Specification No. 3901 shall apply.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the finished wires/cables specified herein are stated in this specification and ESCC Generic Specification No. 3901. Deviations from the Generic Specification, applicable to this specification only, are listed in Para. 4.2.

Deviations from the applicable Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirements and do not affect the components' reliability, are listed in the appendices attached to this specification.

## DEVIATIONS FROM GENERIC SPECIFICATION

### Deviations from Special In-process Controls

None.

### Deviations from Final Production Tests - Chart II

None.

### Deviations from Burn-in and Electrical Measurements - Chart III

Not applicable.

### Deviations from Qualification Tests - Chart IV

Para. 9.21, Resistance to Fluids: 	To be modified as stated in Para. 4.8.11 of this specification.

### Deviations from Lot Acceptance Tests - Chart V

None.

## MECHANICAL REQUIREMENTS

### Dimension Check

The dimensions of the finished wires/cables specified herein shall be checked; they shall conform to those shown in Table 1(a), Figure 2 and Para. 4.4 of this specification (see below for the list of parameters to be checked).

LIST OF PARAMETERS TO BE CHECKED

| Parameter | Table 1(a) | Figure 2 | Para. 4.4 |
| --- | --- | --- | --- |
| COMPOSITION |  |  |  |
| Number of conductors | X |  |  |
| Gauge | X |  |  |
| Shielding | X |  |  |
| Jacket |  | X |  |
| CONDUCTOR |  |  |  |
| Nature |  |  | X |
| Outer diameter | X |  |  |
| Number of strands | X |  |  |
| Strand diameter | X |  |  |
| Length of lay |  |  | X |
| Silver thickness |  |  | X |
| INSULATION |  |  |  |
| Composition and Colour |  | X | X |
| Protective coating |  | X | X |
| Thickness |  |  | X |
| Overlapping |  |  | X |
| Outer diameter | X |  |  |
| SHIELDING |  |  |  |
| Number of strands | X |  |  |
| Type of shielding |  |  | X |
| Strand diameter | X |  |  |
| Nature |  | X | X |
| Silver thickness |  |  | X |
| Shielding lay |  |  | X |
| Shield coverage |  |  | X |
| JACKET |  |  |  |
| Composition and Colour |  | X | X |
| Protective coating |  | X | X |
| Thickness |  |  | X |
| Overlapping |  |  | X |
| Outer diameter | X |  |  |
| Stripe dimensions |  |  | X |

### Weight

The maximum weight of the finished wires/cables specified herein shall be as specified in Table 1(a).

## MATERIALS AND FINISHES

The materials and finishes shall be as specified herein. Where a definite material is not specified, a material which will enable the finished wires/cables specified herein to meet the performance requirements of this specification shall be used. Acceptance or approval of any constituent material does not guarantee acceptance of the finished product.

### Conductor

#### Material Characteristics

All strands used in the manufacture of the conductors shall be silver-coated, soft or annealed, oxygen-free high conductivity copper from AWG 12 to 22 inclusive and silver-coated, high strength copper alloy from AWG 24 to 28. On silver-coated strands, the thickness of the silver shall be 2 microns minimum.

On all copper conductors, any strand shall show a 10% minimum elongation. On all high-strength copper alloy conductors, any strand shall show a 6% minimum elongation at break and a 350N/mm2 minimum tensile strength.

The resistance of the conductors shall be determined at +20°C in accordance with Para. 9.5 of ESCC Generic Specification No. 3901, where the α coefficient for copper alloy is 0.0035.

#### Stranding

The conductors shall be constructed of concentrically laid strands to produce a smooth and uniform conductor of circular cross-section and free from any high strands or other surface irregularities.

The length of the left-hand lay of the external layer shall not be less than 8, nor more than 16 times the maximum conductor diameter specified in Table 1(a).

### Finished Wire/Core Insulation

#### Material

Any insulating material shall be virgin polyimide with only those additives that are necessary for processing and pigmentation.

#### Construction

The insulation shall consist of 2 ribbons wrapped in a reverse way, the overlapping of which shall be equal to, or more than, 51%. Each ribbon (30µm of thickness) shall conform to 0.1/1.0/0.1 type according to MIL-DTL-81381. The insulation shall have a uniform cross-section throughout the length of the finished wire/core and the conductor shall be evenly centred in the insulation. The nominal wall thickness, including the polyimide protective coating, shall be 0.14mm.

#### Insulation Colour

See Paras. 4.4.6.

### Cable 	Assembly

A multicore cable shall be constructed by assembling the cores in a right-hand concentric lay. The length of lay shall not be less than 10, nor more than 14, times the maximum multicore assembly diameter as detailed in Table 1(a).

### Shield

#### Material

Shield strands shall meet the requirements for silver-coated annealed copper as outlined in Para. 4.4.1.1 of this specification.

#### Construction

The shield shall be closely helically wound round the strands and provide not less than 92% coverage, 'K' being calculated by the following formula:

K=n.d L2+P2P.L

where:

K 	= 	% coverage,

n = total number of shield strands,

d 	 = 	mean shield strand diameter,

L 	 = 	apparent shielding lay,

P = 	 	outside perimeter of the shielded cable;

for single core cables, P 	 = 	π(D+d) and for multicore cables, P = 	π(D+d) + xD

- where:

D = 	mean diameter of core insulation,

x = number of cores.

NOTE: The shield may exhibit an occasional gap between strands provided that:

- the coverage coefficient meets the required value.

- the gap width and gap length are no more than 0.5mm and 50mm respectively.

### Jacket

For single-core shielded cables: 2 layers minimum of polyimide tape, type 0.1/1.0/0.1 according to MIL-DTL-81381, coated with pigmented FEP before identification by coloured stripes on the outside.

For multicore shielded cables: 1 layer minimum of polyimide tape, type 0.1/1.0/0.1 according to MIL- DTL-81381, plus 1 layer of coloured PTFE tape with coloured stripes on the outside.

For multicore unshielded cables: 1 layer minimum of polyimide tape, type 0.1/1.0/0.1 according to MIL- DTL-81381, with coloured stripes on the outside.

#### Jacket Colour

Jacket colour: see Para. 4.4.6.

Coloured stripes shall be helically applied on the jacket and grouped in a number equal to that of the quantity of cores. Jacket stripe colour shall be as specified in Para. 4.4.6.

Jacket stripe dimensions shall be as follows:

Stripe width: 0.6mm.

Space between stripes: 1mm.

General tolerance: ±30%.

### Colour Codes

Without Finished Wire/Core Colour Identification (see Para. 4.5.2(a)):

- When the ESCC Component Number, as stipulated in the Purchase Order, does not include a finished wire/core colour identification, the default colour codes for the cable jacket and the jacket stripes as well as all finished wire/cable core(s) insulation shall be as follows:

DEFAULT COLOUR CODING

| Wire Size (AWG) | All Finished Wire/Cable Core(s) Insulation Colour | Cable Jacket Colour |  | Cable Jacket Stripes Colour |
| --- | --- | --- | --- | --- |
|  |  | Polyimide / Unshielded | PTFE or FEP Coating / Shielded |  |
| 28 | Brown | Amber | White | Brown |
| 26 | Black | Amber | White | Black |
| 24 | Khaki-Beige | Amber | Light blue | White |
| 22 | Red | Amber | White | Red |
| 20 | Green | Amber | White | Green |
| 18 | Yellow | Amber | White | Yellow |
| 16 | Brown | Amber | White | Brown |
| 14 | Khaki-Beige | Amber | Light blue | White |
| 12 | Khaki-Beige | Amber | Light blue | White |

With Finished Wire/Core Colour Identification (see Para. 4.5.2(b)):

- When the ESCC Component Number, as stipulated in the Purchase Order, includes a finished wire/core colour identification, the custom colour(s) of the finished wire/cable core(s) insulation shall be as specified by the Orderer in any combination selected from the following 6 available (see Para. 4.5.2.2(b)):

Black, Brown, Red, Yellow, Green, Khaki-Beige

- The colour codes for the cable jacket and the jacket stripes shall be as specified in (a) above.

## MARKING

### General

The marking of all spools of finished wires/cables delivered to this specification shall be in accordance with the requirements of ESCC Basic Specification No. 21700.

Each spool shall be marked in respect of:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number (see Note 1)

Traceability Information.

Additional Marking.

NOTES:

Whenever more than one length of finished wire/cable is wound on a single spool, the full marking for each length including the ESCC Component Numbers shall be marked on the spool. The characteristic code(s) for each length (see Para. 4.5.2.2(a)) may be marked separately on the spool.

### The ESCC Component Number

Each spool shall bear the ESCC Component Number which shall be constituted and marked as follows:

Without finished wire/core colour identification (see Para. 4.4.6(a)):

Example: 390100144B100m

Detail Specification Reference: 3901001

Component Type Variant Number (see Table 1(a)): 44 (as required)

Testing level (B is mandatory): B

Characteristic code: finished wire/cable length: 100m (as required; see Para. 4.5.2.2(a))

With finished wire/core colour identification (see Para. 4.4.6(b)):

Example: 390100144B100m024

Detail Specification Reference: 3901001

Component Type Variant Number (see Table 1(a)): 44 (as required)

Testing level (B is mandatory): B

Characteristic code: finished wire/cable length: 100m (as required; see Para. 4.5.2.2(a))

Characteristic code: finished wire/core colour identification (black, red, yellow): 024 (as required; see Para. 4.5.2.2(b))

#### Characteristics Codes

Characteristics to be codified as part of the ESCC Component Number shall be as follows:

Finished Wire/Cable Length:

- The required length of the finished wire/cable expressed by means of the following codes. The unit quantity shall be metre (m).

| Nominal Length (m) | Code |
| --- | --- |
| X | 00Xm |
| XX | 0XXm |
| XXX | XXXm |

Finished Wire/Core Colour Identification:

- When included as part of the ESCC Component Number, the required custom colour(s) of the finished wire/core(s) insulation expressed by means of up to 3 single digits as follows:

| - No. of Cores | - Code | - Remarks |
| --- | --- | --- |
| - 1 | - X | - See Note 1. Also applies to finished wires |
| - 2 | - XX | - See Note 1 |
| - 3 | - XXX | - See Note 1 |

NOTES:

The individual digits to be used for the 6 available colours are as follows:

| - Black: | 0 |
| --- | --- |
| - Brown: | 1 |
| - Red: | 2 |
| - Yellow: | 4 |
| - Green: | 5 |
| - Khaki-Beige: | 9 |

### Traceability Information

Each spool shall be marked in respect of traceability information in accordance with the requirements of ESCC Basic Specification No. 21700.

### Additional Marking

Each spool shall bear the finished wire/cable manufacturer's Quality Control Inspector's stamp or initials.

## ELECTRICAL MEASUREMENTS

### Electrical Measurements at Room Temperature

The parameters to be measured at room temperature are scheduled in Table 2. The measurements shall be performed at Tamb = +22 ±3°C.

### Electrical Measurements at High and Low Temperatures

Not applicable.

### Circuits for Electrical Measurements (Figure 4)

Not applicable.

## BURN-IN TESTS

Not applicable.

## ENVIRONMENTAL AND ENDURANCE TESTS

### Mechanical Properties of Conductor

As detailed in Para. 4.4.1.1 of this Specification.

### Accelerated Ageing

Ageing Temperature: +230 ±5°C.

The mandrel diameter and appropriate weight used for accelerated age testing of finished wires is given in Table A.

TABLE A – MANDREL DIAMETERS AND LOADS FOR FINISHED WIRES

| Wire Size (AWG) | Mandrel Diameter (mm) | Weight (kg) |
| --- | --- | --- |
| 28 | 6 | 0.125 |
| 26 | 6 | 0.25 |
| 24 | 6 | 0.25 |
| 22 | 6 | 0.4 |
| 20 | 6 | 0.4 |
| 18 | 10 | 0.5 |
| 16 | 10 | 0.5 |
| 14 | 15 | 1 |
| 12 | 20 | 1 |

### Wrap Test at Ambient Temperature

The mandrel diameters and applied loads for wrap testing of finished wires are given in

Table A.

The mandrel diameters and applied loads for cables are given in Table B.

TABLE B – MANDREL DIAMETERS AND LOADS FOR CABLES

| Cable Size (AWG) | Number of Cores | Mandrel Diameter (mm) | Load (kg) |
| --- | --- | --- | --- |
| 16 | 1 | 15 | 0.5 |
| 14 | 1 | 15 | 1 |
| 12 | 1 | 15 | 1 |
| 16 | 2 | 15 | 1 |
| 14 | 2 | 20 | 2 |
| 12 | 2 | 20 | 2 |
| 16 | 3 | 20 | 1.5 |
| 14 | 3 | 20 | 3 |
| 12 | 3 | 25 | 3 |

### Voltage Test

No particular conditions are applicable.

### Shrinkage

The shrinkage temperature shall be +230 ±5°C.

### Blocking

The blocking temperature shall be +200 ±5°C.

### Cold Bend Test

The mandrel diameters and loads shall be as specified in Table C.

TABLE C – MANDREL DIAMETERS AND LOADS FOR FINISHED WIRES/CABLE CORES

| Wire Size (AWG) | Mandrel Diameter (mm) | Weight (kg) |
| --- | --- | --- |
| 28 | 6 | 0.125 |
| 26 | 6 | 0.25 |
| 24 | 6 | 0.25 |
| 22 | 6 | 0.4 |
| 20 | 6 | 0.4 |
| 18 | 10 | 0.5 |
| 16 | 10 | 0.5 |
| 14 | 15 | 1 |
| 12 | 20 | 1 |

### Cut-through Resistance

The mean load measured during the required tests shall not be less than the relevant value specified below:

| Wire Size (AWG) | 28 | 26 | 24 | 22 | 20 | 18 | 16 | 14 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cut-through Load (kg) | 12 | 15 | 17 | 21 | 26 | 34 | 43 | 54 | 66 |

### Notch Resistance

The depth of notch shall be 0.06mm.

### Flammability

No particular conditions are applicable.

### Resistance to Fluids

Tests (e) and (f) shall not be performed.

### Surface Resistance

No particular conditions are applicable.

### Abrasion Resistance

The weight to be applied to the needle is specified below:

| Wire Size (AWG) | 28 | 26 | 24 | 22 | 20 | 18 | 16 | 14 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Scrape Abrasion Load (g) | 500 | 650 | 750 | 800 | 900 | 950 | 1050 | 1100 | 1200 |

### Soldering

No particular conditions are applicable.

### Solderability (applicable to the shield only)

No particular conditions are applicable.

### Radiation Resistance

No particular conditions are applicable.

### Overload Resistance

No particular conditions are applicable.

### Long-term Ageing Test

The long-term ageing temperature shall be +200°C.

### Anthony & Brown Test

No particular conditions are applicable.

TABLE 2 – ELECTRICAL MEASUREMENTS AT ROOM TEMPERATURE

| No. | Characteristics | Spec. and/or Test Method | Test Condition | Limits | Unit |
| --- | --- | --- | --- | --- | --- |
| 1 | Conductor Resistance | ESCC No. 3901, Section 9 | Para. 9.5 | Table 1(a) | Ω/km |
| 2 | Spark Test | ESCC No. 3901, Section 9 | Para. 9.6 Insulation : 3kV Jacket : 1.5kV | Para. 9.6 | - |
| 3 | Voltage Test | ESCC No. 3901, Section 9 | Para. 9.7 | Para. 9.7 | - |
| 4 | Insulation Resistance | ESCC No. 3901, Section 9 | Para. 9.8 | Insulation : ≥ 750 Jacket : ≥ 30 | MΩ.km MΩ.km |
| 5 | Surface Resistance | ESCC No. 3901, Section 9 | Para. 9.22 | > 125 | MΩ.mm |