Page 1 of 15

CAPACITORS, LEADLESS SURFACE MOUNTED, ORGANIC POLYMER TANTALUM, SOLID ELECTROLYTE, ENCLOSED ANODE CONNECTION

BASED ON TYPE TCS

ESCC Detail Specification No. 3012/006

| Issue 6 Draft A | July 2024 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# LEGAL DISCLAIMER AND COPYRIGHT

European Space Agency, Copyright © 2024. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly or indirectly by the use and application of this ESCC publication.

This publication, without the prior permission of the European Space Agency and provided that it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| TBA | Specification upissued to incorporate changes per DCR. |
| Draft 6A S.Thacker 01/07/2024 | DCR per AVX request in email dated 28/06/2024. Changes are highlighted yellow for information. See Paras: 1.4.1.1(c)&(d), 1.4.2, 1.5, 2.4 |

TABLE OF CONTENTS

1	GENERAL	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND Component Type Variants	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants and Range of Components	7

1.5	MAXIMUM RATINGS	8

1.6	PHYSICAL DIMENSIONS and terminal identification	9

1.7	FUNCTIONAL DIAGRAM	9

1.8	Materials and Finishes	10

1.8.1	Terminal Material and Finish	10

2	REQUIREMENTS	10

2.1	GENERAL	10

2.1.1	Deviations from the Generic Specification	10

2.2	MARKING	10

2.3	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	11

2.3.1	Room Temperature Electrical Measurements	11

2.3.2	High and Low Temperatures Electrical Measurements	11

2.4	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	12

APPENDIX A	15

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, and test and inspection data for the component type variants and/or the Component Type Variants and Range of Components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3012.

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND Component Type Variants

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 301200601337MA0015

Detail Specification Reference: 3012006

Component Type Variant Number: 01

Characteristic code: Rated Capacitance (330μF): 337 (as required)

Characteristic code: Capacitance Tolerance (±20%): M

Rating code: DC Rated Voltage (10V): A (as required)

Characteristic code: Maximum Equivalent Series Resistance (15mΩ): 0015

#### Characteristics and Ratings Codes

Characteristics and ratings to be codified as part of the ESCC Component Number shall be as follows:

Rated Capacitance, Cn, expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be picofarad (pF).

| Capacitance Value C (pF) | Code |
| --- | --- |
| XX 106 | XX6 |
| XX 107 | XX7 |

Capacitance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (± %) | Code |
| --- | --- |
| 20 | M |

DC Rated Voltage, UR, expressed by the following codes:

| DC Rated Voltage UR (V) | Code |
| --- | --- |
| 4 | G |
| 6.3 | J |
| 10 | A |
| 16 | C |
| 20 | D |
| 25 | E |
| 35 | V |
| 50 | T |

Equivalent Series Resistance maximum value, ESR, expressed by the following codes. The unit quantity shall be milliohm (mΩ):

| Maximum Equivalent Series Resistance ESR (mΩ) | Code |
| --- | --- |
| XX | 00XX |
| XXX | 0XXX |

### Component Type Variants and Range of Components

The Component Type Variants and Range of Components applicable to this specification are as follows:

| Variant Number | Case Code (Style) (Note 1) | Capacitance Range Cn (µF) (Notes 2, 3) | DC Rated Voltage UR (V) (Note 2) | Maximum Equivalent Series Resistance ESR (mΩ) (Note 2) | Weight Max (g) |
| --- | --- | --- | --- | --- | --- |
| 01 | E (2917) | 15 to 680 | 4 to 50 | 12, 15, 20, 25, 50, 75, 100 | 0.7 |

NOTES:

See Para. 1.6.

The following Rated Capacitance (Cn), DC Rated Voltage (UR) and maximum Equivalent Series Resistance values (ESR) are available for Variant 01 (Case Code: E) (numbers indicate maximum ESR in mΩ):

| Capacitance Cn | DC Rated Voltage UR |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 4V | 6.3V | 10V | 16V | 20V | 25V | 35V | 50V |
| 15µF |  |  |  |  |  |  |  | 100mΩ |
| 22µF |  |  |  |  |  |  | 50mΩ | 75mΩ |
| 33µF |  |  |  |  |  | 50mΩ | 50mΩ |  |
| 47µF |  |  |  |  |  | 50mΩ |  |  |
| 68µF |  |  |  |  | 25mΩ |  |  |  |
| 100µF |  |  |  |  | 25mΩ |  |  |  |
| 150µF |  |  |  | 20mΩ |  |  |  |  |
| 220µF |  |  | 15mΩ | 20mΩ |  |  |  |  |
| 330µF |  | 12mΩ | 15mΩ |  |  |  |  |  |
| 470µF | 12mΩ | 12mΩ |  |  |  |  |  |  |
| 680µF | 12mΩ |  |  |  |  |  |  |  |

The following Capacitance Tolerance is available:

±20% (M)

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| DC Rated Voltage | UR | See Para. 1.4.1.1(c) | V | Note 1 |
| DC Surge Voltage | US | 1.3 x UR | V | Tamb ≤ +85°C |
| DC Category Voltage | UC | 0.8 x UR | V |  |
| Ripple Current | Iripple | See Note 2 | mA | f = 100kHz, Note 3 |
| Operating Temperature Range | Top | -55 to +105 | °C | Tamb |
| Rated Temperature | TR | +85 | °C |  |
| Upper Category Temperature | TC | +105 | °C |  |
| Storage Temperature Range | Tstg | -55 to +105 | °C | Note 4 |
| Soldering Temperature | Tsol | +260 | °C | Notes 4, 5 |

Notes:

            - At Tamb ≤ +85°C. For Tamb > +85°C, derate linearly to UC at Tamb = +105°C.

            - Maximum Iripple, which depends on Cn and UR, shall be as follows at Tamb ≤ +45°C and f = 100kHz:

| Capacitance Cn (µF) | DC Rated Voltage UR (V) | Maximum Ripple Current Iripple (A) |
| --- | --- | --- |
| 15 | 50 | 2 |
| 22 | 35 | 2.9 |
| 22 | 50 | 2.3 |
| 33 | 25 | 2.9 |
| 33 | 35 | 2.9 |
| 47 | 25 | 2.9 |
| 68 | 20 | 4 |
| 100 | 20 | 4 |
| 150 | 16 | 4.5 |
| 220 | 16 | 4.5 |
| 220 | 10 | 5.2 |
| 330 | 10 | 5.2 |
| 330 | 6.3 | 5.8 |
| 470 | 4 | 5.8 |
| 470 | 6.3 | 5.8 |
| 680 | 4 | 5.8 |

            - At Tamb ≤ +45°C. For +45°C < Tamb ≤ +85°C, derate maximum Iripple linearly to 0.7Iripple at Tamb = +85°C. For Tamb > +85°C, derate linearly to 0.47Iripple at Tamb = +105°C.

            - These components are classified as Moisture Sensitivity Level 3 in accordance with J-STD-020. Components shall be delivered in moisture barrier bags with a desiccant and moisture indicator card. Components should be stored still contained within the moisture barrier bags in a non-condensating atmospheric environment of Tamb ≤ +40°C and relative humidity RH ≤ 90%.

- These components have a floor life of 168 hours at Tamb ≤ +30°C and RH ≤ 60%.

            - Duration 5 seconds maximum for wave soldering and 10 seconds maximum for reflow soldering. The solderable area is the terminal pad and up to 1/3 the height of the L-shape terminal (see Para. 1.6).

## PHYSICAL DIMENSIONS and terminal identification

| Variant Number | Case Code | Dimensions (mm) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | L |  | H |  | H1 |  | W |  | W1 |  | A |  | S |  |
|  |  | Min | Max | Min | Max | Min | Max | Min | Max | Min | Max | Min | Max | Min | Max |
| 01 | E | 7.1 | 7.5 | - | 4.3 | 0.7 | - | 4.2 | 4.5 | 2.2 | 2.6 | 1.1 | 1.6 | 4.4 | - |

NOTES:

Terminal identification: The anode terminal shall be indicated by a polarity stripe marked on the top surface of the component. For qualified components, the ESCC qualified components symbol may be used to indicate the anode terminal.

## FUNCTIONAL DIAGRAM

## Materials and Finishes

### Terminal Material and Finish

Terminal material and finish shall be type P17 in accordance with the requirements of ESCC Basic Specification No. 23500.

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Qualification and Periodic Testing - Chart F4

Para. 8.14, Surge Voltage: Data Points: In addition, Capacitance Change shall be measured on completion of testing.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700. The information to be marked shall be:

Terminal Identification (see Para. 1.6).

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number (see Para. 1.4.1).

Traceability information.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

Electrical measurements shall be performed at room, high and low temperatures.

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | Test Method and Conditions | Tolerance | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Capacitance | C | ESCC No. 3012 | ±20% | 0.8Cn | 1.2Cn | µF |
| DC Leakage Current | IL | ESCC No. 3012 | All | - | 0.1Cn x UR | µA |
| Dissipation Factor | DF | ESCC No. 3012 | All | - | 10 | % |
| Equivalent Series Resistance | ESR | ESCC No. 3012 | All | - | Note 1 | mΩ |

NOTES:

See Para. 1.4.2, Note 2.

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | Test Method and Conditions (Note 1) | Tolerance | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Capacitance | C | ESCC No. 3012 |  |  |  | µF |
|  |  | Tamb = -55 (+3 -0)°C: | ±20% | 0.64Cn | 1.2Cn |  |
|  |  | Tamb = +85 ±3°C: | ±20% | 0.8Cn | 1.44Cn |  |
|  |  | Tamb = +105 (+0 -3)°C: | ±20% | 0.8Cn | 1.56Cn |  |
| DC Leakage Current | IL | ESCC No. 3012 | All |  |  | µA |
|  |  | Tamb = +85 ±3°C, V = UR ±2%: |  | - | Cn x UR |  |
|  |  | Tamb = +105 (+0 -3)°C, V = UC ±2%: |  | - | Cn x Uc |  |
| Dissipation Factor | DF | ESCC No. 3012 | All |  |  | % |
|  |  | Tamb = -55 (+3 -0)°C For UR < 10V: For UR ≥ 10V: |  | - - | 15 9 |  |
|  |  | Tamb = +85 ±3°C For UR < 10V: For UR ≥ 10V: |  | - - | 15 9 |  |
|  |  | Tamb = +105 (+0 -3)°C For UR < 10V: For UR ≥ 10V: |  | - - | 20 12 |  |
| Equivalent Series Resistance | ESR | ESCC No. 3012 | All |  |  | % |
|  |  | Tamb = -55 (+3 -0)°C: |  | - | Note 3 |  |
|  |  | Tamb = +85 ±3°C: |  | - | Note 4 |  |
|  |  | Tamb = +105 (+0 -3)°C: |  | - | Note 4 |  |

NOTES:

            - Measurements shall be performed on a sample of 5 components from each manufacturing lot and each capacitance value with 0 failures allowed. In the event of any failure a 100% inspection may be performed.

            - Whichever is greater.

            - 2.5× the limit specified in Para. 2.3.1.

            - 1.5× the limit specified in Para. 2.3.1.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

Unless otherwise specified the test methods and test conditions shall be as per the corresponding test defined in Para. 2.3.1 Room Temperature Electrical Measurements.

| Test Reference per ESCC No. 3012 | Characteristics | Symbols | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Mounting |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Note 1 |  | µF |
| Final Measurements | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -5 | +5 | % |
|  | DC Leakage Current | IL | Note 1 |  | µA |
|  | Dissipation Factor | DF | Note 1 |  | % |
|  | Equivalent Series Resistance | ESR | Note 2 |  | mΩ |
| Robustness of Terminations |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Record Value, Note 3 |  | µF |
| Final Measurements | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -10 | +10 | % (3) |
| Rapid Change of Temperature |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Record Value, Note 3 |  | µF |
| Final Measurements | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -20 | +20 | % (3) |
|  | DC Leakage Current | IL | Note 1 |  | µA |
|  | Dissipation Factor | DF | Note 1 |  | % |
|  | Equivalent Series Resistance | ESR | Note 4 |  | mΩ |
| Vibration |  |  |  |  |  |
| During Last Sweep Cycle | No intermittent contact ≥ 0.5ms, arcing, or open/short circuits | - | - | - | - |
| Climatic Sequence |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Record Value, Note 3 |  | µF |
| Dry Heat | DC Leakage Current (at +125°C; UC) | IL | - Note 5 |  | µA |
| Final Measurements | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -5 | +5 | % (3) |
|  | DC Leakage Current | IL | Note 1 |  | µA |
|  | Dissipation Factor | DF | Note 6 |  | % |
|  | Equivalent Series Resistance | ESR | Note 6 |  | mΩ |
| High and Low Temperature Stability |  |  |  |  |  |
| Step 1 (at +22°C) | Capacitance | C | Record Value, Note 3 |  | µF |
|  | DC Leakage Current | IL | Notes 1, 3 |  | µA |
|  | Dissipation Factor | DF | Notes 1, 3 |  | % |
|  | Equivalent Series Resistance | ESR | Notes 2, 3 |  | mΩ |
| Step 2 (at -55°C) | Capacitance | C | Note 5 |  | µF |
|  | DC Leakage Current | IL | Note 5 |  | µA |
|  | Dissipation Factor | DF | Note 5 |  | % |
|  | Equivalent Series Resistance | ESR | Note 5 |  | mΩ |
| Step 3 (at +22°C) | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change from Step 1 | ΔC/C | -5 | +5 | % |
|  | DC Leakage Current | IL | Note 1 |  | µA |
|  | Dissipation Factor | DF | Note 1 |  | % |
|  | Equivalent Series Resistance | ESR | Note 2 |  | mΩ |
| Step 4 (at +85°C) | Capacitance | C | Note 5 |  | µF |
|  | DC Leakage Current | IL | Note 5 |  | µA |
|  | Dissipation Factor | DF | Note 5 |  | % |
|  | Equivalent Series Resistance | ESR | Note 5 |  | mΩ |
| Step 5 (at +125°C) | Capacitance | C | Note 5 |  | µF |
|  | DC Leakage Current | IL | Note 5 |  | µA |
|  | Dissipation Factor | DF | Note 5 |  | % |
|  | Equivalent Series Resistance | ESR | Note 5 |  | mΩ |
| Step 6 (at +22°C) | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change from Step 1 | ΔC/C | -5 | +5 | % |
|  | DC Leakage Current | IL | Note 1 |  | µA |
|  | Dissipation Factor | DF | Note 1 |  | % |
|  | Equivalent Series Resistance | ESR | Note 2 |  | mΩ |
| Surge Voltage |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Record Value, Note 3 |  | µF |
| Final Measurements | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -30 | +20 | % (3) |
|  | DC Leakage Current | IL | Note 1 |  | µA |
|  | Dissipation Factor | DF | Note 2 |  | % |
|  | Equivalent Series Resistance | ESR | Note 2 |  | mΩ |
| Damp Heat, Steady State |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Record Value, Note 3 |  | µF |
| Final Measurements | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -5 | +35 | % (3) |
|  | DC Leakage Current | IL | Note 4 |  | µA |
|  | Dissipation Factor | DF | Note 6 |  | % |
|  | Equivalent Series Resistance | ESR | Note 6 |  | mΩ |
| Operating Life |  |  |  |  |  |
| Initial Measurements | Capacitance | C | Record Value, Note 3 |  | µF |
| Intermediate Measurements (250h and 1000h)(Note 8) | DC Leakage Current (at T1 = +85°C) | IL | Note 7 |  | µA |
|  | DC Leakage Current (at T2 = +125°C) | IL | Note 7 |  | µA |
| Intermediate Measurements (250h)(Note 9) | DC Leakage Current (at T1 = +85°C) | IL | Note 7 |  | µA |
| Final Measurements (1000h or 2000h)(Note 10) | Capacitance | C | Record Value |  | µF |
|  | Capacitance Change | ΔC/C | -20 | +10 | % (3) |
|  | DC Leakage Current | IL | Note 2 |  | µA |
|  | Dissipation Factor | DF | Note 1 |  | % |
|  | Equivalent Series Resistance | ESR | Note 6 |  | mΩ |

NOTES:

As specified in Para. 2.3.1.

1.25× the limit specified in Para. 2.3.1.

Component characteristic measurements (as applicable) recorded during the final measurements during Mounting may be used for this test. In this case, Capacitance Change for this test shall be referred to the final Capacitance measurement during Mounting.

5× the limit specified in Para. 2.3.1.

As specified in Para. 2.3.2.

2× the limit specified in Para. 2.3.1.

1.25× the limit specified in Para. 2.3.2.

Applicable to Qualification Testing, and to Periodic Testing for renewal of qualification after lapse.

Applicable to Periodic Testing for extension of qualification.

1000 hours is applicable to Periodic Testing for extension of qualification. 2000 hours is applicable to Qualification Testing, and to Periodic Testing for renewal of qualification after lapse.

## APPENDIX A

Agreed Deviations for KYOCERA AVX Components s.r.o. (CZ)

| Items Affected | Description of Deviations |
| --- | --- |
| Para. 2.1.1, Deviations from the Generic Specification: Deviations from Special In-Process Controls - Chart F2 | Internal Visual Inspection: Need not be performed immediately prior to encapsulation but may be performed at various stages during production, as specified in the PID. |
| Para. 2.1.1, Deviations from the Generic Specification: Deviations from Screening Tests - Chart F3, Deviations from Qualification and Periodic Testing - Chart F4 | External Visual Inspection: Visible base material is permitted on the edges of terminals (there may be no plating on edges). |