Page 1 of 12

CAPACITORS, FIXED, CHIPS, CERAMIC DIELECTRIC, TYPE I N2200

BASED ON TYPES 0603 to 1210

ESCC Detail Specification No. 265 (3009/xxx)

| Issue 1 Draft C | January 2019 |
| --- | --- |

Document Custodian: European Space Agency – see https://escies.org

# LEGAL DISCLAIMER AND COPYRIGHT

European Space Agency, Copyright © 2019. All rights reserved.

The European Space Agency disclaims any liability or responsibility, to any person or entity, with respect to any loss or damage caused, or alleged to be caused, directly by the use and application of this ESCC publication.

This publication, without prior permission of the European Space Agency and provided it is not used for a commercial purpose, may be:

copied in whole, in any medium, without alteration or modification.

copied in part, in any medium, provided that the ESCC document identification, comprising the ESCC symbol, document number and document issue, is removed.

# DOCUMENTATION CHANGE NOTICE

(Refer to https://escies.org for ESCC DCR content)

| DCR No. | CHANGE DESCRIPTION |
| --- | --- |
| Draft 1B S.Thacker 13/12/18 | Initial draft ESCC detail spec based on Exxelia draft first issue “3009/xxx” dated November 2018. Comments/questions are included in the review margin for Exxelia’s response. |
| Draft 1C S.Thacker 02/1/19 | New revision draft ESCC detail spec that implements changes resulting from Exxelia’s review comment dated 17/12/18 Comments are included in the review margin for Exxelia’s response. Change from the previous revision are highlighted yellow |
| Draft 1D S.Thacker 14/1/19 | Copy of Draft 1B as agreed by Exxelia 11/01/19, with all highlights and comments removed, submitted for ESA publishing review. |

TABLE OF CONTENTS

1	GENERAL	5

1.1	SCOPE	5

1.2	APPLICABLE DOCUMENTS	5

1.3	TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS	5

1.4	THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS	5

1.4.1	The ESCC Component Number	5

1.4.2	Component Type Variants and Range of Components	6

1.5	MAXIMUM RATINGS	7

1.6	PHYSICAL DIMENSIONS	8

1.7	FUNCTIONAL DIAGRAM	8

2	REQUIREMENTS	8

2.1	GENERAL	8

2.1.1	Deviations from the Generic Specification	8

2.2	MARKING	9

2.3	ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES	9

2.3.1	Room Temperature Electrical Measurements	9

2.3.2	High and Low Temperatures Electrical Measurements	10

2.4	INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS	10

2.5	BURN-IN	12

# GENERAL

## SCOPE

This specification details the ratings, physical and electrical characteristics, and test and inspection data for the component type variants and/or the range of components specified below. It supplements the requirements of, and shall be read in conjunction with, the ESCC Generic Specification listed under Applicable Documents.

## APPLICABLE DOCUMENTS

The following documents form part of this specification and shall be read in conjunction with it:

ESCC Generic Specification No. 3009.

## TERMS, DEFINITIONS, ABBREVIATIONS, SYMBOLS AND UNITS

For the purpose of this specification, the terms, definitions, abbreviations, symbols and units specified in ESCC Basic Specification No. 21300 shall apply.

## THE ESCC COMPONENT NUMBER AND COMPONENT TYPE VARIANTS

### The ESCC Component Number

The ESCC Component Number shall be constituted as follows:

Example: 3009xxx011001KE

Detail Specification Reference: 3009006

Component Type Variant Number: 01 (as required)

Characteristic code: Capacitance Value (1000pF): 1001 (as required)

Characteristic code: Capacitance Tolerance (±10%): K (as required)

Rating code: Rated Voltage (100V): A (as required)

#### Characteristics and Ratings Codes

Characteristics and ratings to be codified as part of the ESCC Component Number shall be as follows:

Rated Capacitance Value, Cn, expressed by means of the following codes in accordance with ESCC Basic Specification No. 21700. The unit quantity shall be picofarad (pF).

| Capacitance Value Cn (pF) | Code |
| --- | --- |
| XXX | XXX0 |
| XXX 101 | XXX1 |
| XXX 102 | XXX2 |

Capacitance Tolerance expressed by the following codes in accordance with ESCC Basic Specification No. 21700:

| Tolerance (±) | Code Letter |
| --- | --- |
| 5% | J |
| 10% | K |
| 20% | M |

Rated Voltage, UR, expressed by the following codes:

| Rated Voltage UR (V) | Code Letter |
| --- | --- |
| 100 | E |
| 200 | G |
| 500 | L |
| 1000 | M |

### Component Type Variants and Range of Components

The component type variants and range of components applicable to this specification are as follows:

| Variant Number | Style | Capacitance Range, Tolerance, Rated Voltage | Terminal Material and Finish |  | Weight Max (g) |
| --- | --- | --- | --- | --- | --- |
|  |  |  | End Terminations | Termination Finish |  |
| 01 | 0603 | See Note 1 | Ag/Pd/Pt | No finish (Note 2) | 0.15 |
| 02 | 0603 | See Note 1 | Ag + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 03 | 0603 | See Note 1 | Ag + Ni barrier | Au plating (Note 2) | 0.15 |
| 04 | 0603 | See Note 1 | Ag + Ag polymer + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 05 | 0603 | See Note 1 | Ag + Ag polymer + Ni barrier | Au plating (Note 2) | 0.15 |
| 06 | 0805 | See Note 1 | Ag/Pd/Pt | No finish (Note 2) | 0.15 |
| 07 | 0805 | See Note 1 | Ag + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 08 | 0805 | See Note 1 | Ag + Ni barrier | Au plating (Note 2) | 0.15 |
| 09 | 0805 | See Note 1 | Ag + Ag polymer + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 10 | 0805 | See Note 1 | Ag + Ag polymer + Ni barrier | Au plating (Note 2) | 0.15 |
| 11 | 1206 | See Note 1 | Ag/Pd/Pt | No finish (Note 2) | 0.15 |
| 12 | 1206 | See Note 1 | Ag + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 13 | 1206 | See Note 1 | Ag + Ni barrier | Au plating (Note 2) | 0.15 |
| 14 | 1206 | See Note 1 | Ag + Ag polymer + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 15 | 1206 | See Note 1 | Ag + Ag polymer + Ni barrier | Au plating (Note 2) | 0.15 |
| 16 | 1210 | See Note 1 | Ag/Pd/Pt | No finish (Note 2) | 0.15 |
| 17 | 1210 | See Note 1 | Ag + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 18 | 1210 | See Note 1 | Ag + Ni barrier | Au plating (Note 2) | 0.15 |
| 19 | 1210 | See Note 1 | Ag + Ag polymer + Ni barrier | Sn/Pb plating (Note 3) | 0.15 |
| 20 | 1210 | See Note 1 | Ag + Ag polymer + Ni barrier | Au plating (Note 2) | 0.15 |

NOTES:

Available capacitance values, tolerances and rated voltages are as follows:

| Variant Number (Style) | Capacitance Range Cn (pF) |  | Tolerance (Value Series) (± %) | Rated Voltage UR (V) |
| --- | --- | --- | --- | --- |
|  | Min | Max |  |  |
| 01 to 05 (0603) | 100 | 1000 | 5 (E24) 10 (E12) 20 (E6) | 200 |
|  | 1200 | 4700 |  | 100 |
| 06 to 10 (0805) | 100 | 330 |  | 1000 |
|  | 390 | 820 |  | 500 |
|  | 1000 | 3300 |  | 200 |
|  | 3900 | 12000 |  | 100 |
| 11 to 15 (1206) | 100 | 1200 |  | 1000 |
|  | 1500 | 2700 |  | 500 |
|  | 3300 | 10000 |  | 200 |
|  | 12000 | 39000 |  | 100 |
| 16 to 20 (1210) | 100 | 2200 |  | 1000 |
|  | 2700 | 5600 |  | 500 |
|  | 6800 | 22000 |  | 200 |
|  | 27000 | 68000 |  | 100 |

- Any capacitance value within the capacitance range specified for each rated voltage may be available on request.

Variants 01, 03, 05, 06, 08, 10, 11, 13, 15, 16, 18, 20 are not suitable for solder assembly methods. They shall be assembled using glue or wire bond techniques.

Sn/Pb plating with minimum 10% Pb.

## MAXIMUM RATINGS

The maximum ratings shall not be exceeded at any time during use or storage.

Maximum ratings shall only be exceeded during testing to the extent specified in this specification and when stipulated in Test Methods and Procedures of the ESCC Generic Specification.

| Characteristics | Symbols | Maximum Ratings | Units | Remarks |
| --- | --- | --- | --- | --- |
| Rated Voltage | UR | 100, 200, 500, 1000 | V | Note 1 |
| Operating Temperature Range | Top | -55 to +125 | °C | Without derating. Tamb |
| Storage Temperature Range | Tstg | -55 to +125 | °C |  |
| Soldering Temperature | Tsol | +260 | °C | Note 2 |

NOTES:

As required; See Para. 1.4.2.

Duration 10 seconds maximum.

## PHYSICAL DIMENSIONS

| Symbols | Dimensions (mm) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Variants 01, 02, 03, 04, 05 |  | Variants 06, 07, 08, 09, 10 |  | Variants 11, 12, 13, 14, 15 |  | Variants 16, 17, 18, 19, 20 |  |
|  | Style 0603 |  | Style 0805 |  | Style 1206 |  | Style 1210 |  |
|  | Min | Max | Min | Max | Min | Max | Min | Max |
| L | 1.45 | 1.75 | 1.7 | 2.3 | 2.95 | 3.45 | 2.8 | 3.6 |
| l | 0.65 | 0.95 | 1.05 | 1.45 | 1.45 | 1.75 | 2.2 | 2.8 |
| e | - | 1 | - | 1.3 | - | 1.6 | - | 1.8 |
| M | 0.1 | 0.5 | 0.1 | 0.75 | 0.2 | 0.75 | 0.2 | 1 |

## FUNCTIONAL DIAGRAM

# REQUIREMENTS

## GENERAL

The complete requirements for procurement of the components specified herein are as stated in this specification and the ESCC Generic Specification. Permitted deviations from the Generic Specification, applicable to this specification only, are listed below.

Permitted deviations from the Generic Specification and this Detail Specification, formally agreed with specific Manufacturers on the basis that the alternative requirements are equivalent to the ESCC requirement and do not affect the component’s reliability, are listed in the appendices attached to this specification.

### Deviations from the Generic Specification

#### Deviations from Qualification and Periodic Tests - Chart F4

Solderability: not applicable to Variants 01, 03, 05, 06, 08, 10, 11, 13, 15, 16, 18, 20.

## MARKING

The marking shall be in accordance with the requirements of ESCC Basic Specification No. 21700 and as follows.

The information to be marked on the component or its primary package shall be:

The ESCC qualified components symbol (for ESCC qualified components only).

The ESCC Component Number (see Para. 1.4.1).

Traceability information.

## ELECTRICAL MEASUREMENTS AT ROOM, HIGH AND LOW TEMPERATURES

Electrical measurements shall be performed at room, high and low temperatures.

### Room Temperature Electrical Measurements

The measurements shall be performed at Tamb = +22 ±3°C.

| Characteristics | Symbols | Test Method and Conditions | Tolerance (± %) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Min | Max |  |
| Capacitance | CA | ESCC No. 3009 |  |  |  | pF |
|  |  |  | 5 | 0.95Cn | 1.05Cn |  |
|  |  |  | 10 | 0.9Cn | 1.1Cn |  |
|  |  |  | 20 | 0.8Cn | 1.2Cn |  |
| Tangent of Loss Angle | tgδ | ESCC No. 3009 | All | - | 15 x10-4 | - |
| Insulation Resistance | RI | ESCC No. 3009 | All |  |  |  |
|  |  | For Cn ≤ 25000pF |  | 20 | - | GΩ |
|  |  | For Cn > 25000pF |  | 500 | - | GΩ.nF |
| Voltage Proof | VP | ESCC No. 3009 | All |  |  | V |
|  |  | For UR < 500V |  | 2.5UR | - |  |
|  |  | For UR = 500V |  | 2UR | - |  |
|  |  | For UR > 500V |  | 1.5UR | - |  |

### High and Low Temperatures Electrical Measurements

| Characteristics | Symbols | Test Method and Conditions (Note 1) | Limits |  | Units |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |
| Insulation Resistance | RI | ESCC No. 3009 Tamb = +125 ±2°C Note 2 |  |  |  |
|  |  | For Cn ≤ 25000pF | 2 | - | GΩ |
|  |  | For Cn > 25000pF | 50 | - | GΩ.nF |
| Temperature Coefficient | TC | ESCC No. 3009 Tamb = -55 ±2°C, +20 ±2°C, +125 ±2°C Note 3 | -2700 | +2700 | 10-6/°C |

NOTES:

The measurements shall be performed on a sample of 5 components from each manufacturing lot with 0 failures allowed. In the event of any failure a 100% inspection may be performed.

Guaranteed but not tested during Chart F3 of the Generic Specification; only tested in Temperature Characterisation during Chart F4 of the Generic Specification.

In the case of a 100% inspection, a 1% total percent defective is allowed.

## INTERMEDIATE AND END-POINT ELECTRICAL MEASUREMENTS

Unless otherwise specified, the measurements shall be performed at Tamb = +22 ±3°C.

Unless otherwise specified the test methods and test conditions shall be as per the corresponding test defined in Para. 2.3.1 Room Temperature Electrical Measurements.

| Test Reference per ESCC No. 3009 | Characteristics | Symbols | Limits |  |  | Units |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Min | Max |  |  |
| Mounting |  |  |  |  |  |  |
| Final Measurements | Capacitance | CA | Record Values |  |  |  |
|  | Tangent of Loss Angle | tgδ | - |  | 15 x10-4 | - |
|  | Insulation Resistance | RI | Note 1 |  |  |  |
| Rapid Change of Temperature |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Notes 1, 2 |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -3 |  | +3 | % |
|  | Tangent of Loss Angle | tgδ | - |  | 30 x10-4 | - |
| Steady State Humidity (85/85) |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Note 1 |  |  |  |
| Final Measurements (1000 hours) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -3 |  | +3 | % |
|  | Tangent of Loss Angle | tgδ | - |  | 30 x10-4 | - |
|  | Insulation Resistance (Note 3): |  |  |  |  |  |
|  | For Cn ≤ 25000pF | RI | 2 |  | - | GΩ |
|  | For Cn > 25000pF | RI | 50 |  | - | GΩ.nF |
| Operating Life |  |  |  |  |  |  |
| Initial Measurements | Capacitance | CA | Notes 1, 2 |  |  |  |
| Intermediate Measurements (1000 hours) (Note 4) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -3 |  | +3 | % |
|  | Insulation Resistance: |  |  |  |  |  |
|  | For Cn ≤ 25000pF | RI | 2 |  | - | GΩ |
|  | For Cn > 25000pF | RI | 50 |  | - | GΩ.nF |
| Final Measurements (1000 or 2000 hours) (Note 5) | Capacitance | CA | Note 1 |  |  |  |
|  | Change in Capacitance | ΔCA/CA | -3 |  | +3 | % |
|  | Tangent of Loss Angle | tgδ | - |  | 30 x10-4 | - |
|  | Insulation Resistance: |  |  |  |  |  |
|  | For Cn ≤ 25000pF | RI | 2 |  | - | GΩ |
|  | For Cn > 25000pF | RI | 50 |  | - | GΩ.nF |
|  | Voltage Proof | VP | Note 1 |  |  | V |
| Temperature Characterisation | Insulation Resistance at Tamb = +125 ±2°C | RI | Note 6 |  |  |  |
|  | Temperature Coefficient | TC | Note 6 |  |  |  |
| Robustness of Terminations |  |  |  |  |  |  |
| Final Measurements | Capacitance | CA | Note 1 |  |  |  |

NOTES:

As specified in Para. 2.3.1 Room Temperature Electrical Measurements.

Capacitance values recorded during Mounting may be used as initial measurements.

Test conditions for Insulation Resistance shall be as specified in Steady State Humidity in the ESCC Generic Specification.

Intermediate measurements are optional at the Manufacturer’s discretion.

1000 hours is applicable to Periodic Testing for extension of qualification. 2000 hours is applicable to Qualification Testing, and to Periodic Testing for renewal of qualification after lapse.

As specified in Para. 2.3.2 High and Low Temperatures Electrical Measurements.

## BURN-IN

The requirements for Burn-in are specified in the ESCC Generic Specification. The following conditions shall also apply:

After Burn-in, the components shall be removed from the chamber and allowed to cool under normal atmospheric conditions for recovery for 24 hours minimum.